Structural Changes in Basalt Fiber Reinforced Concrete Under Load

Jasurbek Ergashov1, a), Rakhimbay Yusupov1, b), Durdona Usmanova1, c), 
Dilsoz Samadova1, d) and Aliaskar Azimov1, e)

1Tashkent University of Architecture and Civil Engineering, 9 Yangi Shahar Street, Tashkent 100011, Uzbekistan

a) Corresponding author: jasurbek_1711@mail.ru
b) raximbay1951@gmail.com
c) durdonanurzod17@gmail.com
d) d.asatullayevna0412@gmail.com
e) aliaskar_1994@gmail.com

Abstract. The results of experimental studies aimed at determining the parametric levels of crack formation and the nature of destruction in basalt fiber reinforced concrete (BFRC) are presented. The technology is based on the preliminary mixing of basalt fibers with coarse aggregate. Practical application of this technology has shown positive results in ensuring uniform distribution of basalt fibers throughout the concrete volume.

Based on statistical data processing, a correlation relationship is proposed for the calculated assessment of parametric levels of crack formation in BFRC, which largely influence its other characteristics.

Keywords: basalt fiber reinforced concrete, strength, deformability, crack formation, composition, loading, destruction, results.

INTRODUCTION

In the field of modern construction in recent years, there has been a tendency to use dispersed reinforced concrete with various fibers, of which basalt fibers based on local raw materials can be distinguished.

The use of basalt fiber concretes is difficult due to the lack of an affordable and reliable technology for producing such concretes with stable properties, as well as insufficient knowledge of the issues of cracking and the nature of their destruction under the action of a short-term axial compressive load.

The use of basalt fibers in the dispersed reinforcement of concrete makes it possible not only to increase the strength indicators, but also to significantly improve its deformative characteristics (extreme deformations under compression and tension, initial modulus of elasticity, etc.).

According to [1], the stress-strain diagram for basalt fiber concrete has a common character with ordinary concrete and due to the development of structural defects They are nonlinear, containing pronounced nonlinear ascending and descending sections.

Crack resistance is a complex property of concrete, which is determined by the microcracking of its structure under the influence of external stress and environmental parameters, and depends on many factors, including the type of concrete. In this regard, there is every reason to believe that for basalt fiber concrete, the determining factor of its crack resistance is the tensile strength and ultimate extensibility.

The results of many experimental and theoretical studies of crack resistance of heavy concretes without additives of optimal compounds recommend their use in certain areas of construction. However, there are currently many examples of successful applications of other types of concrete, such as concrete with dispersed reinforcement. The emergence of improved conditions in the structure of such concretes for resistance to external loads is important for the development and implementation of innovative technologies based on the inclusion of basalt fiber for reinforcement in concrete.

It is known that constantly changing loads lead to an increase in microcracks and their growth to macro-cracks, which are foci of concrete destruction. The presence of dispersed concrete reinforcement creates conditions for increasing the resistance to shrinkage deformations, which usually lead to cracks in concrete without additives that violate the integrity of reinforced concrete structures. Concrete reinforced with basalt fiber, according to experimental studies, has improved physical and technical properties, which is the basis for expanding its fields of application. In this regard, conducting additional targeted research on the crack resistance of basalt fiber concrete is relevant and in demand.

LITERATURE SURVEY

Structural Changes in Basalt Fiber Reinforced Concrete Under Load approaches into three main methods: analytical and numerical method, strengthening and mounting methods, preparation method of concrete mixes: as discussed below.

- Analytical and numerical methods: A method has been developed for calculating the strength and crack resistance of conventional and prestressed bendable BFСGCF elements under short-term dynamic loading, which is based on the theory of areas of relative resistance of such elements in terms of strength and crack resistance and implements a nonlinear deformation model taking into account real material deformation diagrams. This method makes it possible to evaluate the VAT of such elements in numerical and graphical form with a high degree of reliability, as well as to solve problems of a research and applied nature [1].

- Strengthening and mounting methods: In the study herein, the applicability of the basalt fiber as a strengthening material was investigated through various experimental works for durability, mechanical characteristics and strengthening effects. The basalt fiber manufactured in Russia exhibited the tensile strength less than 1000 MPa, which was about 30% of the carbon and 60% of the high strength glass (S-glass) fiber. [2].

- The preparation method of concrete mixes: Technological recommendations have been developed that allow for further improvement of the compositions of other concretes and the development of the production of basalt-fiber concrete based on local materials. [3] Also, the technical and technological advantages inherent in basalt-fiber concrete provide a basis to continue research with the aim of using basalt fiber for reinforcement in load-bearing concrete and reinforced concrete structures.

- Experimental method: The given technique has demonstrated that the study findings concerning the mechanical-and-physical properties of re-enforcing polymeric composites are revealed. [4] Besides, the values of the principal strength and deformation characteristics are determined experimentally with respect to glass fiber-reinforced (GFRP) and carbon reinforced polymers (CFRP) with the static axial loading conditions in tension and compression. This paper estimates the resistance of GFRP and CFRP bars in the alkaline medium. The deformation diagram is created in GFRP bars and CFRP with the application of the static loads. The estimated coefficients are proposed towards strengthening of reinforcement dynamically under the dynamic load.

- Methods for designing: This method is showed clearly the means and methods for designing, producing and using high-strength concrete. [5]

- Experimental method: This method has shown that the addition of fiber contributes more to the strength of less durable concretes. [6] For high-strength concretes, the positive effect of adding fiber is reduced, but it is also observed.

MATERIALS AND RESEARCH METHODOLOGY

Granite crushed stone from the Kuyluk quarry with a maximum size of 20 mm was used as a coarse aggregate. The fine aggregate was river sand with a grain size modulus of 2.39. Coarse and fine aggregates meet the requirements of the relevant standards in their properties.

Concrete mixtures with a mobility of 5-6 cm were placed in metal molds and compacted on a laboratory vibrating table with an oscillation frequency of 3000 rpm and an amplitude of 0.5 mm.

For the production of prototypes of cubes and prisms, two series of concrete and basalt-fiber concrete mixtures were used with a consumption of Portland cement grade 400, respectively, 425 and 530 kg/m3. The consumption of locally produced basalt fibers was assumed to be 1% of the binder consumption per m3 of concrete mixture.

The samples hardened in molds during the day, and after demolding, they were stored in laboratory conditions where the temperature was 20 ± 2 C and humidity was 70 ± 5%.

To prepare a basalt-fiber-concrete mixture, a method of pre-mixing a 50% amount of crushed stone with basalt fiber in 3-4 portions in a gravity concrete mixer was used [2].

To study and compare the strength and deformation characteristics of basalt fiber concrete and ordinary concrete under short-term load, cube samples with a rib size of 10 sm and prism samples with dimensions of 10×10×40 sm were made. The samples were tested under short-term load at the age of 28-40 days.

According to the test results of the cubes, a load mode was assigned for short-term testing of prismatic samples. The load on the prisms was applied in steps equal to about 10% of the expected prism strength up to destruction. The samples were centered in the press along the physical center at a load corresponding to two loading stages. The load endurance at each stage was 5 minutes.

Measurements of the longitudinal and transverse deformations of the prisms were carried out using clock-type indicators with a division price of 0.001 mm mounted on special removable metal frames (fig.1).

FIGURE 1. Concrete prism before testing.

THE METHODOLOGY OF PROCESSING EXPERIMENTAL RESULTS

Studies [3, 4, 5] have established that with an increase in the compression load, the deviation of the “σ−ε” diagram from the rectilinear one is mainly due to a violation of the continuity of concrete (when the boundary of micro-fractures  Rcrc∘ and the subsequent development of microcracks in concrete.

The stress values corresponding to the lower boundary of microcracks Rcrc∘ and the conditional upper boundary of microcracks Rcrcν during compression were determined based on the results of measurements of longitudinal and transverse deformations of the sample.

The differential coefficient of transverse deformation was calculated from the increments of transverse (Δε2) and longitudinal (Δε1) deformations.:

Δν=ΔE2ΔE1						(1)

The stress level corresponding to the beginning of the deviation of Δν from a constant value was taken as a parametric level Rcrc∘, and the achievement of the value Δν=0,5   corresponded to the conditional upper boundary of microcracks Rcrcν. A detailed analysis of the parametric levels Rcrc∘ and Rcrcν was also performed using the curves of the total volume of the sample θ and its increment Δθ. The change in the total relative volume θ at each loading stage was calculated using the formula:

θ=ε1-2ε2						(2)

where  ε1 and  ε2 are the total relative longitudinal and transverse deformations. The increments of the relative volume of the sample were calculated using the formula:

Δθ=Δε1-2Δε2						(3)

In these studies, these methods were used for the first time to study the structural characteristics of basalt fiber concrete and their changes under load.

RESULTS AND DISCUSSIONS

Figure 2 shows the characteristic dependences of the differential coefficient of transverse deformation (a), sample volume (b), and its increments (c). These dependencies make it possible to establish parametric points of the destruction process and, on this basis, identify the features of the micro-destruction process in concrete.

GRAPHS OF CHANGES IN THE VOLUME OF CONCRETE PRISMS

Graphs of growth of volumetric deformations (b)

Graphs of the change in the differential coefficient of transverse deformation

FIGURE 2. Graphs of the specificity of the structural properties of the concrete prism sample

°- for basalt fiber concrete; •- for heavy concrete.

When considering figure 2, it is noteworthy that in all cases there are sufficiently clear parametric points. This feature can be explained by the conditions of formation of the initial structure of basalt fiber concrete, which differs from ordinary concretes, i.e. the existence of basalt fibers in its structure.

The results of processing the data obtained, shown in figure 3, indicate that the boundaries of Rcrc∘ and Rcrcν of basalt fiber concrete are systematically higher than those of ordinary concrete without additives.

FIGURE 3. Dependence of crack formation parameters in basalt fiber concrete on its prismatic strength

_______ - dependence for heavy concrete on [5];

- - - -    dependence on experimental results for basalt fiber concrete.

This circumstance should be attributed to the increased density of the initial structure of basalt fiber concrete, which, as noted, in turn, leads to an increase in the tensile strength and tensile strength of this concrete. This is confirmed by the results of measuring the transverse deformation of basalt reinforced concrete, which, when reaching the Rcrc∘ boundary, usually amounted to 15×10-5 and higher.

An important feature following from figure 3 is the existence of a fairly close relationship between the relative levels of Rcrc∘/Rb and Rcrcν/Rb and the prism strength of concrete Rb, and the nature of this relationship is similar to that observed for conventional concretes [4, 6].

Therefore, while maintaining the structure of approximating expressions for describing these dependencies in heavy concretes, we can propose similar expressions for estimating Rcrc∘/Rb and Rcrcν/Rb in basalt fiber concrete:

Rcrc∘/Rb=0,35lg⁡Rb-0,38					(4)

Rcrcν/Rb=0,35lg⁡Rb-0,08					(5)

The results of statistical processing of data on parametric levels of cracking of basalt fiber concrete in comparison with heavy concrete without additives are shown in the table.

TABLE 1. Results of the statistical processing of data on the parametric levels of crack formation in basalt fiber reinforced concrete

| № | Name of the crack formation parameter of concretes |  | Values of statistical distribution parameters |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | η | σ | δ, % |  |
| 1. | Lower boundary of microcrack formation for heavy concrete (Rcrc∘) |  | 0,95 | 0,024 | 2,6 |  |
| 2. | Upper boundary of microcrack formation for heavy concrete (Rcrcν) |  | 0,97 | 0,013 | 1,3 |  |
| 3. | Lower boundary of microcrack formation for basalt fiber reinforced concrete (Rcrc∘) |  | 0,97 | 0,013 | 1,3 |  |
| 4. | Upper boundary of microcrack formation for basalt fiber reinforced concrete (Rcrcν) |  | 0,96 | 0,011 | 1,2 |  |
| Notes. |  | η – mean value of the ratio of experimental to calculated values; σ – the standard deviation of the mean of this ratio; δ – coefficient of variation. |  |  |  |

Statistical processing of the experimental results confirms that the use of expressions (4) and (5) provides the best possible difference between the experimental and calculated values Rcrc∘  and Rcrcν  for basalt fiber concrete and their stability, as well as reliability for practical use.

These results confirm that the use of basalt fibers makes it possible to improve the basic compressive strength characteristics of concrete and, consequently, a number of its physical and technical properties[6], on which the operational qualities of reinforced concrete structures depend.

According to the experimental results, it can be noted that the process of concrete destruction consists of a sequential break in the continuity of the structure, starting with the appearance of individual cracks, which, after combining several such cracks, turn into main cracks. Usually, the destruction of concrete prisms occurs in two ways:

- using a cement-sand matrix bypassing coarse aggregate grains, which is typical for conventional concretes with a strength of less than 50 MPa;

-from transverse rupture in concretes with large aggregates with weak strength.

According to the results of experimental studies and observations, it has been established that after the maximum stress acting in prisms made of ordinary concrete, intense brittle fracture begins, accompanied by a strong sound. Such destruction is not typical for experimental prisms made of basalt fiber concrete due to the manifestation of large plastic deformations due to maximum stress, which is associated with the presence of basalt fibers in its composition. The destruction of experimental concrete prisms made of basalt-fiber concrete is viscous (see fig.4).

FIGURE 4. Characteristic destruction of basalt-fiber-reinforced concrete prisms

Analysis of the results shows that the nature of the destruction of concrete prisms largely depends on the packing density of the material structure with a large aggregate, the consumption of basalt fibers per unit volume, which determine the intensity of the destruction of continuity and changes in transverse deformations.

Under the action of a compressive load on a basalt-concrete prism, basalt fibers, randomly arranged in the composition of concrete, exert resistance and reaction to deformations, as if resembling a "damping effect". When an external force acts on basalt fiber concrete, the fibers of the mortar component of concrete and other concrete components perceive compressive stresses in the longitudinal direction, and tensile stresses in the transverse direction.By such work, basalt fibers unload the contact zones of large aggregates, contributing to the strengthening of the structure, leading to an increase in the strength of such concretes as a whole. Another important reason for such work of basalt fiber concrete under external load is, in all likelihood, the adaptation of basalt fibers to the perception of external load, leading to increased tensile strength, respectively, and crack resistance.

The progressive development of micro-fractures of the concrete structure at a certain loading level leads to an increase in the sample volume, as evidenced by the nature of the destruction of basalt fiber concrete.It can also be noted that changes in the structure of such concrete under the influence of an external load can be a function not only of its strength, leading to the process of micro-destruction, but also of other technological and structural factors that ensure the formation of density and internal bonds.

APPLICATIONS

Following are the application areas of the implemented system:

- Bridge and Overpass Construction: Used in high-load structures to enhance crack resistance and long-term durability.

- Pavements and Airport Runways: Helps reduce microcracking under repeated loading and heavy traffic.

- Underground Structures (Tunnels, Subways): Offers resistance to pressure, moisture, and vibration; ideal for long-term use due to corrosion resistance.

- Hydraulic Structures (Dams, Reservoirs, Water Infrastructure): Suitable for water-exposed environments thanks to its low permeability and high crack control capacity.

- Fire-Resistant Structures: Basalt fibers do not melt under high temperatures, making them ideal for fire-prone areas.

- Industrial Floors and Heavy-Load Warehouses: Improves structural stability and minimizes surface cracking under dynamic and concentrated loads.

- Seismic-Resistant Construction: Enhances elasticity and crack resistance, which is crucial for structures in earthquake-prone zones.

CONCLUSION

So, the characteristics of basalt fiber concrete is the high values of the microcracking boundaries as compared with other similar indicators of heavy concrete without any additives, as until a loading level of 0.5-0.6 with a prism strength of 30-60 MPa, of such concretes the structure is compacted without visible micro-fractures and this fact is explained by the increase of the tensile strength of the concrete and of ultimate extensibility.

All the conditions are at hand to use basalt-fiber concrete in the construction of a building and structure with heavy reinforced concrete under construction in regions of seismic activity - the availability of local basalt fibers, optimum technology of basalt-fiber concrete mixtures and the recommendation of rationing its strength and deformation characteristics, which is considered in calculation. These findings prove the fact that when uniting dispersed reinforcement in the form of basalt fibers, one can upgrade the fundamental properties of a basalt-fiber concrete in compression and tension in comparison with the standard one and, as a consequence, many of its qualities, in which the working performance of reinforced concrete constructions lie.

FUTURE SCOPE

Structural behavior of Basalt Fiber Reinforced Concrete (BFRC) under loads is the developing field of study, and some prospects in its development may be proposed.

Hybrid fiber systems can be used with future research where basalt fibbers are integrated with other natural or artificial fibers (carbon or glass fibers, or polymer fibers) and their synergistic effect is measured.

The real time testing needs to be done on the performance of BFRC under the dynamic loading conditions like earthquakes, vibrations or high frequency loads caused by traffic.

The effects of various curing methods (e.g., moist, steam or accelerated curing) on fiber-matrix bond and the related mechanical performance ought to be analyzed in details.

To evaluate the service life of BFRC in harsh environment, such as freeze thaw cycle, high temperature, or saline (coastal) environment, should be considered in the long-term durability.

These modern methods of computations like Finite Element Analysis (FEA) have provided the capacity to estimate the distribution of stress and crack propagation under various load conditions.

Imbalanced fiber may cause structural weaknesses. Thus, AI-assisted control systems and sensors used to monitor and optimize the placement of fibers in the process of mixing and pouring are an interesting research area.

That the BFRC has a resistance to high loads and vibration, which makes it has the potential of being used in high-speed rail systems and especially in the use of the rail in the ballast less track slabs.

In the case of basalt being a naturally occurring material and thus friendlier towards the environment, additional studies into the use of recycled or industrial waste material-based fibers would sell the environment off as well as investment into construction.

What is expected to occur in the future is the implementation of sensors into fibers in order to produce smart materials that allow overseeing the process of stress, temperature changes and crack formation in real time.

It requires the formulation of national and international standards and guidelines of using BFRC in railway and infrastructure projects so as to provide safety, uniformity, and reliability.

REFERENCES

- K. Akramov, S. Davlyatov, and A. Nazirov, E3S Web of Conferences 452, 06006 (2023).

- J. Sim and C. Park, Composites Part B: Engineering 36(6–7), 504–512 (2005).

- K. Akramov, R. Yusupov, and J. Ergashov, E3S Web of Conferences 452, 06003 (2023).

- V. Plevkov and K. Kudyakov, EPJ Web of Conferences 221, 01026 (2019).

- M. A. Caldarone, High-Strength Concrete: A Practical Guide (CRC Press, Boca Raton, 2008).

- M. G. Zertsalov and E. A. Khoteev, Proceedings of Moscow State University of Civil Engineering (Vestnik MGSU) (2014).