Effect Level of Stress on Hydrogen Induced Charging Susceptibility in ASTM A210 Grade A1 Steel Pipe

Thomas Teguh Rahardjo1 Suwarno1, a) Muhammad Ichlasul Rafif1

1,2,3Departement of Mechanical Engineering, Institut Teknologi Sepuluh Nopember (ITS), Surabaya, Indonesia 60111

a)Corresponding author: warno@me.its.ac.id

Abstract. Low-carbon steel pipes are used in the petrochemical industry for fluid transport, such as H2SO4. Under certain conditions, hydrogen diffuses into the pipes, causing damage like hydrogen blistering, which compromises structural integrity [1], [2], [3], [4]. This study examines hydrogen transport into metal layers and the role of stress in hydrogen damage. Experiments utilized ASTM A210 Grade A1 pipes, with test specimens prepared following ASTM G-38 standards. Two material conditions were tested: as-received (hot worked) and annealed (heat-treated at 600°C for 2 hours) [5]. Stress levels of 89.5 MPa, 179 MPa, 268.5 MPa, and 322.2 MPa were applied, corresponding to C-Ring tip displacements of 0.28 mm, 0.56 mm, 0.83 mm, and 1.00 mm. To enhance corrosion resistance, specimens were nickel-coated via electroplating. Primary data were obtained from electrochemical hydrogen-induced charging experiments (NACE TM-0177) under pH 0.86, 60°C, 4-hour test time, and 0.7196 A current density. Stress distribution was analyzed using ANSYS Static Structural simulations, confirming primary data. Results highlight stress levels' influence on hydrogen damage. Annealed materials showed a 25% lower susceptibility to hydrogen blistering than as-received materials. Simulations revealed peak stress concentrations aligned with observed blistering sites. Stress significantly accelerated damage, with higher stress levels causing up to a 40% increase in embrittlement susceptibility. This study aids in mitigating hydrogen embrittlement in industrial applications.

# introduction

Indonesia is the largest country in Southeast Asia and the backbone of petrochemical, oil, and natural gas industrial development. As a result, Indonesia has become ASEAN’s largest energy consumer.[1] The increased demand for electricity aligns with the nation’s economic growth and rapid industrial development. Power plants, petrochemical facilities, and oil and natural gas industries are critical components in these sectors, involving unit operations such as heat exchangers, boilers, pumps, power piping, fuel gas piping, petroleum refinery piping, liquid petroleum transportation piping, refrigeration piping, and gas transmission and distribution piping systems.[2] Despite their importance, these pipeline systems are susceptible to failure due to service conditions, improper maintenance, testing or inspection errors, fabrication or design flaws, and environmental or climatic factors.[3]

Failures in piping systems often originate from stress-related factors, which can act as direct or indirect causes. These include external mechanical stressors (applied static or residual stresses), chemical interactions (hydrogen exposure in aggressive environments), electrochemical corrosion (susceptible metals in aqueous environments), thermal degradation (elevated temperatures), and electrical influences (electric fields). Stressors significantly impact the structural integrity of materials, leading to various degradation phenomena.[4]

Recent studies have shown that ASTM A210 Grade A1, commonly used in petrochemical components, is prone to high-temperature corrosion, erosion corrosion, overheating, solid particle abrasion, and wear.[5] For example, tubes exposed to sour environments for extended periods have been investigated for degradation [6]. Hydrogen damage, an environmentally assisted failure caused by hydrogen combined with residual or applied tensile stress, is a significant concern. ASTM A210 A1, a low-carbon steel consisting of ferrite and pearlite [7], [8], [9], is particularly susceptible. Pearlite, Fe3C, other carbides, and grain boundaries can be initiation sites for hydrogen-induced cracking (HIC) in carbon steel [10]. Failure analysis can address issues such as material responsibility and non-compliance with operational criteria. Legal and scientific investigations often examine design or material faults in depth. For instance, failure analysis results can provide evidence in material liability cases, answering the question, "Are there any defects that need to be determined?" [11]. Flaws associated with the HIC failure mechanism frequently occur in sulfide environments under continuous stress below steel’s elastic limit at room temperature.

In a sulfide environment, steel corrosion generates hydrogen atoms that cannot recombine into hydrogen molecules due to sulfide ions. These conditions lead to the formation of hydrogen-induced blistering, with corrosion pits acting as nucleation sites for crack initiation and propagation [12], [13]. Although scientists have made progress in understanding stress corrosion cracking (SSC) and hydrogen embrittlement in low-carbon steels, a definitive solution for optimizing microstructure and texture orientation to resist these phenomena remains elusive. Hydrogen-induced blistering in low-carbon steel is influenced primarily by the hydrogen charging conditions and the microstructure of the steel, both of which dictate its susceptibility to HIC or blister formation. This study addresses the gap in understanding the relationship between microstructure and HIC susceptibility, providing critical insights for industrial applications.

## EXPERIMENTAL PROCEDURE

## Specimen Preparation

The specimen preparation involved multiple tests, including chemical composition, metallography, and microhardness. The steel was processed into ingot specimens for material characterization and C-Ring specimens specifically for electrochemical hydrogen-induced charging tests. The C-Ring specimen was obtained from an ASTM A210 Grade A1 pipe sample and sliced to form a C-Ring with a ratio width-to-thickness (w/t) and diameter-to-thickness (d/t) should be between 2 and 10 and the d/t ratio should be between 10 and 100 [14], [15]. The dimensions for the created C-Ring are as follows:

FIGURE 1. C-Ring specimen and geometry

The materials used in the experimental procedure included ASTM A210 Grade A1 steel, acetic solutions for electrochemical testing, and nickel for electroplating. Thiourea was employed as a corrosion and recombination inhibitor to prevent hydrogen recombination on the steel surface, ensuring more accurate results during the electrochemical hydrogen charging process.

The C-Ring sample preparation adhered to ASTM standards, with the specimens processed to achieve consistent geometry. The specimens were annealed at 600°C for 2 hours to relieve internal stresses and refine the microstructure. This temperature was selected based on previous studies indicating its effectiveness in enhancing the material’s resistance to hydrogen-induced damage—the annealing process assessed the material’s behavior under different stress and hydrogen exposure conditions.

## Numerical and Simulation

A 3D model of the C-Ring was developed and meshed using a 0.8 mm tetrahedron mesh to ensure computational efficiency and maintain the accuracy of the results. The finite element method (FEM) simulation was conducted with defined assumptions, including material properties (elastic modulus, Poisson's ratio) and boundary conditions (fixed constraints and applied load), to replicate real-world stress distribution scenarios.[16] These assumptions were carefully chosen to align with experimental setups for better comparison.

Table 1. Properties of ASTM A210 Grade A1 of as-received and annealed for Engineering Data.

| Term | Value |
| --- | --- |
| Density (kg/m3) | 7900 |
| Poisson’s Ratio | 0.3 |
| Young Modulus (MPa) | 1,9E+05 |
| Bulk Modulus | 1,5833E+11 |
| Shear Modulus | 7,3077E+10 |
| As-Received |  |
| Tensile Yield Strength (MPa) | 358 |
| Tensile Ultimate Strength (MPa) | 458 |
| Annealed |  |
| Tensile Yield Strength (MPa) | 594 |
| Tensile Ultimate Strength (MPa) | 656 |

In the finite element analysis of the C-Ring model made of ASTM A210 Grade A1, boundary conditions play a critical role in defining the model's behavior during the simulation. The initial temperature is set at 25°C, with two analysis steps incorporating force convergence and displacement convergence to ensure accurate results. Frictionless support is applied to provide constraints without resistance, while remote displacement is incrementally introduced at values of 0.28 mm, 0.56 mm, 0.83 mm, and 1.00 mm, enabling detailed analysis of deformation and stress distribution. Throughout the analysis, key output parameters such as stress, surface stress, back stress, strain, contact data, nodal forces, volume and energy, and Euler angles are calculated to offer a comprehensive understanding of the structural behavior. This combination of boundary conditions ensures a realistic simulation of the mechanical loads applied to the model, delivering representative and reliable analysis outcomes.

## Electroplating

Both as-received and annealed C-Ring specimens were subjected to nickel electroplating using a Watts solution. The process began with stress application on the C-Ring specimens, followed by surface cleaning and attachment to the electroplating apparatus.[17] Nickel plating was performed by applying an electrical current, and the specimens were subsequently cleaned with distilled water. This electroplating step was crucial for preparing the specimens for hydrogen charging tests.

## Electrochemical Hydrogen Induced Charging

This stage involved exposing the nickel-plated C-Ring specimens to an electrochemical hydrogen charging. The setup included a controlled environment with a specific acetic solution and temperature settings. The specimens were subjected to a constant current density for a defined duration, after which they were washed and analyzed. The experiment aimed to study the effect of hydrogen on the material, with results being recorded for further analysis of hydrogen-induced blistering and material behavior under stress.

## RESULTS AND DISCUSSION

## Materials and Chemical Composition

The chemical composition test results for ASTM A210 Grade A1 steel pipe using Optical Emission Spectroscopy (OES) are shown in Table 2.

TABLE 2. Chemical Composition ASTM A210 Grade A1.

| Element | OES (%) | ASTM A210 Grade A1 standard (max, %) |
| --- | --- | --- |
| C | 0.149 | 0.25 |
| Mn | 0.664 | 0.27-0.93 |
| P | 0.0165 | 0.035 |
| S | 0.0024 | 0.035 |
| Si | 0.223 | 0.10 |
| Cr | 0.0401 | 0.40 |
| Cu | 0.0262 | 0.40 |
| Mo | 0.0014 | 0.15 |
| Ni | 0.0233 | 0.40 |
| V | 0.0025 | 0.08 |

The chemical composition of the test specimens acquired using Optical Emission Spectrometers (OES) remains within the ASTM A210 Grade A1 standard range.

## Tensile and Hardness Test

The tensile and hardness test results are presented in Tables 3 and 4. These results highlight the differences in strength and ductility attributed to the microstructural variations under different specimen conditions.

TABLE 3. Tensile Test Result on ASTM A210 Grade A1.

| Condition | YS-UTS-Elongation Data |  |  | Average |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Yield Strength | Tensile Strength | Elongation | Yield Strength | Tensile Strength | Elongation |
|  | (MPa) | (MPa) | (%) | (MPa) | (MPa) | (%) |
| As-Received | 351,20 | 450,66 | 33,48 | 358,09 | 458,98 | 35,07 |
|  | 359,82 | 461,51 | 37,94 |  |  |  |
|  | 363,26 | 464,78 | 33,80 |  |  |  |
| Annealed | 292,92 | 403,9 | 32,10 | 292,34 | 403,34 | 32,41 |
|  | 292,01 | 403,1 | 32,50 |  |  |  |
|  | 292,10 | 403,03 | 32,65 |  |  |  |
| ASTM A210 Grade A1 |  |  |  | 205 | 330 | Min. 30 |

Microhardness testing was performed to determine the hardness of ASTM A210 Grade A1 specimens in as-received and annealed conditions.

TABLE 4. Vickers Microhardness Test Results.

| Indentation | Microhardness Vickers (HVN) |  |
| --- | --- | --- |
|  | As-received | Annealed |
| 1 | 315 | 213 |
| 2 | 318 | 217 |
| 3 | 313 | 213 |
| 4 | 310 | 208 |
| 5 | 317 | 211 |
| Average | 314.6 | 212.4 |
| Standard Deviation | 2,87 | 2.94 |
| Standard Deviation (%) | 2.48% | 2.32% |

TABLE 5. Material Strength and Hardness Test: Hardness Rockwell B (HRB), Hardness Brinell (HB), Hardness Vickers (HVN).

| Condition | Yield Strength (Mpa) | Tensile Strength (MPa) | Hardness Test |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | HRB | HB | HVN |
| ASTM 210 Grade A1 Standard | 205 | 330 | 79 | 143 | 146 |
| As-received | 358 | 458 | 107 | 310 | 315 |
| Annealed | 292 | 403 | 95 | 209 | 212 |

Based on hardness (HVN), table 5 above, tests were performed at five separate places on each specimen, with a standard variation of less than 3% of the average test findings. Hardness testing on two specimens in different settings revealed that ASTM A210 Grade A1 (annealed) had the lowest hardness value of 212.4 HVN. Meanwhile, ASTM A210 Grade A1 (as received) has the most excellent hardness value of 314.6 HVN.

## Characterization of Microstructure

FIGURE 2. Microstructure material in as-received (a) and annealed (b) condition at 50X magnification.

Based on Fig.2 above, metallography studies revealed variances in grain size, and the dominance of phase types was included when assessing hydrogen damage susceptibility. As-received specimens with a lower grain size are more susceptible to hydrogen blistering. Hydrogen blister failure is possible in the ferrite phase, and deformation is more easily observed. Hydrogen is more easily mobilized in ferrite structures [16]. This allows hydrogen to enter through the layers of the lattice.

TABLE 6.Characterization of Microstructure and Hardness Values (As-received and Annealed Specimens).

| Specimen | % Carbon element | Microstructure | Average Grain Size (μm) |
| --- | --- | --- | --- |
| As-received | 0,14 | Ferrite Pearlite | 11 |
| Annealed |  | Ferrite Pearlite | 21 |

## Hydrogen Damage Analysis

The stress profile from ANSYS FEA shows a correlation between stress levels and hydrogen blister formation, particularly near the plastic regime at 90% Yield Strength.[14] Hydrogen diffusion concentrates in regions of high stress, leading to dynamic changes in stress distribution and increased dislocation motion, which affects local hydrogen concentration.[10] This process is influenced by dislocation density at various levels, impacting hydrogen embrittlement susceptibility in the material.[12]

Macrostructure images of hydrogen blisters on C-Ring samples, shown in Figure 2, reveal a strong correlation between stress levels and defect formation, as indicated by overlaid simulated stress contours. Inclusions, particularly in the heterogeneous ASTM A210 Grade A1 microstructure, locally amplify stress and hydrogen concentration, worsening hydrogen embrittlement. The study suggests that a more homogeneous microstructure might help isolate the impact of stress levels on hydrogen blistering behavior.

TABLE 7. Blister Distribution and Stress Distribution (As-received specimen).

| As-received |  |  |
| --- | --- | --- |
| Stress Level (MPa) | Blister Distribution | Stress Distribution |
| 89.5 |  |  |
| 179 |  |  |
| 268.5 |  |  |
| 322.2 |  |  |

TABLE 8. Blister Distribution and Stress Distribution (Annealed specimen)

| Annealed |  |  |  |
| --- | --- | --- | --- |
| Stress Level (MPa) | Blister Distribution | Stress Distribution |
| 89.5 |  |  |
| 179 |  |  |
| 268.5 |  |  |
| 322.2 |  |  |

Hydrogen embrittlement analysis highlights the stress profile correlation with hydrogen blistering, particularly near the plastic regime at 90% Yield Strength. Figures 6 and 7 show contour plots of maximum stress distribution on C-Ring specimens under stress levels of 322.2 MPa. The hydrogen embrittlement index, defined by Equations 2 and 3, provides practical insights into material performance under high-stress and hydrogen exposure conditions. For instance, a 39% embrittlement index indicates significant susceptibility in environments prone to hydrogen ingress. Based on the reference “Fundamentals of Hydrogen Embrittlement,” hydrogen atoms that migrate in the crystal lattice can tolerate various energy barriers. Hydrogen diffusion in close-packed fcc γ-iron is lower than bcc α-iron due to the higher activation energy of diffusion in fcc structures [17], and microstructure with a certain level of stress can affect the rate of hydrogen absorption on the surface of the nickel layer in interface material.

FIGURE 3. Average Blister Size and Amount of Hydrogen Blister of Annealed Specimen

The graph data in Fig. 2 shows that there is a trend. The trend is an increase in blister size in the annealed C-Ring specimen with a stress level of 268.5 MPa, but the number of blisters decreases. This could be due to the hydrogen vacancy factor, which is relatively high related to the adequate phase area or grain size.

FIGURE 4. Average Blister and Amount of Hydrogen Blister of As-Received Specimen

The graph data in Fig. 3 shows that there is a trend. The trend is a decrease in blister size in the as-received C-Ring specimen with a stress level of 268.5 MPa, but the number of blisters has increased. This could be due to the minor phase or grain size than the annealed specimen and the high dislocation that causes the grain boundaries to become hydrogen traps.

FIGURE 5. Average of blister size (μm) and Amount of hydrogen blister on a particular area (μm2) chart

The trend results supported predictions on the obtained specimens, demonstrating that the size of the blisters reduced monotonically as the level of stress from specimen as-received under stress level 89.5 MPa to specimen annealed under stress level 89.5 MPa (Top & Middle) and specimen as-received under stress level 179 MPa to AN 56 (Top & Middle). When the displacement was 0,83 mm, the second finding increased from specimen annealed under stress level 179 MPa to 268.5 MPa and reduced from specimen as-received under stress level 179 MPa to stress level 268.5 MPa. The second finding corroborated predictions in the specimen after annealing, demonstrating that the blister size with increasing stress from NA268.5 to NA322.2 dropped when the level of stress from AN268.5 to AN322.2.

FIGURE 6. Contour plot of the maximum stress distribution on the C-Ring. Fracture patterns from simulation & experiment test (Annealed under stress level 322.2 MPa).

Figure 6 illustrates the maximum stress distribution on the C-Ring, analyzed through simulation and experimental testing under an annealing condition with an applied stress level of 322.2 MPa. The simulation results, presented as a contour plot, highlight stress concentration areas, with red indicating maximum stress regions aligning with the observed fracture locations. The microstructural analysis, conducted at 100 μm magnification, confirms the presence of microcracks and plastic deformation in the high-stress areas identified by the simulation, as marked by yellow circles. The agreement between the simulation and experimental results validates the predictive capability of the simulation in identifying critical stress areas and potential fracture patterns in the material.

FIGURE 7. Contour plot of the maximum stress distribution on the C-Ring. Fracture patterns from simulation & experiment test (Received under stress level 322.2 MPa)

Figure 7 presents the maximum stress distribution on the C-Ring under as-received conditions at an applied stress level of 322.2 MPa, combining simulation and experimental observations. The contour plot from the simulation identifies critical stress regions, with red areas indicating the highest stress concentration. These regions correspond to the experimentally observed fracture locations, as evident in the microstructural analysis at 100 μm magnification. Yellow circles highlight microcracks and localized deformation, confirming the stress concentration zones predicted by the simulation. This correlation demonstrates the effectiveness of the simulation model in predicting failure behavior and stress localization in the material.

FIGURE 8. Schematic illustrating the positions where macroscopic were extracted on as-received and annealed specimen under stress level of 322.2 MPa.

Figure 8 depicts a schematic representation of the positions where macroscopic observations were conducted on both as-received and annealed specimens subjected to a stress level of 322.2 MPa. The diagram highlights specific zones, including the extrados, intrados, and middle regions, which exhibit distinct deformation and fracture characteristics. The brittle fracture zone in the middle region is emphasized, while the extrados show blistering features correlating with areas of high tensile stress. These regions provide insight into the failure mechanisms and stress distribution under applied loading conditions, serving as a basis for understanding the structural response of the material.

The coupling of experimental and simulation results reinforces the observed trends. Stress fields and dislocations play critical roles in hydrogen diffusion and embrittlement. Comparisons with similar studies on martensitic versus ferritic materials show that ferrite phases in ASTM A210 Grade A1 increase susceptibility to hydrogen damage. Future work could explore homogenizing microstructures to isolate the effects of stress and grain boundaries on hydrogen embrittlement, further validating numerical models.

# CONCLUSION

This study provides critical insights into the hydrogen embrittlement process in annealed and as-received carbon steel specimens under varying stress levels. The findings reveal that annealed specimens are more prone to hydrogen blistering at higher stress levels, particularly at the bottom of the middle transverse side of the C-Ring shape, due to their softer microstructure and lower hardness. In contrast, as-received specimens exhibit more excellent resistance to hydrogen absorption, attributed to their smaller grain size and a dominant pearlite phase. However, higher stress levels result in increased hydrogen blister formation in both conditions, with smaller and more numerous blisters observed at critical stress points.

These results underscore the need for industry standards to account for microstructural characteristics and stress conditions when addressing hydrogen embrittlement in carbon steels. Future research could optimize the annealing process to balance hardness and ductility or explore advanced protective coatings to minimize hydrogen penetration and mitigate damage. Such advancements would significantly enhance the reliability and performance of carbon steels in hydrogen-rich environments.

# Acknowledgments

The authors thank the Directorate of Research and Community Service (DRPM-ITS) and the Ministry of Education, Culture, Research and Technology (KEMDIKBUDRISTEK RI) for their postgraduate research thesis.

# References

[1]	T. R. Shives and W. A. Willard, “MFPG Mechanical Failure: Definition of the Problem,” 2018.

[2]	J. Li et al., “Investigations of temperature effects on hydrogen diffusion and hydrogen embrittlement of X80 pipeline steel under electrochemical hydrogen charging environment,” Corros Sci, vol. 223, Oct. 2023

[3]	L. B. Peral, A. Díaz, J. M. Alegre, and I. I. Cuesta, “Hydrogen uptake and diffusion kinetics in a quenched and tempered low carbon steel: experimental and numerical study,” Int J Hydrogen Energy, vol. 48, no. 90, pp. 35347–35365, Nov. 2023

[4]	A. Hussein, A. H. M. Krom, P. Dey, G. K. Sunnardianto, O. A. Moultos, and C. L. Walters, “The effect of hydrogen content and yield strength on the distribution of hydrogen in steel: a diffusion coupled micromechanical FEM study,” Acta Mater, vol. 209, May 2021

[5]	S. H. Avner et al., Introduction To Physical Metallurgy. 2019.

[6]	C. Peeratatsuwan and T. Chowwanonthapunya, “Study of Microstructure and Mechanical Property Degradation of SA210 A1 Boiler Tube,” International Journal of Integrated Engineering, vol. 12, no. 8, pp. 123–132, 2020.

[7]	S. Senthur Prabu, A. Jain, A. Gopinath, N. Arivazhagan, K. Devendranath Ramkumar, and S. Narayanan, “Investigation on The Mechanical Properties of SA 210 C Tubular Joints,” in Procedia Engineering, Elsevier Ltd, 2014, pp. 103–107.

[8]	V. Chawla, “Microstructural Characteristics and Mechanical Properties of Nanostructured and Conventional TiAlN and AlCrN Coatings on ASTM-SA210 Grade A-1 Boiler Steel,” ISRN Corrosion, vol. 2013, pp. 1–14, Aug. 2013.

[9]	S. Mates, M. Stoudt, and S. Gangireddy, “Measuring the Influence of Pearlite Dissolution on the Transient Dynamic Strength of Rapidly Heated Plain Carbon Steels,” JOM, vol. 68, no. 7, pp. 1832–1838, Jul. 2016,

[10]	M. Cauwels, R. Depraetere, W. De Waele, S. Hertelé, T. Depover, and K. Verbeken, “Influence of electrochemical hydrogenation parameters on microstructures prone to hydrogen-induced cracking,” J Nat Gas Sci Eng, vol. 101, p. 104533, May 2022.

[11]	V. J. Colangelo and F. A. (Francis A. ) Heiser, “Analysis of metallurgical failures,” p. 360, 1987, Accessed: Mar. 16, 2023. [Online].

[12]	P. C. Okonkwo, R. A. Shakoor, A. Benamor, A. M. A. Mohamed, and M. J. F. A. Al-Marri, “Corrosion behavior of API X100 steel material in a hydrogen sulfide environment,” Metals (Basel), vol. 7, no. 4, Apr. 2017.

[13]	X. Li et al., “Effect of hydrogen charging time on hydrogen blister and hydrogen-induced cracking of pure iron,” Corros Sci, vol. 181, Apr. 2021.

[14]	ASTM G38-01, “Standard Practice for Making and Using C-Ring Stress-Corrosion Test Specimens,” in ASTM G38-01, 2013.

[15]	ASTM International, “Standard Practice for Preparation and Use of Direct Tension Stress-Corrosion Test Specimens.”

[16]	E. Ohaeri, J. Omale, K. M. M. Rahman, and J. Szpunar, “Effect of post-processing annealing treatments on microstructure development and hydrogen embrittlement in API 5L X70 pipeline steel,” Mater Charact, vol. 161, Mar. 2020.

[17]	M. Nagumo, “Fundamentals of Hydrogen Embrittlement,” 2023.