# Effect of Calcination Variable on Electrochemical Performance of LiNi0,8Mn0,1Co0,1O2 (NMC 811) Cathode Material for Lithium-Ion Batteries

H. Hariyanto, S. Suwarno*, B. Anggraini

Department of Mechanical Engineering, Institut Teknologi Sepuluh Nopember (ITS), Surabaya, Indonesia 60111

*Corresponding author: warno@me.its.ac.id

Abstract. Lithium-ion batteries are one of the electrical energy storage components in electric cars due to their high energy density and long cycle life. This study investigates the effect of calcination temperature and holding time on the electrochemical performance of LiNi0,8Co0,1Mn0,1O2 (NMC 811) cathode material for lithium-ion batteries. The findings indicate notable improvements in capacity retention and cycling stability. The study shows that NMC 811 calcined at 750°C-9h has higher battery retention capacity than other samples. The largest battery retention capacity was found in NMC 811 calcined at 750°C-9h of 86,30%. Meanwhile, the smallest battery retention capacity was found in the calcined at 900°C-12h of 60,87%. A higher calcination temperature tends to increase the reversibility of the redox reaction, as seen from the smaller difference of redox potential peaks in the CV measurement curve. The smallest redox peak potential difference was obtained in the calcined at 750°C-9h of 1,82 V. Meanwhile, the largest redox peak potential difference was obtained in the calcined at 900°C-12h of 2,30 V. Based on EIS measurement data, the best ion conductivity value was obtained in the calcined at 750°C-9h of 0,713 S/cm. This corresponds to the lowest cation mixing value with a peak ratio of I(003)/I(104) is 2,10. The findings from this study offer important guidelines for the development of high-performance NMC electrodes.

Keywords: Lithium-ion battery, cathode, NMC, calcination, high-performance

INTRODUCTION

The electric vehicle industry has seen remarkable growth worldwide. Sales of electric vehicles are projected to increase tenfold by the end of the decade, with nearly 90% of the demand for lithium-ion (Li-ion) batteries coming from this sector [1]. Li-ion batteries are crucial for storing electrical energy in electric cars due to their high energy density and long lifespan [2]. Currently, lithium-ion (Li-ion) battery technology represents the most promising choice for electrochemical energy storage in hybrid electric vehicles (HEV) and battery electric vehicles (BEV) [3]. Ongoing research on Li-ion batteries continues to focus on developing materials that offer high capacity, affordability, safety, and long-term durability for energy storage applications.

The selection of positive electrode (cathode) materials is crucial in the development of lithium-ion (Li-ion) batteries for electric vehicles, as the battery's energy density must be sufficient to meet the mileage requirements. Among the various types of positive electrode materials, those with a high nickel content in the LiNixCoyMnzO2 layer structure, where x+y+z = 1 and x > y+z, such as NMC 811, have been extensively utilised in Li-ion batteries for electric vehicles [4].

In principle, batteries containing nickel-rich cathodes like NMC 811 are widely used due to their highest energy density compared to low-nickel cathodes such as NMC 622, NMC 532, and NMC 333. However, NMC 811 batteries have drawbacks, including cation mixing resulting in reduced battery cycle life [4]. Therefore, efforts are needed to improve the NMC 811 material, such as by adjusting the temperature and calcination time to achieve a higher specific discharge capacity and retention capacity. The following are the energy density values for various types of lithium battery cathodes.

Figure 1. Energy density and cobalt content from LCO to NMC-xyz with increasing nickel content [5]

MATERIALS AND METHODS

Synthesis of NMC

The eight samples are 750°C-9h, 800°C-9h, 850°C-9h, 900°C-9h, 750°C-12h, 800°C-12h, 850°C-12h, and 900°C-12h. To create these precursors, begin by preparing the raw materials, namely NiSO4.6H2O, MnSO4.H2O, and CoSO4.7H2O. Then, all the raw materials are dissolved in distilled water using a beaker glass with an integrated magnetic stirrer. Stirring was carried out at a heating temperature of 55oC for 12 hours until the solution was mixed evenly with a stirring speed of 700 rpm. NaOH and NH4OH were added to adjust the pH to 11.5 and left for 12 hours. The precipitate was filtered, washed, dried at 120oC for 24 hours, ground until smooth, and sieved with a 100-mesh size.

The outcome of these processes is NMC 811 cathode powders, which are then combined with LiOH at a ratio of 1:0.55. Then, crush, sieve, and heat the cathode powders in an oven at 400°C for 6 hours to remove organic compounds. Then, the NMC 811 cathode powders were transferred to the muffle furnace for the calcination process by heating it to a temperature of 750oC, 800oC, 850oC, and 900oC for 9 hours and 12 hours and flowing with O2 gas. The NMC 811 cathode powders were ground and sieved using a 400-mesh sieve. The final result of these processes is NMC 811 cathode precursors with various temperature and time calcination, which are then characterised using XRD and SEM-EDS.

Material Characterization

X-ray diffractometer (XRD) was used to determine crystal structure with a CuKα X-ray source (λ = 1.54056 Å) at 40 kV and 100 mA. The morphology was examined using Scanning Electron Spectroscopy (SEM) at 15 kV and 100 mA.

Cell Assembly and Electrochemical Characterization

Begin by creating a cathode slurry using a mixture of AM (active material), SBR (styrene-butadiene rubber), CMC (carboxymethyl cellulose), AB (acetylene black), and OA (oleic acid) in the ratio of 90:3:2:3:2. Add distilled water and stir until evenly distributed. Then, apply the cathode slurry onto aluminium foil using a doctor blade coater. Dry for 30 minutes at 100 °C, add another layer, and repeat the process. Once done, press and cut the material to 5.6 cm before attaching it to an aluminium plate using an ultrasonic welding machine.

To assemble the battery cells, roll together the cathode, graphite anode, and polypropylene separator. The separator serves to prevent short circuits. Use spot welding to attach the copper plate on the anode to the casing, and use ultrasonic equipment to attach the aluminium plate to the cover. After vacuum oven ageing, fill the battery cells with 5 ml of LiPF6 electrolyte and seal them. Finally, conduct tests on the assembled battery cells for charge-discharge, EIS, and CV.

RESULTS AND DISCUSSION

Figure 2 displays the X-ray diffraction (XRD) results processed using Highscore Plus software for active materials at different temperatures and durations. The crystal structure was identified for samples processed at 750°C-9h, 800°C-9h, 850°C-9h, 900°C-9h, 750°C-12h, 800°C-12h, 850°C-12h, and 900°C-12h. To assess the suitability of the crystal structure, data from the Crystallography Open Database (COD) No. 96-152-0790 was utilised. As per the literature, the crystal structure of NMC 811 is hexagonal. This is evident from the main peaks (003) and (104) [6], [7], [8], [9], [10].

A

C

B

Figure 2. (a) XRD patterns of all NMC 811 samples; (b) Diffraction peak shift pattern at peak 003; (c) Diffraction peak shift pattern at peak 104

In addition to revealing the crystal structure, XRD results can also identify the presence of cation mixing, where Ni2+ ions enter the Li layer due to the similar ion radii of Li+ (0.76Å) and Ni2+ (0.69Å) [11]. However, cation mixing is not favourable for the material. Low cation mixing indicates better electrochemical properties of the NMC material. According to the literature, the formula I(003)/I(104) is used to determine the cation mixing value. When the value of I(003)/I(104) is less than 1.2, the material will exhibit poor electrochemical properties, which will affect the performance of the lithium-ion battery [12]. Table 1 provided below presents the calculation of the intensity ratio I(003)/I(104) for all samples from COD data.

Table 1. Calculation of intensity ratio I(003)/I(104)

| Sample | I(003 | I(104) | Intensity of Ratio I(003)/I(104) |
| --- | --- | --- | --- |
| 750oC -9h | 100 | 47,51 | 2,10 |
| 800oC -9h | 100 | 62,87 | 1,59 |
| 850oC -9h | 100 | 65,61 | 1,52 |
| 900oC -9h | 100 | 79,66 | 1,25 |
| 750oC -12h | 100 | 45,78 | 2,18 |
| 800oC -12h | 100 | 56,09 | 1,78 |
| 850oC -12h | 100 | 64,25 | 1,55 |
| 900oC -12h | 100 | 76,17 | 1,31 |

Based on the calculations, it is evident that all variations of calcined samples exhibit a peak ratio value of I(003)/I(104) > 1.20, indicating very low cation mixing across all samples. A higher peak ratio value of I(003)/I(104) corresponds to less cation mixing, which can potentially enhance the performance of lithium-ion batteries. Figure 2 below shows the morphology of the grains in SEM testing.

d

c

b

a

Figure 3. SEM test results at 20,000X magnification with a holding time of 9 hours on the sample; (a) 750 oC – 9h ; (b) 800 oC – 9h  ; (c) 850 oC – 9h; (d) 900 oC – 9h

d

b

a

c

Figure 4. SEM test results at 20,000X magnification with a holding time of 12 hours on the sample; (a) 750 oC – 12h ; (b) 800 oC – 12h  ; (c) 850 oC – 12h; (d) 900 oC – 12h

ImageJ software was used to determine the particle diameter size in these SEM results. In Figure 3 and Figure 4, it can be seen that the higher the calcination temperature, the more dispersed the grain morphology and the larger the particle diameter. Then, holding time also has an influence where the longer holding time will make the particle diameter larger too.

Overall, it can be concluded that the higher the temperature and the longer the holding time in the calcination process, the larger the particle diameter will be. Larger particle size will hinder the lithium-ion diffusion process, which will result in a larger Li+ ion diffusion distance [13]. The slow diffusion rate of lithium ions will hinder the charging/discharging process and reduce the specific capacity of the battery [14]. Afterwards, this precursor will be tested for electrochemical performance, namely Galvanostatic Charge-Discharge (GCD). This was carried out using the Landt Instruments Battery Test System CT-3002AU equipment.

B

A

Figure 5. Specific discharge capacity test results with a c-rate of 0.5C for 100 cycles on sample types with (a) holding time 9 hours; (b) holding time 12 hours

Based on the results presented in Figure 5.a and Figure 5.b, it is evident that the cathode calcinated at 750°C exhibits a higher retention capacity (84.93%) compared to samples calcinated at 800°C, 850°C, and 900°C. Furthermore, the holding time also influences the retention capacity, with samples held for 9 hours demonstrating higher retention capacity than those held for 12 hours.

The difference in retention capacity values can be attributed to cation mixing (Li+ and Ni+ ions)  during the charging process. XRD results showing a ratio of I(003)/I(104) below 1.2 indicate high cation mixing, leading to decreased battery capacity [1]. The higher the value of the ratio I(003)/I(104)  indicates the very low cation mixing. Additionally, calcination at 750°C and a holding time of 9 hours can mitigate oxygen release by reinforcing oxide bonds in the NMC structure, thereby enhancing structural stability [13].

B

A

Figure 6. Specific discharge capacity test results with various c-rate variations of 5 cycles to 20 cycles each on samples with variations in calcination and variations in holding time

The graph in Figure 6 shows the specific discharge capacity of batteries at different c-rates: 0.1C, 0.3C, 0.5C, and 1C. Each c-rate was tested for 5 cycles, resulting in a total of 20 cycles. The graph clearly shows a decrease in capacity at each tested c-rate. The electrochemical performance is influenced by the transfer of lithium ions at high currents. At higher c-rates, the chemical reaction process within the battery speeds up, leading to the accumulation of ions and non-optimal reactions, consequently reducing the specific capacity of the battery. To demonstrate reversibility, charge-discharge testing was conducted with varying current rates.

The results reveal that all samples with variations in calcination and holding time at a c-rate of 0.1C exhibited the best battery performance. In contrast, at c-rates of 0.3C, 0.5C, and 1C, the performance continued to decline. The analysis indicates that the sample calcined at 750°C outperformed others at all c-rates (0.1C, 0.3C, 0.5C, and 1C). Moreover, the sample with a holding time of 9 hours demonstrated better performance than the sample held for 12 hours. These results also show that 750oC calcination and a holding time of 9 hours are able to increase the charge-discharge stability of the NMC 811 battery. Subsequently, EIS (electrochemical impedance spectroscopy) testing was carried out. EIS testing is a test to determine the impedance of a battery and is a non-destructive test.

A

B

Figure 7. Nyquist plot curves for all types of cathodes with (a) holding time 9 hours; (b) holding time 12 hours

Based on Figures 7.a and 7b, it can be seen that the charge transfer resistance (Rct) of the cathode with a calcination temperature of 750°C is lower than those with calcination temperatures of 800°C, 850°C, and 900°C. Furthermore, it is noticeable that the cathode calcined for 9 hours exhibits a smaller Rct compared to the one calcined for 12 hours, as indicated by the difference in the diameter of the semi-circle. This is appropriate with the presence of higher cation mixing, which leads to increased resistance. The obstacles in the crystal layer slow the kinetic reactions [15], [16], [17], [18].

In addition to the Rct, cation mixing also impacts the ion conductivity of each cathode type. Overall, it can be observed that higher calcination temperatures correspond to lower ion conductivity values. Similarly, a holding time of 12 hours results in lower ion conductivity compared to a holding time of 9 hours. This aligns with the increased cation mixing, which naturally leads to higher resistance in ion transfer. Furthermore, ion conductivity is linked to the diffusion of lithium ions, a process influenced by electrolyte resistance and electrode characteristics [16].

In Figure 8, the results of the CV (cyclic voltammetry) testing are presented. This test aimed to identify the oxidation-reduction reaction at the cathode using the Autolab Potentiostat/Galvanostat PGSTAT302N, with a potential window of 2.5 V – 4.2 V and a scan rate of 0.01 mV/s. The purpose of this study was to calculate the distance between the oxidation-reduction reaction peaks to determine lithium-ion diffusion. As the battery charges, oxidation takes place, and ions move towards the anode. Conversely, during discharging, reduction occurs, and ions return to the cathode. The redox voltage difference value is crucial in determining reversibility. A smaller value indicates closer peaks, requiring less energy for the reaction cycle.

B

A

Figure 8. dQ/dV curve against voltage for all cathode samples: (a) holding time 9 hours; (b) holding time 12 hours

According to Figure 8, the sample that was calcined at 750oC-9h hours exhibits the smallest difference in redox voltage, measuring 1.82 V, with an oxidation peak at 4.21 V and a reduction peak at 2.39 V. On the other hand, the sample calcined at 900oC -12h shows the largest redox voltage difference, which is 2.30 V, with an oxidation peak at 4.21 V and a reduction peak at 1.91 V. It is evident that samples calcined at 750°C demonstrate the smallest redox voltage difference compared to those calcined at 800°C, 850°C, and 900°C. Additionally, the holding time also plays a significant role, as samples with a holding time of 9 hours exhibit a smaller difference in redox voltage compared to those held for 12 hours. Furthermore, Figure 4.8 illustrates a narrow and sharp curve peak, suggesting that lithium ions can quickly intercalate and deintercalate [19]. Moreover, a smaller distance between the reduction-oxidation reaction peaks indicates faster intercalation and deintercalation processes of lithium ions [17].

CONCLUSIONS

Based on the research that has been carried out, the synthesis results of the NMC 811 cathode which was calcined at all samples can influence the morphology of the grains formed, where the higher the calcination temperature and the longer the holding time, the more uniform the morphology. The granules make the particle diameter slightly larger. The synthesis results of the NMC 811 cathode which was calcined at all samples produced a hexagonal structure. The higher the calcination temperature and the longer the holding time can also reduce the crystal size and not change the hexagonal structure. The NMC 811 sample calcined at a temperature of 750oC, and the sample with a holding time of 9 hours overall had a higher battery retention capacity than the other samples.

The largest battery retention capacity was found in the 750oC-9h sample at 84.93%. Meanwhile, the smallest battery retention capacity was found in the 900oC-12h sample at 57.97%. High calcination temperatures and long holding times tend to reduce the reversibility of oxidation-reduction reactions during the charge-discharge cycle, as seen from the increasing difference in redox potential peaks in the CV measurement curve. The smallest redox peak potential difference was obtained in the 750oC-9h sample, namely 1.82 V. Meanwhile, the largest redox peak potential difference was obtained in the 900oC-12h sample, namely 2.30 V. Based on EIS measurement data, the best ion conductivity value was obtained for the 750oC-9h sample, namely 0.713 S/cm. This corresponds to the lowest cation mixing value with a peak ratio of I(003)/I(104) of 2.10.

REFERENCES

[1]	W. Li, S. Lee, and A. Manthiram, “High‐Nickel NMA: A Cobalt‐Free Alternative to NMC and NCA Cathodes for Lithium‐Ion Batteries,” Advanced Materials, vol. 32, no. 33, Aug. 2020, doi: 10.1002/adma.202002718.

[2]	S. Lei, Y. Shi, and G. Chen, “A lithium-ion battery-thermal-management design based on phase-change-material thermal storage and spray cooling,” Appl Therm Eng, vol. 168, Mar. 2020, doi: 10.1016/j.applthermaleng.2019.114792.

[3]	Dipl.-I. M. Westermeier, I. G. Reinhart, and Dr.-I. Tobias Zeilinger, “Method for Quality Parameter Identification and  Classification in Battery Cell Production,” IEEE 2013 3rd International Electric Drives Production Conference (EDPC)-Nuremberg, Germany, 2013. doi: 10.1109/EDPC.2013.6689742.

[4]	H. Zhang and J. Zhang, “An overview of modification strategies to improve LiNi0·8Co0·1Mn0·1O2 (NCM811) cathode performance for automotive lithium-ion batteries,” eTransportation, vol. 7. Elsevier B.V., Feb. 01, 2021. doi: 10.1016/j.etran.2021.100105.

[5]	S. Lee and A. Manthiram, “Can Cobalt Be Eliminated from Lithium-Ion Batteries?,” ACS Energy Letters, vol. 7, no. 9. American Chemical Society, pp. 3058–3063, Sep. 09, 2022. doi: 10.1021/acsenergylett.2c01553.

[6]	W. Tang et al., “An effective etching-induced coating strategy to shield LiNi0.8Co0.1Mn0.1O2 electrode materials by LiAlO2,” J Power Sources, vol. 412, pp. 246–254, Feb. 2019, doi: 10.1016/j.jpowsour.2018.11.062.

[7]	K. Park et al., “High‐Capacity Concentration Gradient Li[Ni 0.865 Co 0.120 Al 0.015 ]O 2 Cathode for Lithium‐Ion Batteries,” Adv Energy Mater, vol. 8, no. 19, Jul. 2018, doi: 10.1002/aenm.201703612.

[8]	J.-H. Kim, K.-J. Park, S. J. Kim, C. S. Yoon, and Y.-K. Sun, “A method of increasing the energy density of layered Ni-rich Li[Ni 1−2x Co x Mn x ]O 2 cathodes ( x = 0.05, 0.1, 0.2),” J Mater Chem A Mater, vol. 7, no. 6, pp. 2694–2701, 2019, doi: 10.1039/C8TA10438G.

[9]	J. Zheng, W. H. Kan, and A. Manthiram, “Role of Mn Content on the Electrochemical Properties of Nickel-Rich Layered LiNi 0.8– x Co 0.1 Mn 0.1+ x O 2 (0.0 ≤ x ≤ 0.08) Cathodes for Lithium-Ion Batteries,” ACS Appl Mater Interfaces, vol. 7, no. 12, pp. 6926–6934, Apr. 2015, doi: 10.1021/acsami.5b00788.

[10]	K. M. Shaju, G. V. Subba Rao, and B. V. R. Chowdari, “Performance of layered Li(Ni1/3Co1/3Mn1/3)O2 as cathode for Li-ion batteries,” Electrochim Acta, vol. 48, no. 2, pp. 145–151, Nov. 2002, doi: 10.1016/S0013-4686(02)00593-5.

[11]	X. Yao et al., “Oxalate co-precipitation synthesis of LiNi0.6Co0.2Mn0.2O2 for low-cost and high-energy lithium-ion batteries,” Mater Today Commun, vol. 19, pp. 262–270, Jun. 2019, doi: 10.1016/j.mtcomm.2019.02.001.

[12]	W. Zhao et al., “Optimized Al doping improves both interphase stability and bulk structural integrity of Ni-rich NMC cathode materials,” ACS Appl Energy Mater, vol. 3, no. 4, pp. 3369–3377, 2020.

[13]	J. Zhang, J. Qiao, K. Sun, and Z. Wang, “Balancing particle properties for practical lithium-ion batteries,” Particuology, vol. 61, pp. 18–29, Feb. 2022, doi: 10.1016/j.partic.2021.05.006.

[14]	P. Luo and Z. Huang, “Fabrication of scandium-doped lithium manganese oxide as a high-rate capability cathode material for lithium energy storage,” Solid State Ion, vol. 338, pp. 20–24, Oct. 2019, doi: 10.1016/j.ssi.2019.05.006.

[15]	H. Xie et al., “Synthesis of LiNi 0.8 Co 0.15 Al 0.05 O 2 with 5-sulfosalicylic acid as a chelating agent and its electrochemical properties,” J Mater Chem A Mater, vol. 3, no. 40, pp. 20236–20243, 2015, doi: 10.1039/C5TA05266A.

[16]	D. Mouraliraman et al., “Thermally Stable PVDF-HFP-Based Gel Polymer Electrolytes for High-Performance Lithium-Ion Batteries,” Nanomaterials, vol. 12, no. 7, p. 1056, Mar. 2022, doi: 10.3390/nano12071056.

[17]	C. J. Jafta, K. I. Ozoemena, M. K. Mathe, and W. D. Roos, “Synthesis, characterisation and electrochemical intercalation kinetics of nanostructured aluminium-doped Li[Li0.2Mn0.54Ni0.13Co0.13]O2 cathode material for lithium ion battery,” Electrochim Acta, vol. 85, pp. 411–422, Dec. 2012, doi: 10.1016/j.electacta.2012.08.074.

[18]	X. Jin, Q. Xu, H. Liu, X. Yuan, and Y. Xia, “Excellent rate capability of Mg doped Li[Li0.2Ni0.13Co0.13Mn0.54]O2 cathode material for lithium-ion battery,” Electrochim Acta, vol. 136, pp. 19–26, Aug. 2014, doi: 10.1016/j.electacta.2014.05.043.

[19]	J. Pires et al., “Tris(2,2,2-trifluoroethyl) phosphite as an electrolyte additive for high-voltage lithium-ion batteries using lithium-rich layered oxide cathode,” J Power Sources, vol. 296, pp. 413–425, Nov. 2015, doi: 10.1016/j.jpowsour.2015.07.065.