Incorporation of silica from rice husk ash into chitosan-polyvinyl alcohol composite membranes for direct methanol fuel cell applications

Mochammad Purwanto1,a,*, Ayu Oktari Rahman2,b, Umi Sholikah2,c, Riza Hudayarizka2,d, Dian Permana3,e,*, Edi Ilimu3,f, Musyarofah4,g, Lukman Atmaja5,h

Author Affiliations

1Department of Chemical Engineering, Institut Teknologi Kalimantan, Balikpapan 76127, Indonesia

2Department of Environmental Engineering, Institut Teknologi Kalimantan, Balikpapan 76127, Indonesia

3Department of Chemistry Education, Universitas Sembilanbelas November Kolaka, Kolaka 93517, Indonesia

4Department of Physics, Institut Teknologi Kalimantan, Balikpapan 76127, Indonesia

5Department of Chemistry, Faculty of Science and Data Analytics, Institut Teknologi Sepuluh Nopember, Surabaya 60111, Indonesia

Author Emails :
a)Corresponding author: m.purwanto@lecturer.itk.ac.id

b)13181012@student.itk.ac.id

c) umisholikah@lecturer.itk.ac.id

d)riza.hudayarizka@lecturer.itk.ac.id

f)ediilimu@gmail.com

g)musyarofah@lecturer.itk.ac.id

h)lukman_at@chem.its.ac.id

Abstract. Direct Methanol Fuel Cell (DMFC) is a part of fuel cell technology that converts electrochemical energy using a liquid methanol solution as fuel. One of the important components in the DMFC system is the proton exchange membrane (PEM) which functions as a proton conductor and separator between the cathode and anode. An organic polymer-based material that is interesting to develop is a combination of chitosan and Polyvinyl alcohol (PVA). To improve its performance, in this research, silica extracted from rice husk ash has been incorporated into the chitosan-PVA composite membrane. Membrane synthesis was carried out via the phase inversion method using acetic acid as a solvent. The integration of silica derived from locally grown rice husk waste presents a novel strategy to enhance the morphological density and overall performance of the chitosan–PVA composite membrane. Membrane performance analysis was carried out by testing water and methanol uptake, ion exchange capacity, methanol permeability and proton conductivity. The best water uptake value was 60% while the lowest methanol uptake was 26%, both of which were obtained on the Ch-PVA/Silica 15 membrane. The best ion exchange capacity and methanol permeability values were also obtained on the Ch-PVA/Silica 15 membrane with a value of 1.68 mmol.g-1 and 2.03 x 10-6 cm2.s-1, respectively. The test results have confirmed that the incorporation of silica from rice husk ash into the chitosan-PVA composite membrane shows good performance in direct methanol fuel cell applications.

# INTRODUCTION

Fossil energy consumed in high quantities causes an increase in greenhouse gas emissions which results in an unstable climate, an increase in the earth's temperature and rising sea levels (1). Apart from that, fossil fuels are non-renewable natural resources, making the availability of fossil fuels in the world increasingly depleted (2). All countries around the world are considering the creation of alternative and sustainable resources. Fuel cell technology is an interesting option to develop, namely by converting chemical energy into electrical energy (3,4). Direct methanol fuel cell (DMFC) is a type of fuel cell based on electrochemical energy using a liquid methanol solution as fuel.

The electrolyte membrane is one of the important components of a fuel cell which functions as a proton conductor and separator between the cathode and anode (5). Perfluorosulfonic acid (Nafion) is the material most widely used commercially for electrolyte membranes, because it has high proton conductivity, but it still has several disadvantages, including being relatively expensive, high methanol crossover, and easily dehydrated at high temperatures (6). Therefore, various efforts have been made to produce good alternative membranes for fuel cell applications. The use of organic-based materials is considered to have the opportunity to overcome this problem. Chitosan is a biopolymer that can be used as an electrolyte membrane which can be obtained from crustacean shells (7,8). Modification of chitosan with other materials is known to improve the quality of electrolyte membranes (9). In previous research, it was reported that modification of chitosan with phosphotungstic acid showed an increase in ion exchange capacity values (10).

Polyvinyl alcohol (PVA) has good potential for collaboration with chitosan because of its several superior properties, including ease of preparation, excellent film formation, and reactive chemical properties that are favorable for cross-linking thereby providing a proton pathway that can increase its conductivity (11,12). In addition, in order to improve the performance of chitosan-based electrolyte membranes, it is necessary to add a number of additives in the membrane synthesis process (13). In this research, the addition of silica additives was prepared from rice husk ash obtained from local agricultural waste. The addition of this silica additive can have a good influence in DMFC applications because the hydrophobic nature of the hybrid membrane can reduce methanol permeability so that the crossover will be smaller (14,15). The addition of silica to chitosan-based membranes which show low methanol permeability has also been reported in previous studies (14).

This research will focus on the synthesis of chitosan and chitosan/PVA-based biopolymer electrolyte membranes with the addition of silica additives, which aims to produce membranes with low methanol permeability and high ion exchange capacity. In the initial stage, chitosan is extracted from shrimp shell waste, while silica is synthesized from rice husk ash. The properties and characteristics of the synthesized membrane will be determined to support its properties and performance in direct methanol fuel cell applications.

MATERIALS AND METHODS

Materials

Shrimp shell powder that has passed a 100-mesh sieve as raw material for the extraction of chitosan biopolymer, rice husks obtained from agricultural waste as a source of silica. Hydrochloric acid (HCl), acetic acid (CH3COOH), sodium hydroxide (NaOH) were purchased from Sigma Aldrich. Sodium Chloride (NaCl), Methanol (CH3OH), phenolphthalein (PP) indicator and polyvinyl alcohol (PVA) were purchased from Merck.

Preparation of Chitosan Extraction

Chitosan extraction consists of three steps, the first is deproteination by heating and stirring shrimp shell powder in 3.5% NaOH solution with a ratio of 1:10 (w/v) at 70 ºC for 2 hours. The samples were washed with distilled water until the pH was neutral and then dried in an oven. The second stage is demineralization, namely the dried powder is stirred in a 1M HCl solution with a ratio of 1:10 (w/v) at 70 ºC for 2 hours. The samples were washed with distilled water until the pH was neutral and then dried in an oven. The resulting dry powder obtained at this stage is called chitin. The third stage is deacetylation, chitin is stirred in 50% NaOH solution with a ratio of 1:10 (w/v) at 120 ºC for 2 hours. The sample was washed with distilled water until the pH was neutral and then dried in an oven to obtain a dry powder, called chitosan.

Preparation of Silica from Rice Husk Ash

The cleaned rice husks are burned using a furnace at a temperature of 600 ºC for 3 hours. Next, the ash from the combustion is crushed and sieved at 200 mesh. The ash resulting from the sieving was put into a 6 M HCl solution with a ratio of 1:7.5 (w/v) and stirred at a temperature of 105 oC for 2 hours. The precipitate obtained was then filtered and washed repeatedly using distilled water until the pH was neutral. The precipitate was dried in an oven at 105 °C for 1 hour, then ground using a pestle and mortar to produce a fine powder.

Membrane fabrication

Acetic acid solution with a concentration of 2% was prepared in an amount of 75 ml and divided into 2 beaker glasses. The first beaker glass was filled with 37.5 ml of acetic acid and chitosan powder was added at a temperature of 80 °C and stirred at 400 rpm for 30 minutes. In the other part, 37.5 ml of acetic acid was added with PVA-Silica powder and sonicated for 30 minutes. The two mixtures were combined into one and stirred at 400 rpm at a temperature of 80 °C for 30 minutes. Furthermore, the mixture was given a sonication treatment for 30 minutes, then lifted and left at room temperature for 30 minutes. The mixture was sonicated again for 30 minutes, then poured into a mold and dried at room temperature for 7 days.

Membrane Characterizations

The membrane was prepared with a size of 2 x 2 cm2 and dried in an oven at a temperature of 50°C for 1 hour. The dried membrane was weighed as the initial weight (Wdry) and then soaked in water or 1 M methanol solution for 24 hours. Then the membrane was lifted and weighed as the wet weight (Wwet). The determination of water and methanol absorption values ​​was calculated using equation (1).

Uptake (%) = W wet - W dryW dry x 100          … (1)

Determination of ion exchange capacity (IEC) value was carried out by titration method using 0.01 M NaOH solution. In the initial stage, the membrane was prepared with a size of 2 x 2 cm2 and weighed as dry weight (Wdry). Furthermore, the membrane was soaked in 0.1 M HCl solution for 24 hours. The membrane was removed and cleaned, then soaked in 0.1 M NaCl solution for 24 hours, as a second protonate. The ion exchange capacity value was calculated using equation (2).

IEC (mmol/gram) = V x CW dry 	          … (2)

Where IEC is the Ion Exchange Capacity (mmol/gram), C is the concentration of NaOH (M), V is the volume of NaOH used to neutralize NaCl (mL), and Wdry is the dry weight of the membrane (gr).

Methanol permeability was analyzed using a two-compartment diffusion cell, with the membrane clamped and placed between the two compartments. Compartments A and B were filled with 1M methanol solution and deionized water, respectively. Water in compartment B was taken with a pipette every 30 minutes and put into a pycnometer and then weighed. The water collection process was repeated for up to 180 minutes. Methanol permeability was calculated using equation (3).

P (cm2.s-1) = (ΔCBΔt).(L VBA CA)           … (3)

Where P is the methanol permeability (cm2.s-1), ΔCB/Δt is the slope of the variation of methanol concentration in compartment B with a function of time (mol.L-1.s-1), VB is the volume of water in compartment B (cm3), L is the membrane thickness (cm), CA is the methanol concentration in compartment A (mol.L-1), and A is the contact/diffusion area of ​​the membrane connected in the compartment (cm2).

RESULTS AND DISCUSSIONS

Membrane Fabrication

Chitosan preparation has been successfully carried out from shrimp shell waste through three important stages, namely deproteination, demineralization, and deacetylation. In the first stage, deproteination is intended to remove the protein content in shrimp shells. While in the demineralization stage, it aims to remove the mineral content in shrimp shells (16). From the two stages of the process, an intermediate product is produced in the form of chitin, which contains an acetyl group. In the next stage, a further process is carried out in the form of removing the acetyl group through the deacetylation stage (17,18). This stage is intended to break the bond of the acetyl group (-COCH3) which is bound to the nitrogen atom (N) in chitin and replace the bond with an amine group (-NH2), which is a typical group of chitosan. The chitosan obtained is in the form of a white powder as shown in Figure 1 (a).

Figure 1. Chitosan powder (a), silica (b) and chitosan-PVA/Silica composite membrane (c)

Silica synthesis has been carried out using rice husk waste using the ashing and purification method. During the ashing process, the hydrocarbons in the rice husk decompose releasing water vapor and CO2 gas. After the ash is formed, the purification process is carried out using an acid solution and dried until white silica powder is obtained, as shown in Figure 1 (b). Membrane fabrication with the collaboration of chitosan and polyvinyl alcohol with a combination of silica has been carried out through the phase inversion method using acetic acid solvent. The results of the membrane fabrication show a flat surface morphology as shown in Figure 1 (c). To prepare the membrane to support its properties as a proton conductor medium in fuel cell applications, a coupling agent has been carried out by immersing the membrane in H2SO4 solution to present sulfonate groups in the membrane structure layer.

Figure 2. FTIR spectra from chitosan and silica

Analysis of the structure and functional groups of the Ch/PVA-Silica composite membrane with FTIR spectra is presented in Figure 1. The typical characteristics of chitosan are shown at wave numbers 3375 cm-1, 1623 cm-1 and 1547 cm-1 which are hydroxyl, amide I and amide II groups, respectively. The peaks at 1407 cm-1 and 1026 cm-1 indicate the presence of –CH2 bending and C–O stretching, respectively (19). In addition, the typical characteristics of silica can also be seen from the presence of Si-O groups from Si-O-Si at wave numbers 1073.84 cm-1, and Si-O groups from Si-OH at wave numbers 796.57 cm-1.

Water and methanol uptake

Water and methanol uptake was carried out to determine the characteristics of the membrane produced in absorbing water and methanol (20). During the process of converting chemical energy into electrical energy in fuel cell applications, the membrane is required to be hydrated as a proton delivery medium. Therefore, good water uptake properties can support membrane performance in direct methanol fuel cell applications. In contrast to testing the properties of methanol uptake, a good membrane is a membrane that absorbs little methanol. This is because methanol on the anode side should not enter the membrane structure layer because it can interfere with its effectiveness. Thus, membranes with small methanol uptake values ​​are preferred in this application. The water and methanol uptake test can be shown in Figure 3.

Figure 3. Water and methanol uptake of Ch/PVA-silica membranes

Figure 3 shows the water uptake value increases with increasing silica load in the membrane structure layer. The highest water uptake value of 61% was obtained in the Ch/PVA-Silica 15 membrane. Increasing the composition of silica in the membrane can affect the increase in water absorption, this is due to the presence of the -SO2 group, which has the role of the O group with electronegativity strength so that it can interact through hydrogen bonds with water. Water that diffuses into the membrane can be trapped to pass through the empty cavities in the membrane so that the water absorption capacity of the membrane increases (21). In previous studies (22), it has been reported that the addition of silica in the chitosan-based membrane structure layer shows an increase in the water uptake value along with the increasing amount of silica filler load in the membrane structure layer. However, methanol uptake test showed a decreasing trend on Ch/PVA-Silica membrane as shown in Table 1.

Table 1. Water and methanol uptake Ch/PVA-Silica membrane composite

| Membranes | Water Uptake (%) | Methanol Uptake (%) |
| --- | --- | --- |
| Ch/PVA-Silica 5 | 20 | 81 |
| Ch/PVA-Silica 10 | 55 | 36 |
| Ch/PVA-Silica 15 | 61 | 27 |

Table 1 shows that the results of the methanol uptake test show a downward trend along with the increasing silica filler load in the membrane. The lowest methanol uptake value of 26% was obtained on the Ch/PVA-Silica 15 membrane. This phenomenon indicates that the addition of silica to the membrane can increase the density in the membrane structure layer so that the amount of methanol entering the membrane is small. A low methanol uptake value means that it supports the resistance of the membrane properties to prevent methanol from entering the membrane which has the potential to reduce its effectiveness in the fuel cell system. A good membrane is a membrane that has a small methanol uptake value which indicates that the membrane obtained is able to withstand the movement of methanol through the membrane (23).

Ion Exchange Capacity (IEC)

Ion Exchange Capacity testing is carried out to determine how many protons can be bound in the membrane structure layer. This parameter is important as an analysis of the potential quality of the membrane as a medium for proton pathways. Electrolyte membranes that are able to bind large amounts of protons will have the opportunity for optimal performance in DMFC applications (24). The results of the IEC value test for the Ch/PVA-Silica composite membrane can be shown in Figure 4. The highest IEC value of 1,676 mmol/gram was obtained in the Ch/PVA-Silica 15 membrane. In general, increasing the amount of silica in the membrane composition causes an increase in the IEC value. The phenomenon of increasing IEC values ​​with the role of silica in polymer-based membranes has also been reported by previous researchers (13).

Figure 4. Ion Exchange Capacity for Ch/PVA-Silica membranes

In addition to the role of silica, in this type of membrane the presence of PVA charge also has a good impact on the characteristics of the membrane. The presence of PVA in the membrane structure layer provides an opportunity to increase the proton binding activity of the membrane during the immersion process in solution. The functional group (-OH) contained in PVA has an impact on the binding and uptake of protons by the membrane during immersion (25). The collaboration of materials in the membrane has a good impact on its characteristics in proton binding, which is an important parameter for membrane quality for fuel cell applications. Membranes that have a lot of proton binding capacity will have the opportunity as a path for large numbers of protons, thereby increasing their performance in DMFC applications.

Methanol Permeability

Electrolyte membranes can work well in fuel cell systems if there is no interference, for example methanol crossing from the anode into the membrane structure. The phenomenon of methanol entering the membrane is called methanol crossover, which has an impact on decreasing the performance of the electrolyte membrane (3,26). The analysis that can be done to measure the symptoms of methanol crossover is through methanol permeability testing. A membrane that has high methanol permeability means that it is not resistant to methanol crossover attacks, conversely if the methanol permeability is low, the membrane has the ability to reject methanol and can prevent methanol crossover from occurring. The results of the methanol permeability test for the Ch/PVA-Silica composite membrane are shown in Figure 5.

Figure 5. Methanol permeability for Ch/PVA-Silica composite membranes

Figure 5 shows that the methanol permeability value decreases along with the decrease in the silica filler load in the membrane composition. The role of silica as a filler can fill the empty spaces in the chitosan and PVA-based membranes, making the membrane denser and stronger. This property greatly supports the membrane's resistance in preventing the movement of methanol from the anode into the membrane structure, thereby reducing the possibility of methanol crossover. The Ch/PVA–Silica 15 composite membrane exhibited the lowest methanol permeability value of 2.03 × 10⁻⁶ mg·cm²/s, indicating superior resistance to methanol crossover compared to Nafion 117, which recorded a permeability of 2.74 × 10⁻⁶ cm²/s (27). The trend of decreasing methanol permeability values ​​has also been reported in previous studies (28), with the presence of silica loads on nafion-based membranes showing a decreasing methanol permeability value.

# CONCLUSION

The incorporation of silica into the chitosan/PVA membrane through phase inversion has been successfully demonstrated. Among the prepared membranes, Ch/PVA-Silica 15 exhibited the best balance of properties, with high water uptake (61%), low methanol uptake (26%), the highest ion exchange capacity (1.676 mmol/g), and the lowest methanol permeability (2.03 × 10⁻⁶ cm²/s). These results indicate that the Ch/PVA-Silica composite membrane is a promising candidate for direct methanol fuel cell applications. However, its long-term stability has not been evaluated, which remain as limitations. Future work should focus on enhancing conductivity and durability, for example through crosslinking strategies, incorporation of hybrid fillers, or stability testing under fuel cell operating conditions.

# Acknowledgments

The authors would like to thank the Chemical Engineering Laboratory and the Institute for Research and Community Service, Institut Teknologi Kalimantan for their support. The authors would also like to thank the Ministry of Education, Research, and Technology, Indonesia for the grant funding for this research.

# References

1. 	Setyono AE, Kiono BFT. Dari Energi Fosil Menuju Energi Terbarukan: Potret Kondisi Minyak dan Gas Bumi Indonesia Tahun 2020 – 2050. J Energi Baru dan Terbarukan. 2021;2(3):154–62.

2. 	Noviyanti AR, Yuliyati YB, Eddy DR, Solihudin, Tjokronegoro R. Struktur Dan Morfologi Elektrolit Apatit Lantanum Silikat Berbahan Dasar Silika Sekam Padi. J Mater dan Energi Indones. 2016;06(02):1–6.

3. 	Ravichandran T, Jaafar J, Ilbeygi H, Purwanto M. Review on the development of fuel cells and its future prospects. J Teknol. 2021;83(3):75–84.

4. 	Song F, Fu Y, Gao Y, Li J, Qiao J, Zhou XD, et al. Novel Alkaline Anion-exchange Membranes Based on Chitosan/Ethenylmethylimidazoliumchloride Polymer with Ethenylpyrrolidone Composites for Low Temperature Polymer Electrolyte Fuel Cells. Electrochim Acta [Internet]. 2015;177:137–44. Available from: http://dx.doi.org/10.1016/j.electacta.2015.02.015

5. 	Das S, Dutta K, Nessim GD, Kader MA. 1 - Introduction to direct methanol fuel cells. In: Dutta K, editor. Direct Methanol Fuel Cell Technology [Internet]. Elsevier; 2020. p. 1–12. Available from: https://www.sciencedirect.com/science/article/pii/B978012819158300001X

6. 	Lufrano F, Baglio V, Staiti P, Antonucci V, Arico’ AS. Performance analysis of polymer electrolyte membranes for direct methanol fuel cells. J Power Sources [Internet]. 2013;243:519–34. Available from: http://dx.doi.org/10.1016/j.jpowsour.2013.05.180

7. 	Cheba BA. Chitosan: Properties, modifications and food nanobiotechnology. Procedia Manuf [Internet]. 2020;46(2019):652–8. Available from: https://doi.org/10.1016/j.promfg.2020.03.093

8. 	Doobi FA, Mir FQ. Exploring the development of natural biopolymer (chitosan)-based proton exchange membranes for fuel cells: A review. Results in Surfaces and Interfaces [Internet]. 2024;15(April):100218. Available from: https://doi.org/10.1016/j.rsurfi.2024.100218

9. 	Lewandowska K. Characterization of chitosan composites with synthetic polymers and inorganic additives. Int J Biol Macromol [Internet]. 2015;81:159–64. Available from: http://dx.doi.org/10.1016/j.ijbiomac.2015.08.003

10. 	Purwanto M, Widiastuti N, Gunawan A. Preparation and Properties of Chitosan / Montmorillonite Supported Phosphotungstic Acid Composite Membrane for Direct Methanol Fuel Cell Application. 2021;31(7):375–81.

11. 	Hari Gopi K, Dhavale VM, Bhat SD. Development of polyvinyl alcohol/chitosan blend anion exchange membrane with mono and di quaternizing agents for application in alkaline polymer electrolyte fuel cells. Mater Sci Energy Technol [Internet]. 2019;2(2):194–202. Available from: https://doi.org/10.1016/j.mset.2019.01.010

12. 	Liao GM, Yang CC, Hu CC, Pai YL, Lue SJ. Novel quaternized polyvinyl alcohol/quaternized chitosan nano-composite as an effective hydroxide-conducting electrolyte. J Memb Sci [Internet]. 2015;485:17–29. Available from: http://dx.doi.org/10.1016/j.memsci.2015.02.043

13. 	Liu G, Tsen WC, Wen S. Sulfonated silica coated polyvinylidene fluoride electrospun nanofiber-based composite membranes for direct methanol fuel cells. Mater Des [Internet]. 2020;193:108806. Available from: https://doi.org/10.1016/j.matdes.2020.108806

14. 	Purwanto M, Widiastuti N, Saga BH, Gusmawan H. Synthesis of Composite Membrane Based Biopolymer Chitosan with Silica from Rice Husk Ash for Direct Methanol Fuel Cell Application. IOP Conf Ser Earth Environ Sci. 2021;830(1).

15. 	Liu H, Gong C, Wang J, Liu X, Liu H, Cheng F, et al. Chitosan/silica coated carbon nanotubes composite proton exchange membranes for fuel cell applications. Carbohydr Polym [Internet]. 2016;136:1379–85. Available from: http://dx.doi.org/10.1016/j.carbpol.2015.09.085

16. 	Trisnawati E, Andesti D, Saleh A. Pembuatan Kitosan dari Limbah Cangkang Kepiting sebagai Bahan Pengawet Buah Duku dengan Variasi Lama Pengawetan. J Tek Kim. 2013;19(2):17–26.

17. 	Nugraeni CD, Atmaja L, Hayati N, Purwanto M, Santoso M, Kusumawati Y. Fabrication and Characterization of Chitosan/N-Phthaloyl Composite Membrane for DMFC Application. J Ris Kim. 2021;12(2):143–50.

18. 	Agusta I. Ekstraksi Kitosan Dari Limbah Kulit Udang Dengan Proses Deasetilasi. CHEMTAG J Chem Eng. 2021;2(2):38.

19. 	Atmaja L, Purwanto M, Salleh MT, Mohamed MA, Jaafar J, Ismail AF, et al. GPTMS-Montmorillonite-filled biopolymer chitosan membrane with improved compatibility, physicochemical, and thermal stability properties ochemical and thermal stability properties. Malaysian J Fundam Appl Sci. 2019;15(4):492–7.

20. 	Proton K, Hidrofil S, Kitosan K, Gptms M, Langsung AM. Correlation Between Proton Conductivity, Hydrophilicity, and Thermal Stability of Chitosan/Montmorillonite Composite Membrane Modified Gptms and Their Performance in Direct Methanol Fuel Cell. Malaysian J Anal Sci. 2017;21(3):675–89.

21. 	Ma J, Sahai Y. Chitosan biopolymer for fuel cell applications. Carbohydr Polym [Internet]. 2013;92(2):955–75. Available from: http://dx.doi.org/10.1016/j.carbpol.2012.10.015

22. 	Ranjani M, Pannipara M, Al-Sehemi AG, Vignesh A, kumar GG. Chitosan/sulfonated graphene oxide/silica nanocomposite membranes for direct methanol fuel cells. Solid State Ionics [Internet]. 2019;338(May):153–60. Available from: https://doi.org/10.1016/j.ssi.2019.05.010

23. 	S. AB, Handika G, Purwanto M, Pramono E, Linaya R. C. Electrolyte Membrane Composite from Modified Chitosan-Vanillin and Zeolite Filler for Direct Methanol Fuel Cell Application. 2020;94–9.

24. 	Shirdast A, Sharif A, Abdollahi M. Effect of the incorporation of sulfonated chitosan/sulfonated graphene oxide on the proton conductivity of chitosan membranes. J Power Sources [Internet]. 2016;306:541–51. Available from: http://dx.doi.org/10.1016/j.jpowsour.2015.12.076

25. 	Kakati N, Maiti J, Das G, Lee SH, Yoon YS. An approach of balancing the ionic conductivity and mechanical properties of PVA based nanocomposite membrane for DMFC by various crosslinking agents with ionic liquid. Int J Hydrogen Energy [Internet]. 2015;40(22):7114–23. Available from: http://dx.doi.org/10.1016/j.ijhydene.2015.04.004

26. 	Permana D, Atmaja L, Priyangga A, Kedang YI, Santoso M. Utilization of cellulose-based carbon nanodots in sulfonated polysulfone based membrane for direct methanol fuel cell. South African J Chem Eng [Internet]. 2024;48(October 2023):265–75. Available from: https://doi.org/10.1016/j.sajce.2024.02.009

27. 	Muhmed SA, Jaafar J, Daud SS, Hanifah MFR, Purwanto M, Othman MHD, et al. Improvement in properties of nanocrystalline cellulose/poly (vinylidene fluoride) nanocomposite membrane for direct methanol fuel cell application. J Environ Chem Eng [Internet]. 2021;9(4):105577. Available from: https://doi.org/10.1016/j.jece.2021.105577

28. 	Li J, Xu G, Luo X, Xiong J, Liu Z, Cai W. Effect of nano-size of functionalized silica on overall performance of swelling-filling modified Nafion membrane for direct methanol fuel cell application. Appl Energy [Internet]. 2018;213:408–14. Available from: https://www.sciencedirect.com/science/article/pii/S0306261918300643