Understanding the Mechanisms of Antimicrobial Action in Tungsten Carbide - Nickel Sulphide Composites

Kathryn Kiruba1 , S.Madhav1,a)

1Kathy Home Health Solutions, Vijayawada, Andhra Pradesh, India

Corresponding Author: a)madhav.152501022.saveetha@gmail.com

Abstract: Nanotechnology has enormously progressed the advancement of antimicrobial specialists, driven by the challenge of microbial resistance. Among these developments, tungsten carbide-nickel sulfide (WC-NiS) nanocomposites have appeared with surprising potential due to their one-of-a-kind physicochemical properties. Tungsten carbide, famous for its hardness and erosion resistance, disturbs microbial cell dividers and DNA, showing solid biocompatibility and negligible harmfulness. Nickel sulfide upgrades antimicrobial productivity through biofilm penetration and oxidative stress induction. This study centers on the amalgamation, characterization, and antifungal assessment of WC-NiS composites. Tungsten carbide was synthesized through diminishment with hydrogen gas, followed by a response with dicyandiamide. Nickel sulfide was arranged by responding nickel nitrate with sodium sulfide. The composite was shaped through microwave illumination, followed by exhaustive washing, drying, and calcination.  Characterization procedures such as UV-DRS spectroscopy, X-ray diffraction (XRD), Fourier-transform infrared spectroscopy (FTIR), and transmission electron microscopy (TEM) affirmed the composite's auxiliary and optical properties. These investigations uncovered a crystalline structure with tall absorbance within the unmistakable range, well-defined useful bunches, and nanoscale morphology, guaranteeing its appropriateness for antimicrobial applications.  The antifungal movement was evaluated utilizing the disk dissemination strategy against Candida albicans and Aspergillus species. Comes illustrated a concentration-dependent increment in zones of hindrance, highlighting the composite's strong antifungal viability. At 100 μL, hindrance zones come to 50 mm for Candida albicans and 25 mm for Aspergillus. This investigation underscores the potential of WC-NiS composites in treating parasitic diseases, especially against pathogens like Candida albicans and Aspergillus. Future studies should investigate biocompatibility and broader biomedical applications to realize the composite's capabilities fully.

Keywords: Nanocomposites, nickel nanoparticles, ammonium metatungstate, nonmetallic compounds, High-resolution Transform electron microscopy

# INTRODUCTION

Nanotechnology has vastly expanded in diverse industries using nanocomposites. Nanocomposites exhibit specific and size-dependent physical and chemical properties, thus are greatly sought after in biomedicine and engineering (Bankier et al., 2019). Hence, the last decade has seen an increasing interest and in-depth studies into overcoming microbial resistance with the development of new antimicrobial agents deriving from multiple sources  (Mounyr et al., 2016). Such features or physicochemical characteristics of nanocomposites, particularly those that combine metallic and nonmetallic compounds, provide possible solutions.Nanocomposites of tungsten carbide (WC) and nickel sulphide (NiS) have promising prospects. Tungsten carbide is the hardest material after diamond, and it can withstand harsh conditions for longer periods of exposure  (Hoque et al., 2022). The virucidal activity increased with longer incubation periods found in WC-NiS. The higher virus concentration in the aliquots revealed that virucidal activity was due to a dose-related effect(Ramsundar et al., 2023; Rieshy et al., 2023; Singh et al., 2023). The corrosion-resistant property of tungsten carbide ensures that its antimicrobial effects can persist even under extreme conditions. Studies have shown that WC can destroy the cell wall membranes and DNA by microbes, thus leading finally to cell death. This has been one of the major reasons this is suitable for microbiological applications (as it has been found to be very biocompatible and cleverly devoid of toxicity towards microbes) In the research work done by Gu et al, 2015, Nickel sulphide showed tremendous catalytic properties along with antibacterial action against several microorganisms due to penetrating biofilms of microbes and disrupting their growth and replication. The research paper presented by Gomaji et al. 2015 focuses on the chemically reduced nickel nanoparticles (Ni NPs) ' antimicrobial activity. A corresponding research paper by Wang et al. (2017) discussed how NiS nanoparticles disrupt microbial membranes and induce the production of reactive oxygen species (ROS). This creates an oxidative environment that halts bacterial growth. These findings will be incorporated into dental materials to help combat microbial colonization effectively(Pavithra et al., 2023; Shenoy et al., 2023; Thomas & Jain, 2023).Candida albicans and Aspergillus are the most prevalent fungi in human diseases. Candida albicans is the most common fungal species in the human microbiota and is considered to be probiotic, mostly found in the gut and mouth (40–60%). It has the potential to cause disease in individuals with compromised immune systems under various circumstances. C. albicans causes mucosal infections (Erdogan et al., 2015; Rajeshkumar & Lakshmi, 2021; Sivakumar et al., 2021). Aspergillus is a common fungus that is found in the debris of the air that humans inhale but not all species cause infection, only a few cause severe diseases like life-threatening fungal infections, including Allergic BronchoPulmonary Aspergillosis (ABPA), aspergilloma, chronic necrotizing aspergillosis, and invasive Aspergillosis (Arastehfar et al., 2021). The presence of these fungi is a significant threat to human health, and it is mandatory to eliminate them using compounds with antimicrobial properties. However, the tungsten carbide-nickel sulphide composites play a huge role in the antimicrobial community(Gandhi et al., 2021; Katyal et al., 2023; Priyadharshini et al., 2023). The synthesis of WC-NiS nanocomposites generally involves methods such as carbothermal reactions and microwave radiation to conserve the form and prevent clumping of the material(Doshi et al., 2023; Lampl et al., 2023; Pandiyan et al., 2023). Rane et al, reviewed these methods, revealing the need for precise control over particle size and distribution to optimize both mechanical and antimicrobial properties . Characterization techniques like X-ray diffraction (XRD), Transform electron microscopy (TEM), High-resolution Transform electron microscopy (HR-TEM) and Fourier transform infrared spectroscopy (FTIR) were used to analyze the synthesis, optical properties, structure, and absorption of the WC-NiS nanocomposites.

# METHODS AND MATERIALS

## SYNTHESIS OF WC-NiS NANOCOMPOSITES

### SYNTHESIS OF TUNGSTEN CARBIDE

0.5 g of ammonium metatungstate is reduced to elemental tungsten in the presence of hydrogen gas (H2). It acts as a reducing agent. Reduction stops, which converts tungsten compounds into tungsten metal. Reduced tungsten is reacted with the required amount of dicyandiamide (carbon source) at a temperature of 1200 °C. The carbon atoms from dicyandiamide react with tungsten atoms to form tungsten carbide. Afterward, the mixture was subjected to an aqueous workup, involving 4-5 washes with water, followed by drying under reduced pressure at 80 °C for 12 hours.

### SYNTHESIS OF NICKEL SULPHIDE

To synthesize nickel sulphide (NiS) nanoparticles, 2.3263 g of nickel nitrate was mixed in 50 mL distilled water with stirring, yielding a light teal solution (Solution A). Separately, 2.3054 g of sodium sulfide was dispersed in 50 ml of distilled water, forming a green solution (Solution B ). Solution B was introduced dropwise to Solution A using a burette, causing the mixture to turn black (Solution C). The combined solution was stirred continuously for one hour to ensure thorough mixing and reaction.

### FINAL SYNTHESIS OF WC-NiS COMPOSITES

1 g of tungsten carbide is combined with 25 mL of distilled water, and 1 g of carbon derived from seaweed is also combined with 25 ml of distilled water. These two mixtures were simultaneously added to Solution C. The final mixture was then subjected to microwave irradiation for 10 minutes, at 2-minute intervals. Following microwave treatment, the sample was subjected to centrifugation and subsequent washing with distilled water, ethanol, and acetone, repeated thrice. The resulting product was subjected to drying at 80 °C for 24 hours, followed by calcination at 300 °C for 3 hours

## CHARACTERIZATION STUDIES OF WC-NiS NANOCOMPOSITES

UV-DRS spectroscopy provides insights into the optical properties such as absorbance, reflectance, band gap energy, and electronic structure of the material synthesized. The optical band gap energy of the synthesized material was determined using diffuse reflectance spectroscopy.X-ray diffraction (XRD) analysis offers detailed insights into the phase composition, crystalline structure, and orientation of the materials under investigation and detects impurities in the synthesized material by measuring the diffracted X-rays' intensity at 2θ angles. The diffraction pattern is a plot of intensity versus 2θ which contains many characteristic peaks signifying specific crystalline phases. The pattern is compared to the ICDD database. Fourier transform infrared spectroscopy (FTIR) is a spectroscopic technique that utilizes the absorption of electromagnetic radiation within the mid-infrared region (4000–400 cm−1) to identify functional groups in molecules. FTIR is used to identify the functional groups and presents the molecular composition, vibration stretch of the particles, and structure based on the absorption of infrared light when exposed to the material synthesized. The results are graphed indicating the stretch vibrations of the different functional group bondings.Transmission electron microscopy (TEM) is a powerful technique that employs a high-energy electron beam to image the microstructure of materials at the nanoscale. The interaction between the electron beam and sample results in the transmission of electrons, which are subsequently detected to construct the final image (Rafi et al., 2024). TEM is commonly used to analyze nanoparticle size and shape, giving accurate estimations of nanoparticle homogeneity.The SAED technique is combined with TEM to show the pattern with specific spots corresponding to the respective diffraction conditions (Tuluwengjiang et al., 2024). SAED is a crystallographic experimental technique performed inside a TEM. It involves the diffraction of electrons in a selected area of the sample to provide information about the crystal structure and phase identification.

## EVALUATION OF ANTIFUNGAL ACTIVITY OF WC-NiS COMPOSITES

The disk diffusion method is a cost-effective technique used to assess the effectiveness of antimicrobial agents against specific microorganisms. It involves placing paper discs with different antimicrobial agents on an agar plate with microorganisms and measuring zones of inhibition to determine susceptibility or resistance. The antifungal activity of the WC-NiS composites was determined using the disk diffusion method. The inoculum was prepared by using the standardized fungal strain(s) - C.albicans and Aspergillus - grown in optimum conditions until an adequate number of spores were obtained. The test samples, along with the controls were assigned to the agar plates to confirm proper dilution. After confirmation, the fungal strains were incubated on the prepared agar plates under optimal conditions, including controlled temperature and humidity for a specific period. The diameter of the zone of inhibition was measured following the incubation period using a spectrophotometer and the percentage of inhibition was calculated and compared with the standard controls.

## RESULTS & DISCUSSIONS

## CHARACTERIZATION STUDIES OF WC-NiS NANOCOMPOSITES

### UV-DRS SPECTRA

Figure 1. UV-DRS spectra of synthesized WC-NiS composite

The UV-DRS spectrum (figure 1) shows the significant absorption of the synthesized material under the visible range (400-700 nm). This indicates that the composite remains absorbed even beyond the UV region and exhibits photocatalytic activity which is utilized in disrupting the microbial cells.

WC-NiS composite showed high potential photocatalytic activity and was completely absorbed under a range of 400 - 500 nm indicating that it has a high light absorbance rate  (Li et al., 2018). In the study by K.Lilly Mary et al., nickel-doped indium sulfide nanoparticles exhibited shifts in absorption bands and changes in optical band gap energy as nickel dopants were introduced, impacting the photocatalytic efficiency and electrochemical performance. Additionally, Azile Nqombolo and Peter A. Ajibade's research on NiS nanoparticles synthesized from Ni(II) dithiocarbamate complexes highlighted blue-shifted absorption spectra and red-shifted photoluminescence emission maxima, indicating unique optical characteristics of the nanocrystals (Nqombolo & Ajibade, 2016). In the study by Jang, J. S, the UV-Vis spectra analysis indicates that tungsten carbide does not absorb visible light, which limits its direct contribution to photocatalytic activity. However, its presence in the composite with CdS affects the light absorption characteristics of CdS, which is a critical factor in the overall photocatalytic process (Jang et al., 2008). These findings emphasize the importance of UV-Vis DRS analysis in elucidating the optical behavior of tungsten carbide-nickel sulfide composites, providing valuable insights into their potential applications in various fields.

## X-RAY DIFFRACTION

Figure 2. X-ray Diffraction analysis - WC-NiS composites

The obtained results of XRD analysis (Figure 2) show that the synthesized material is crystalline. The peaks marked in black correspond to the phase of tungsten carbide while the peaks marked in red correspond to the phase of nickel sulphide. The WC peaks were notable at 2θ≈31.5,35.7,48.1,64.3,74.0 for the (110),(100),(101),(002),(110) planes. The NiS peaks were notable at 2θ≈32.4,37.8,49.9,58.7,74.8 for the (001),(100),(101),(110),(002) planes. Some peaks are seen in common for both WC and NiS, which infers the composite formation. The XRD pattern indicates the successful synthesis of a WC-NiS composite, with distinct peaks corresponding to both tungsten carbide and nickel sulfide phases. The sharp and well-defined peaks suggest high crystallinity for both WC and NiS components. The relative intensities of the peaks can give insights into the proportion and crystallographic orientation of the phases present.

The XRD pattern validates the existence of both WC and NiS phases in the synthesized composite, indicating the successful incorporation of nickel sulfide into the tungsten carbide matrix. The crystallinity and phase distribution are evidenced by the distinct and sharp diffraction peaks. In the study by Kumar et al, the diffraction pattern exhibits two prominent peaks at 2θ = 35.72° and 2θ = 48.42°, which can be ascribed to the planes of WC, respectively. The additional two low-intensity peaks at 2θ = 31.58° and 63.44° are indexed planes of hexagonal WC." These indicate that the synthesized nanoparticles are hexagonal structures. A similar study by Hoffman et al showed a predominant hexagonal pattern and peaks that show the crystalline nature of the tungsten carbide were observed in the XRD pattern Hoffmann, P. et al (“FTIR Studies of Tungsten Carbide in Bulk Material and Thin Film Samples,” 2003). Research by Tarkowski et al. (Tarkowski et al., 2012) highlights that Ni-W coatings exhibit an fcc phase structure with a lattice parameter dependent on the tungsten content, affecting the crystallite size and lattice strain. Additionally, Rose et al. (Rose et al., 2023) discuss the XRD pattern of NiS nanoparticles, showing an orthorhombic structure, which is essential for identifying the crystallographic characteristics of the material. These findings highlight the importance of XRD for characterizing WC-NiS composites.

### FOURIER TRANSFORM INFRARED (FTIR) SPECTROSCOPY

Figure 3. FTIR of synthesized WC-NiS composites

The FTIR Pattern seen in Figure 3 confirms the presence of functional groups of the tungsten carbide-nickel sulphide nanocomposites. The peaks at 3411.77 cm-1 denote O-H stretching vibrations of adsorbed hydroxyl groups and 1592.48 cm-1 is indicative of the N-H stretching vibrations signifying the existence of amine groups (–NH2), primary amines, or secondary amines in the material. 1084.96 cm-1 This peak corresponds to Si-O stretching vibrations, suggesting the presence of silica or silicates. 606.96 cm -1 This peak can be ascribed to Ni-S stretching vibrations, indicating the presence of nickel sulfide. 412.35 cm-1 This peak likely corresponds to W-C stretching vibrations, which are typical for tungsten carbide.In the study by Fazli, Y et al, 2016 (Fazli et al., 2016), the FTIR spectrum of the vibrational patterns of different groups was observed in the previous study on NiS. Nevertheless, peaks identified at 3476 and 1675 cm-1 indicate the absorption of H2O in the sample and the development of hydrated NiS nanoparticles. Furthermore, the peak observed at 652 cm is attributed to the Ni–S–Ni bending vibration mode. The FTIR patterns of tungsten carbide nickel sulphide (NiS) composites exhibit characteristic peaks corresponding to the functional groups present in the materials, as confirmed in the study by Olivas et al.(Olivas et al., 2004). These peaks are unique to the specific chemical bonds within the composites, distinguishing them from other transition metal carbides. Additionally, the FTIR spectra provide valuable information about the synthesized materials' structural properties and bonding configurations, aiding in their characterization. In contrast, the FTIR analysis of other transition metal carbides, such as tungsten carbide with nickel and cobalt, may show different peak positions and intensities due to variations in the chemical compositions and bonding arrangements, as discussed in the previous studies. These differences in FTIR patterns contribute to the distinct identification and differentiation of tungsten carbide nickel sulphide composites from other transition metal carbides.

### TRANSMISSION ELECTRON MICROSCOPY (TEM) & HIGH-RESOLUTION TRANSMISSION ELECTRON MICROSCOPY

The TEM image shows particles appearing as irregular, somewhat agglomerated masses with varying degrees of opacity, suggesting different thicknesses or densities within the sample. The scale bar at the bottom indicates that the entire field of view spans 20 nm, which helps in understanding the nano-scale size of these particles. The darker areas indicate thicker or denser regions, whereas the lighter areas are thinner or less dense.

Figure 4. TEM & HR-TEM for the synthesized WC-NiS composites

The HR-TEM image provides a much closer look at the crystalline structure of the WC-NiS composites. The scale bar here indicates a span of 2 nm, showing a highly magnified view. This image reveals the atomic lattice, visible as a regular pattern of dots. These dots represent columns of atoms in the crystal lattice of the material, and the pattern's clarity and uniformity suggest good crystallinity. This detailed view is crucial for analyzing the structural integrity and the periodicity of the atomic layers, which are important for understanding the material's properties at the atomic level.Studies have shown that these composites consist of large WC particles embedded in a Ni-based matrix, showcasing a pronounced microstructural and mechanical heterogeneity. The TEM analysis of these composites reveals a high quality of WC-metal matrix interfaces, along with the presence of dislocations, planar defects in the WC particles, and dislocations, micro twins within the matrix areas (Richter & Chrapoński, 2018). The TEM & HR-TEM images in the study by XG Yang & CY Wang 2005 indicate that the tungsten carbide nanoparticles are spherical in shape and also confirm the physical properties of the same. Additionally, the Ni-based alloy coatings with WC particles exhibit a three-dimensional reticular microstructure, where the WC particles are evenly distributed among the Ni-based alloying particles, contributing to enhanced macrohardness and microhardness compared to the substrate. These TEM & HR-TEM patterns give the significance of structural characteristics and mechanical properties of tungsten carbide nickel composites, highlighting their potential for various industrial applications.

### SELECTED AREA ELECTRON DIFFRACTION (SAED)

Figure 5. SAED of the synthesized WC-NiS nanocomposites

The SAED analysis of the tungsten carbide-nickel sulphide product revealed maximum attributions to the tungsten carbide-nickel sulphide. The concentric rings in the SAED pattern indicate that the material is polycrystalline that each ring corresponds to a set of crystallographic planes in the material, and the radius of the rings is related to the interplanar spacing (d-spacing) of these planes. The presence of discrete spots along the rings suggests that the crystallites are well-aligned in certain orientations. The more intense spots are typically associated with planes that have higher atomic density. Structure, confirming the presence of a cubic structure, and the interplanar distances for the WC-NiS were identified. The SAED analysis provided valuable information about the crystal structure of the tungsten carbide particles, aiding in the identification and characterization of the synthesized product. Research by Singh et al. demonstrated the formation of Ni-WC composites through direct current electrodeposition, showcasing improved mechanical properties compared to pure nickel deposits. Additionally, the study by Grigoryants et al. investigated the gradient structure of laser-surface coatings using WC powders in a nickel alloy, revealing the presence of WC carbide, nickel solid solution, intermetallic phases, and oxide inclusions within the coating structure (Grigoryants et al., 2017). These findings suggest that the SAED patterns of tungsten carbide nickel composites may exhibit diffraction spots corresponding to the various phases present in the material, providing valuable insights into its crystalline structure and composition.

## ANTIFUNGAL ASSAY OF WC-NiS COMPOSITES

:

Figure 6. Antifungal activity of WC-NiS composites on a. Candida albicans

and b.  Aspergillus

Table 1. Zone of inhibition of different concentrations of A12(H) Candida albicans

| CONCENTRATION OF A12(H) | Candida albicans |
| --- | --- |
| 50 µL | 40 mm |
| 75 µL | 45 mm |
| 100 µL | 50 mm |
| NEGATIVE CONTROL | 10 mm |

Table 2.  Zone of inhibition of different concentrations of A12(H) Aspergillus

| CONCENTRATION OF A12(H) | Aspergillus |
| --- | --- |
| 50 µL | 21 mm |
| 75 µL | 23 mm |
| 100 µL | 25 mm |
| NEGATIVE CONTROL | 10 mm |

The antifungal assay of the C.albicans and Aspergillus results confirms the efficacy of the antifungal properties of the WC-NiS composites as seen in Figure 7 and Table 1 and 2The antifungal activity against Candida albicans is depicted in Figure 6a and Table 1. The WC-NiS composites again demonstrated a concentration-dependent increase in antifungal activity, revealing zones of inhibition of 40, 45, and 50 mm for concentrations of 50, 75, and 100 μL, respectively. The negative control displayed a negligible zone of inhibition of 10 mm. These findings indicate that WC-NiS composites are highly effective against Candida albicans, with higher concentrations resulting in significantly larger zones of inhibition. The antifungal activity against Aspergillus is shown in Figure 6b and Table 2. Results indicate that the WC-NiS composites exhibited a concentration-dependent increase in antifungal activity. At concentrations of 50, 75, and 100 μL, the observed zones of inhibition were 21, 23, and 25 mm, respectively. The negative control exhibited a minimal zone of inhibition of 10 mm, indicating the baseline antifungal activity without the composite. These findings suggest that WC-NiS composites exhibit potent antifungal activity against Aspergillus, with a dose-dependent increase in the zone of inhibition.In the study by S.H.S. Dananjaya, the minimum inhibitory concentration (MIC) values for ZnO NPs and ZnO-C NCs against C. albicans were determined to be 200 μg/mL and 75 μg/mL, respectively. These results indicate that ZnO-C NCs exhibit significantly higher antifungal activity compared to ZnO NPs (Dananjaya et al., 2018) Notably, the efficacy of the composites against Candida albicans was significantly higher than that of CuO nanoparticles, which showed inhibition zones of 15 mm to 22 mm at concentrations of 50 μg/mL to 100 μg/mL. Research has shown that novel materials, including nanomaterials and nanocomposites, hold promise in reducing infections caused by pathogenic microorganisms, especially in the face of increasing antimicrobial resistance (Matharu et al., 2020). Additionally, the development of newer structural complexes, such as Nickel-Schiff bases, has demonstrated enormous inhibitory activity against multi-drug resistant strains of Candida albicans, emphasizing the potential of these compounds as effective antimicrobial agents(Janani et al., 2021; Kachhara et al., 2021; Subramanian et al., 2023). Furthermore, the synthesis and characterization of ZrO2-Ag2O nanoparticles have shown promising antifungal effects against various Candida species, indicating the potential for alternative therapies to treat fungal diseases in humans (Ayanwale et al., 2021). These findings collectively highlight the importance of exploring innovative materials and compounds to combat fungal pathogens and address the challenges posed by antimicrobial resistance.

# LIMITATIONS

The research primarily examines antifungal activity against Candida albicans, which may not represent the full spectrum of microbial resistance challenges. The process of synthesizing the materials was too long which can be reduced in the future. Experiments were conducted in a lab setting, which may not reflect real-world conditions affecting the efficacy of the composites. The study does not extensively address the long-term effectiveness or biocompatibility of WC-NiS composites in practical applications. These limitations suggest areas for further research to enhance the understanding and application of WC-NiS composites in combating microbial resistance.

# CONCLUSION

This study involved the synthesis and characterization of WC-NiS nanocomposites. We conclude that the characterization studies signify that the nanocomposite had shown a crystalline structure in all the means of studies and that the material can be used against fungus, especially Candida albicans, and Aspergillus. This WC-NiS composite can be further researched in the future for biocompatibility and biomedical applications.

# REFERENCES

Arastehfar, A., Carvalho, A., Houbraken, J., Lombardi, L., Garcia-Rubio, R., Jenks, J. D., Rivero-Menendez, O., Aljohani, R., Jacobsen, I. D., Berman, J., Osherov, N., Hedayati, M. T., Ilkit, M., Armstrong-James, D., Gabaldón, T., Meletiadis, J., Kostrzewa, M., Pan, W., Lass-Flörl, C., … Hoenigl, M. (2021). Aspergillus fumigatus and aspergillosis: From basics to clinics. Studies in Mycology, 100. https://doi.org/10.1016/j.simyco.2021.100115

Ayanwale, A. P., Estrada-Capetillo, B. L., & Reyes-López, S. Y. (2021). Evaluation of Antifungal Activity by Mixed Oxide Metallic Nanocomposite against Candida spp. Processes, 9(5), 773.

Bankier, {C, Matharu, R. K., Cheong, Y. K., Ren, G. G., E Cloutman, G., & Ciric}, L. (2019). Synergistic Antibacterial Effects of Metallic Nanoparticle Combinations. Scientific Reports. https://doi.org/10.1038/s41598-019-52473-2

Dananjaya, S. H. S., Kumar, R. S., Yang, M., Nikapitiya, C., Lee, J., & De Zoysa, M. (2018). Synthesis, characterization of ZnO-chitosan nanocomposites and evaluation of its antifungal activity against pathogenic Candida albicans. International Journal of Biological Macromolecules, 108. https://doi.org/10.1016/j.ijbiomac.2017.11.046

Doshi, K., Nivedhitha, M. S., Solete, P., Dp, S., Jacob, B., & Siddique, R. (2023). Effect adhesive strategy universal adhesives noncarious cervical lesions-an updated systematic review meta-analysis. BDJ open. 9.

Erdogan, A., Rao, S. S., Gulley, D., Jacobs, C., Lee, Y. Y., & Badger, C. (2015). Small intestinal bacterial overgrowth: duodenal aspiration vs glucose breath test. Neurogastroenterology and Motility, 27(4). https://doi.org/10.1111/nmo.12516

Fazli, Y., Pourmortazavi, S. M., Kohsari, I., Karimi, M. S., & Tajdari, M. (2016). Synthesis, characterization and photocatalytic property of nickel sulfide nanoparticles. Journal of Materials Science: Materials in Electronics, 27(7), 7192–7199.

FTIR studies of tungsten carbide in bulk material and thin film samples. (2003). Materials Characterization, 50(4-5), 255–259.

Gandhi, J. M., Gurunathan, D., Doraikannan, S., & Balasubramaniam, A. (2021). Oral health status for primary dentition - A pilot study. Journal of the Indian Society of Pedodontics and Preventive Dentistry, 39(4), 369–372.

Grigoryants, A. G., Ya. Stavertiy, A., Bazaleeva, K. O., Yu. Yudina, T., Smirnova, N. A., Tretyakov, R. S., & Misyurov, A. I. (2017). Laser surfacing of nickel-based composite war-resisting coatings reinforced with tungsten carbide. Welding International. https://doi.org/10.1080/09507116.2016.1213039

Hoque, M. E., Showva, N.-N., Ahmed, M., Rashid, A. B., Sadique, S. E., El-Bialy, T., & Xu, H. (2022). Titanium and titanium alloys in dentistry: current trends, recent developments, and future prospects. Heliyon, 8(11), e11300.

Janani, K., Teja, K. V., & Ajitha, P. (2021). Cytotoxicity of oregano essential oil and calcium hydroxide on L929 fibroblast cell: A molecular level study. Journal of Conservative Dentistry: JCD, 24(5), 457–463.

Jang, J. S., Ham, D. J., Lakshminarasimhan, N., Choi, W. Y., & Lee, J. S. (2008). Role of platinum-like tungsten carbide as cocatalyst of CdS photocatalyst for hydrogen production under visible light irradiation. Applied Catalysis. A, General, 346(1-2), 149–154.

Kachhara, S., Nallaswamy, D., Ganapathy, D., & Ariga, P. (2021). Comparison of the CBCT, CT, 3D printing, and CAD-CAM milling options for the most accurate root form duplication required for the root analogue implant (RAI) protocol. Journal of Indian Academy of Oral Medicine and Radiology, 33(2), 141–145.

Katyal, D., Jain, R. K., Sankar, G. P., & Prasad, S. (2023). Antibacterial, Cytotoxic, Mechanical Characteristics Novel Chitosan-Modified Orthodontic Primer: : In-Vitro: Study. Journal International Oral Health, 15(3), 284–289.

Lampl, S., Gurunathan, D., Krithikadatta, J., Mehta, D., & Moodley, D. (2023). Reasons for Failure of CAD/CAM Restorations in Clinical Studies: A Systematic Review and Meta-analysis. The Journal of Contemporary Dental Practice, 24(2), 129–136.

Li, C., Wang, H., Naghadeh, S. B., Zhang, J. Z., & Fang, P. (2018). Visible light driven hydrogen evolution by photocatalytic reforming of lignin and lactic acid using one-dimensional NiS/CdS nanostructures. Applied Catalysis. B, Environmental, 227, 229–239.

Matharu, R. K., Ciric, L., Ren, G., & Edirisinghe, M. (2020). Comparative Study of the Antimicrobial Effects of Tungsten Nanoparticles and Tungsten Nanocomposite Fibres on Hospital Acquired Bacterial and Viral Pathogens. Nanomaterials (Basel, Switzerland), 10(6). https://doi.org/10.3390/nano10061017

Mounyr, B., Moulay, S., & Ibnsouda, S. K. (2016). Methods for in vitro evaluating antimicrobial activity: A review. Journal of Pharmaceutical and Biomedical Analysis, 6(2), 71–79.

Nqombolo, A., & Ajibade, P. A. (2016). Synthesis and spectral studies of Ni(II) dithiocarbamate complexes and their use as precursors for nickel sulphides nanocrystals. Journal of Chemistry, 2016, 1–9.

Olivas, A., Camacho, A., Yacamán, M. J., & Fuentes, S. (2004). Nickel–tungsten bimetallic sulfide nanostructures of fullerene type. Journal of Materials Research, 19(7), 2176–2184.

Pandiyan, I., Arumugham, M. I., Doraikannan, S. S., Rathinavelu, P. K., Prabakar, J., & Rajeshkumar, S. (2023). Antimicrobial and Cytotoxic Activity of Ocimum tenuiflorum and Stevia rebaudiana-Mediated Silver Nanoparticles - An In vitro Study. Contemporary Clinical Dentistry, 14(2), 109–114.

Pavithra, S., Paulraj, J., Rajeshkumar, S., & Maiti, S. (2023). Comparative evaluation antimicrobial activity compressive strength conventional thyme-modified glass ionomer cement. Annals Dental Specialty, 11(1-2023), 70–77.

Priyadharshini, G., Gheena, S., Ramani, P., Rajeshkumar, S., & Ramalingam, K. (2023). Assessment antimicrobial efficacy cytotoxicity Cocos nucifera Triticum aestivum combination gel formulation therapeutic use. World Journal Dentistry, 14(5), 414–418.

Rafi, D. M., Lakshmi, T. V., Shirley, C. P., Ravivarman, G., & Senthilkumar, G. (2024, April). Improving Prostate Cancer Diagnosis with Weakly Supervised Learning and Radiology-Confirmed Negative MRI Data. In 2024 International Conference on Inventive Computation Technologies (ICICT) (pp. 1183-1188). IEEE.

Rajeshkumar, S., & Lakshmi, T. (2021). Green synthesis gold nanoparticles using kalanchoe pinnata its free radical scavenging activity. Int J Dentistry Oral Sci, 8(7), 2981–2984.

Ramsundar, K., Jain, R. K., Balakrishnan, N., & Vikramsimha, B. (2023). Comparative evaluation bracket bond failure rates novel non-primer adhesive conventional primer-based orthodontic adhesive-a pilot study. Journal Dental Research, 17(1).

Richter, J., & Chrapoński, J. (2018). Application of FIB in the preparation of TEM specimens of experimental supercoarse WC-Co(Ni) composites. International Journal of Refractory Metals and Hard Materials, 75. https://doi.org/10.1016/j.ijrmhm.2018.04.016

Rieshy, V., Chokkattu, J. J., Rajeshkumar, S., & Neeharika, S. (2023). Mechanism action clove ginger herbal formulation-mediated TiO2 nanoparticles against lactobacillus species: vitro study. Journal Advanced Oral Research, 14(1), 61–66.

Rose, M. M., Christy, R. S., Benitta, T. A., & Thanka Kumaran, J. T. (2023). Phase transition in nickel sulphide nanoparticles. Phase Transitions, 96(5), 301–310.

Shenoy, A., Maiti, S., Nallaswamy, D., & Keskar, V. (2023). An in vitro comparison of the marginal fit of provisional crowns using the virtual tooth preparation workflow against the traditional technique. Journal of Indian Prosthodontic Society, 23(4), 391–397.

Singh, S., Prasad, A. S., & Rajeshkumar, S. (2023). Cytotoxicity, antimicrobial, anti-inflammatory and antioxidant activity of camellia sinensis and citrus mediated copper oxide nanoparticle-an in vitro study. Journal of International Society of Preventive & Community Dentistry, 13(6), 450–457.

Sivakumar, N., Geetha, R. V., Priya, V., Gayathri, R., & Ganapathy, D. (2021). Targeted phytotherapy forreactive oxygen species linked oral cancer. Int J Dent Oral Sci, 8.

Subramanian, A. K., Lalit, H., & Sivashanmugam, P. (2023). Preparation, characterization, and evaluation of cytotoxic activity of a novel titanium dioxide nanoparticle-infiltrated orthodontic adhesive: An in vitro study. World Journal of Dentistry, 14(10), 882–887.

Tuluwengjiang, G., Rasulova, I., Ahmed, S., Kiasari, B. A., Sârbu, I., Ciongradi, C. I., & Samaniego, S. S. C. (2024). Dendritic cell-derived exosomes (Dex): Underlying the role of exosomes derived from diverse DC subtypes in cancer pathogenesis. Pathology-Research and Practice, 254, 155097.

Tarkowski, L., Indyka, P., & Bełtowska-Lehman, E. (2012). XRD characterisation of composite Ni-based coatings prepared by electrodeposition. Nuclear Instruments & Methods in Physics Research. Section B, Beam Interactions with Materials and Atoms, 284, 40–43.

Thomas, & Jain, R. K. (2023). Influence operator experience scanning time accuracy two different intraoral scanners-a prospective clinical trial. Turkish Journal Orthodontics, 36(1).