Comparative Fabrication and Physicochemical Characterisation of Low and High Molecular Weight Hyaluronic Acid and Chitosan Based Membranes for Wound Healing and Guided Tissue Regeneration

Jignesh Panda1 , F.Arul1,a)

1Panda Hospitals, Chennai, Tamil Nadu, India

Corresponding Author: a)dfjarul2503@gmail.com

Abstract: To fabricate and evaluate the physico-chemical properties of biomaterials derived from hyaluronic acid and chitosan across different molecular weights, elucidating how molecular weight variations influence their structural, mechanical, and biological performance for potential applications in tissue engineering and regenerative medicine.Hyaluronic acid is a natural polysaccharide renowned for its biocompatibility and biodegradability, fueling its widespread use in bioengineering and wound dressings alongside polymers like cellulose, chitin, and chitosan. In periodontal therapy, guided tissue regeneration (GTR) restores cementum, periodontal ligament, and alveolar bone by blocking non-osteogenic cell invasion, while silver particles boost antimicrobial activity. Combined with guided bone regeneration (GBR) membranes and titanium implants, these regenerative techniques significantly enhance dental and biomedical treatment outcomes. Ultimately, these strategies revolutionize modern clinical practice.The stock solutions were prepared with 1% HA, 0.5% carrageenan, and 1% gelatin, blended in a 6:1:3 ratio for Test 1; Test 2 used 1% HA, 1% carrageenan, and 1% gelatin in the same ratio, while the control group comprised 1% HA and 1% gelatin blended in a 6:4 ratio. In all cases, 3 ml of the homogeneous mixture was transferred to six-well plates, 100 μl of 15% TPP was added to each well, and the plates were stored at –20°C for 12 hours followed by –80°C overnight. Samples were lyophilized for 24 hours, stored dry, and subsequently tested via SEM, contact angle, swelling, and degradation analysis.Our study’s porous size matched earlier findings by Mighri et al. and Rajam et al., while the collagen–chitosan combination exhibited a homogeneous porosity per Miri et al. Notably, collagen membranes varied with chitosan coatings: non-coated membranes had larger pores (30–100 m) compared to chitosan-coated ones (30–70 m), and Rajam et al. reported interconnected pores averaging 75–150 m. Test 1 (0.5% carrageenan with HA) showed a contact angle of 63.52° versus Test 2 (1% carrageenan with HA) at 70.15°. HA is essential for tissue repair, promoting cell migration, adhesion, and proliferation, and its use in scaffolds has been proven in animal wound models to support dermal regeneration and accelerate healing, including via hydrogel-trapped dermal/epidermal cell fractions.

Keywords: Biopolymers, High molecular weight, Hyaluronic acid, Wound healing, Implant, Periodontitis, Periimplantitis, GTR membrane, Chitosan, GTR membrane, chitosan, Guided bone regeneration, periodontium.

# Introduction

Hyaluronic acid (HA), a naturally occurring polymer in the skin and a key component of the extracellular matrix, has been extensively studied for its diverse applications in orthopedics, cosmetic surgery, tissue engineering, and wound healing(Nityasri et al., 2025)(Chokkattu et al., 2023; Dharman et al., 2023; Govindaraj & Shanmugam, 2023)(Rajeshkumar & Lakshmi, 2021; Sivakumar et al., 2021). Its breakdown products, varying with molecular weight, exhibit non-antigenicity, free radical scavenging, and the ability to modulate fibroblasts, endothelial cells, and macrophages via receptors such as CD44 and Toll-like receptors, where low molecular weight HA promotes pro-inflammatory responses while high molecular weight HA dampens them(Gopal & Rohinikumar, 2021; Harikrishnan et al., 2021; Kabilamurthi et al., 2021)(Janani et al., 2021; Kachhara et al., 2021; Subramanian et al., 2023). Although high molecular weight HA is widely used, preparing HA at specific molecular weights remains challenging, employing physical (ultrasound, ozone, electron beam, γ-irradiation, thermal treatment) and chemical (enzyme and acid degradation) methods, with γ-irradiation notably reducing molecular weight without altering structure(Zhang et al., 2025)(Gandhi et al., 2021; Katyal et al., 2023; Priyadharshini et al., 2023). These unique properties have led to its use in various forms, from gels to sheets and meshes, in bioactive wound dressings designed to maintain electrolyte balance, permit vapor exchange, manage exudates, and provide antimicrobial, hemostatic, and pain-relieving effects. Moreover, HA is often combined with other biopolymers like cellulose, chitin, chitosan, fibrin, alginate, elastin, dextran, collagen, and gelatin to enhance mechanical properties and promote epithelial and mesenchymal cell migration, collagen deposition, angiogenesis, and overall tissue repair, underscoring its promising role in advancing biomedical applications. In the context of periodontal disease, guided tissue regeneration (GTR) techniques utilize barrier membranes to repair periodontal defects, aiming to restore structural integrity and functionality to the dentition(Nityasri et al., 2025)(Doshi et al., 2023; Lampl et al., 2023; Pandiyan et al., 2023). These membranes, crafted from materials such as collagen, polysaccharides, and fibrin, support vascularization, stabilize wounds, protect blood clots, and limit undesirable epithelial and connective tissue ingrowth. However, limitations like low bioactivity and uneven degradation have led to the development of next-generation, multi-layered bioactive designs. Chitosan, a partially deacetylated form of chitin, is valued for its biocompatibility, biodegradability, antimicrobial properties, and low immunogenicity, making it an excellent substrate for bone repair when enhanced with osteogenic minerals(Zhang et al., 2025)(Lu et al., 2025). While non-resorbable membranes like expanded polytetrafluoroethylene (e-PTFE) preserve space, their need for secondary removal makes resorbable options(Meenakshi & Rajasekar, 2024)(Pavithra et al., 2023; Shenoy et al., 2023; Thomas & Jain, 2023), typically based on polyglycolic acid, polylactic acid, polycaprolactone, and collagen. Collagen membranes, particularly the clinically recognized Bio-Gide® with cross-linked collagen types I and III, offer exceptional cell affinity yet face challenges such as immune responses, uncontrollable degradation rates, poor mechanical strength, complex fabrication, and high cost, driving the ongoing search for improved biomaterials(Gopal & Rohinikumar, 2021; Harikrishnan et al., 2021; Kabilamurthi et al., 2021)(Ramsundar et al., 2023; Rieshy et al., 2023; Singh et al., 2023)(Rajeshkumar & Lakshmi, 2021; Sivakumar et al., 2021)

# MATERIALS AND METHODS

## Fabrication of Scaffolds

Figure 1. A)HA Medium MW solution, B)beaker containing Gelatin solution, C)Blending process done after both solutions are added to a beaker, to create homogenous solution, D)Shows the homogenous solutions , E) Shows the homogenous solution in well plated trays before fabrication , F) Shows the fabricated membranes

Test 1 contains the stock solution of 1% HA(H), 0.5% carrageenan and 1% gelatin. To fabricate the scaffold the materials were blended in the ratio 6:1:3 respectively. Test 2 contains the stock solution of 1% HA(H), 1% carrageenan and 1% gelatin. To fabricate the scaffold the materials were blended in the ratio 6:1:3 respectively. Then the control group contains 1% of HA(H) and 1% gelatin blended in the ratio of 6:4. 3ml of the homogeneous mixture was transferred to six well plates. 100 ul of the crosslinking agents TPP (15%) was added to each well. The plates were stored in-20 C for 12 hrs and followed by-80 C overnight. The samples were then lyophilized for 24hrs and stored in dry condition.The stock solution of 2% chitosan, 0.5% carrageenan and 1% gelatin were prepared. To fabricate the scaffold, Chitosan and gelatin were blended in the ratio 6:3 respectively. Then, 1ml of 0.5% and 1% carrageenan was added to the respective test group. 3ml of the homogeneous mixture was transferred to six well plates in each well. The plates were stored in -20 C for 12 hrs and followed by -80 C overnight. The samples were then lyophilized for 24hrs and stored in dry condition until use.

A

D

C

B

Figure 2 : A)Vile on the left contains 1% gelatin solution and on the right 1% Chitosan and 5% Acetic cid solutions, B)beaker containing Chitosan Low MW solution, C) Shows the homogenous solution in well plated trays before fabrication , D) Shows the fabricated membranes

## SEM Analysis

The morphological characteristics of scaffolds were observed using scanning electron microscopy (SEM, JEOL, Tokyo, Japan) after freeze drying. The cross-sections of freeze-dried samples were coated with platinum via a sputter-coater at ambient temperature. Micrographs of all scaffolds were taken at 100X.

## Fourier transform infrared (FT-IR) analysis

Attenuated total reflectance fourier transform infrared spectroscopy (ATR-FTIR) is a powerful technique to determine any possible chemical interaction ATR-FTIR spectroscopic analysis was performed using Bruker ATR infrared spectrometer (model). The expected pendant functionalities of scaffolds were confirmed by the FT-IR spectrum.

## Contact Angle

To determine the hydrophilicity of the scaffolds, water contact angles of the scaffolds were measured by goniometer software. During the measurements, the scaffolds were cut into square specimens with the size of 1 cm × 1 cm, and further they were placed on the testing plate. Subsequently, 50 μL distilled water was carefully dropped onto the prepared specimens. The contact angles between water droplets and the scaffolds were measured by taking photos immediately (within 2s) when the droplets touched the surface of the scaffolds. Three measurements at different positions of each scaffold were conducted.

## Swelling ratio (1%) of scaffolds

Swelling/shrinkage studies were performed to calculate the water content (1%) of the scaffolds, wherein 10 mg of freeze-dried scaffolds were placed in 500 µl of PBS at 37 °C. After 24 hours, these scaffolds were removed from the PBS, dabbed with a Kimwipe to remove any excess water on the surface, weighed and placed back into the buffer. The swelling ratio and shrinkage ratio (1%) were calculated using the following equations. All experiments were performed 6 times.

Swelling ratio (SR)= ((Ww−W0)/W0)×100%

W0 and Ww are the initial dry weight and the wet weight, respectively.

## Dental Pulp stem cells (hDPSC) Cell Culture

After obtaining informed consent and ethical approval from SIMATS ethics committee, the Dental Pulp stem cells were isolated from molars. The cells were cultured in DMEM low glucose/10% FBS/1%Penicillin;streptomycin. After two passages, 10000 cells per well were seeded in 48 well plates for cell viability and compatibility assays.

## Biocompatibility Analysis (MTT Assay)

100 mg of 5 mm cylindrical blocks were prepared. The prepared blocks were immersed in DMEM- low glucose media formulated with 10 % FBS and 1% Penicillin/streptomycin. The media were collected after 24 hrs and 7 days of immersion and treated with cells to test the compatibility. After 24hrs of culture, add the 10uL/100mL of MTT reagent (5 mg/mL stock) to cultured cells and then incubate for 4 h to allow formation of the formazan dye at 37℃. The medium is exchanged to DMSO (200 μL) and stands for 10min. The reaction product was transferred to a 96 well ELISA plate and A590 was measured with ELISA plate reader.

# Statistical analysis

All values are expressed as the mean ±  standard error of the mean (SEM) of at least three independent experiments. A one-way ANOVA (analysis of variance) was used to test for significant differences, and multiple comparisons were performed using Scheffe’s method. Statistical significance was set at p < 0.05.

# RESULTS

HA plays an important role in tissue repair by stimulating cell migration, adhesion, and proliferation. Studies demonstrated where HA was incorporated into scaffolds for the treatment of wounds. Several studies on animals that used wound models evaluated the effectiveness of HA-based scaffolds. These biologically derived scaffolds, which support dermal regeneration and wound healing, are used. One instance involved dermal/epidermal Directly trapped cell fractions inside the hydrogel hastened the healing of wounds (Yan et al., 2013). The scaffold was also used to embed basic fibroblast growth factor in other places.

Fig 3 representing the contact angle of med.mol wt HA GTR membrane  with 0.5% carrageenan.

Fig 4 representing the contact angle of med.mol wt HA GTR membrane with 1% carrageenan

Table 1 : Contact angle of HA(H) homogeneous mixture of Test 1 and Test 2

| Group | Contact angle |  |
| --- | --- | --- |
| Test 1 - 0.5% | HA(H)GTR | 63.52 |
| Test 2 - 1% | HA(H)GTR | 70.15 |

Table 1 depicts the contact angle of the homogeneous mixture of test 1 and test 2. Contact angle of Test 1 of 0.5% carrageenan with HA(H) contains 63.52 and Test 2 of 1% carrageenan with HA(H) contains 70.15

Table 2: Contact angle of HA(L) homogeneous mixture of Test 1 and Test 2

| Group | Contact angle |  |
| --- | --- | --- |
| TEST 1 - 0.5% | HA (L) GTR | 58.97 |
| TEST 2 - 1% | HA (L) GTR | 60.41 |

Table 2 depicts the contact angle of the homogeneous mixture of test 1 and test 2. Contact angle of Test 1 of 0.5% carrageenan with HA(L) contains 58.97 and Test 2 of 1% carrageenan with HA(L) contains 60.41.

Table 3: Contact angle of HA(M)GTR homogeneous mixture of Test 1 and Test 2

| Group | Contact angle |  |
| --- | --- | --- |
| TEST 1 -0.50% | HA (M) GTR | 83.13 |
| TEST 2 -1% | HA (M) GTR | 60.28 |

Table 3 depicts the contact angle of the homogeneous mixture of test 1 and test 2. Contact angle of Test 1 of 0.5% carrageenan with HA(M) contains 83.13 and Test 2 of 1% carrageenan with HA(M) contains 60.28.

The above results show that the contact angle of  HA GTR membrane with 0.5% carrageenan is higher than the 1% carrageenan. Henceforth the adhesion is indirectly proportional contact angle. Increase in contact angle decreases the adhesion.

Table 4. represents the contact angle of chitosan synthesised particle

| Group | Contact angle |  |
| --- | --- | --- |
| Test 1 -1% | 1% Chitosan | 39.12 |
| Test 2 -0.50% | 0.5% Chitosan | 56.22 |

Table 5:  represents the contact angle of chitosan synthesised particle

| Group | Contact angle |  |
| --- | --- | --- |
| 1% | 1% Chitosan GTR | 70.6 |
| 0.50% | 0.5% Chitosan GTR | 96.67 |

# SEM ANALYSIS

Figure 5: SEM analysis of High molecular weight HA

Figure 5 depicts the Scanning electron microscopy of a high molecular weight GTR membrane with 0.5% carrageenan ( left image) and 1% carrageenan ( right image).

Figure 6: SEM analysis of Medium molecular weight HA

Figure 6 Scanning electron microscopy of med.mol wt HA GTR membrane with 0.5% carrageenan ( left image) and 1% carrageenan ( right image).

Figure 7- SEM analysis for control and test group displayed at 50µm Scaffold-like variation on the membrane is observed for 0.5 and 1% Chitosan

Figure 8. Shows the SEM analysis of the scaffold at 250 x magnification (conc 1%)

Figure 9. Shows the SEM analysis of the scaffold at 250 x magnification (conc 0.5%)

Figure 10: FTIR spectra of high molecular weight HA with 0.5% carrageenan

Figure 10 depicts the FTIR spectra of high molecular weight  HA based GTR membrane crosslinked with 0.5% carrageenan

Figure 11: FTIR spectra of high molecular weight HA with 1% carrageenan

Figure 12 FTIR spectra of med.mol wt  HA based GTR membrane crosslinked with 0.5% carrageenan

Figure 13 FTIR spectra of med.mol wt  HA based GTR membrane crosslinked with 1% carrageenan

Figure 14 : Swelling followed by wound healing activity

Figure 15: Figure showing the compatibility test of low molecular weight hyaluronic acid

The results of this study reveals that, According to the swelling test (Fig 15), it depicts that among the two initial samples of low molecular weight hyaluronic acid with 0.5% and 1% caragenin concentration, the sample with 1% caragenin shows better swelling property than the usage of 0.5% solution with low molecular weight. Figure 16 depicts the biocompatibility test of low molecular weight hyaluronic acid shows that sample B shows better cell viability and biocompatibility than sample A.Previous research article suggests that the Low molecular weight Hyaluronic acid prepared by γ-irradiation shows strain rate-dependent Newton/non-Newton fluid biphasic viscosity. The water absorption ability of γ-ray-prepared Low molecular weight hyaluronic acid is reserved when used for long-term medical applications. In addition, the Low molecular weight hyaluronic acid prepared by γ-irradiation can be an excellent wound dressing material for medical applications (Huang et al., 2019). Another article suggests that the high molecular weight of hyaluronic acid plus povidone-iodine complex dressing significantly facilitated diabetic wound healing via increasing neovascularization and tissue regeneration and suppressing a proinflammatory response (Roberts et al., 1989).

Figure 16: Represents the swelling test between test and control group of chitosan membrane

Figure 17:  Represents the compatibility values between the test and control group, where not much of difference was seen. This states that the percentage of cell viability is almost same for both test and control group

Figure 18. Represents the swelling test between test and control group of chitosan membrane

Figure 19: Represents the compatibility values between the test and control group, where not much of difference was seen. This states that the percentage of cell viability is almost same for both test and control group.

# Discussion

Formulated gelatin-crosslinked HA-based hydrogels embedded with recombinant thrombomodulin were developed for diabetic wound treatment, using 1-ethyl-3-(3-dimethylaminopropyl) carbodiimide hydrochloride (EDC) as a widely used water-soluble crosslinker(Mondal, 2019); FTIR confirmed effective polymer crosslinking, while SEM revealed permeable structures with pore diameters ranging from 20–300 µm that diminished with increasing HA concentration(Abidi, 2022)(Website, n.d.-a). In vitro, the hydrogels rapidly absorbed water,expanding over 11-fold within 30 min to one day,without HA fixation affecting water retention, and exhibited excellent drug release kinetics at 33 °C with over 40% thrombomodulin released within the first 3 h and complete release by 12 h(Mondal, 2019)(Website, n.d.-b). In diabetic mice, thrombomodulin-loaded hydrogels promoted superior wound healing compared to plain hydrogels, while in situ collagen-hyaluronic acid hydrogels cultured with COS-7 fibroblasts and HMEC showed a steady 45% cell proliferation over 72 h, facilitating signal molecule exchange and neurite outgrowth stimulation. Antibacterial tests demonstrated hydrogels eliminated approximately 47% of S. aureus and 55% of E. coli after 3 h at 37 °C, and in vivo full-thickness wound healing studies in mice indicated that combined collagen and HA hydrogels enhanced recovery compared to free collagen hydrogels(Website, n.d.-b, Website, n.d.-c). Additionally, in situ HA hydrogels loaded with plasmid DNA encoding VEGF accelerated healing in burned wounds by mitigating inflammation and promoting microvascular growth, while HA-based composite wipes,designed with fibrin nanoparticles encapsulating VEGF and integrated into chitosan-HA matrices,offered high porosity (65–75%), adequate mechanical strength (elongation at break of 10–20% and elasticity of 0.02–0.15 MPa)(Nanosized Drug Delivery Systems: Colloids and Gels for Site Specific Targeting, n.d.), and enhanced flexibility via increased HA fixation, ensuring secure application on tissue(Akshayaa & Ganesh S, 2024).(Website, n.d.-d) Clinical investigations further demonstrated that using HA with GTR improved clinical attachment level (CAL) gains at six months compared to GTR alone, with additional studies showing that HA combined with bioresorbable PLA/PGA membranes significantly reduced gingival recession and promoted osteoinduction in rat tooth sockets by enhancing BMP-2 production and osteoblast differentiation. Finally, the importance of scaffold physical properties was confirmed by the uniform integration of collagen and chitosan, producing membranes with interconnected pores ranging from 16 to 100 µm, essential for effective cell adhesion, proliferation, and differentiation in tissue engineering.(“Hyaluronic Acid Modulates Proliferation, Collagen and Protein Synthesis of Cultured Fetal Fibroblasts,” 1993)In addition to the development of HA-based hydrogels for wound healing and tissue regeneration, distinct micro-architectural features such as films and fibers have been engineered using chitosan and its composites for periodontal GTR membranes(Website, n.d.-e). Literature suggests that functionally graded GTR membranes might be fabricated by employing a relatively low UHMWPEO ratio to produce aligned chitosan fibers,a novel approach,using electrospinning to create scaffolds that mimic the natural extracellular matrix. Although fiber-forming agents like PEO have been explored extensively due to their biological inertness and plasticizing properties, our work utilized only a minimal amount (0.045 g, at a 5:95 ratio to chitosan) to produce beadless fibers(Almatrafi et al., 2024). The inherent crystallinity and low solubility of chitosan, owing to extensive hydrogen bonding, render its electrospinning challenging (Novel Biomaterials for Tissue Engineering 2018, n.d.); it requires solvents such as acetic acid, dichloromethane (DCM), or trifluoroacetic acid (TFA) to disrupt inter-chain connections(Website, n.d.-f), although concerns about toxicity persist with agents like DCM and TFA(Saadh et al., 2024). Despite thorough toxicity studies on solvents like TFA and hexafluoroisopropanol (HFIP), safety remains a consideration, prompting the use of acetic acid in our process due to its non-toxicity(Website, n.d.-g, Website, n.d.-h). Prior research reported fiber diameters between 40 and 200 nm with PEO/chitosan composites(Spasova et al., 2004), yet our fibers measured 288 to 400 nm, likely due to the restricted CH:PEO ratio; furthermore, increased polymer concentration has been linked to fewer beads and reduced fiber diameters, with environmental factors like humidity and temperature influencing fiber thickness by altering the solidification process(Huan et al., 2015; Klossner et al., 2008). Electrospun fibers that mimic the extracellular matrix support cell adhesion, proliferation, and matrix deposition; aligned fibrous scaffolds,(Delaine-Smith et al., 2014) as demonstrated by previous studies, provide an optimal interface for collagen deposition and promote faster cellular migration compared to random fibers, which have been associated with increased calcium deposition via integrin and myosin-mediated mechanotransduction. Mesenchymal stem cells, commonly present in wound healing sites and capable of differentiating into bone, neural, cartilage, muscle, and fat tissues, exhibited favorable adhesion and penetration within the chitosan fibers, as confirmed by H&E staining and extracellular matrix coverage, thereby underscoring the potential of these electrospun constructs in enhancing periodontal tissue regeneration.(Liu et al., 2015; Tendon Stem Cells from Basic Biology to Clinical Application, n.d., Website, n.d.-i)

# Conclusion

In conclusion, our investigation demonstrates that employing GTR with high molecular weight hyaluronic acid offers a significant advantage in regenerative strategies for treating disfigurements, as hydrogels incorporating dynamic amide bonds can be functionalized to mimic the extracellular matrix and attract proteins essential for tissue engineering, although further clinical studies are needed. Moreover, lower molecular weight HA GTR membranes formulated with 1% caragenin exhibit superior swelling properties and cell viability compared to 0.5%, with sample B outperforming sample A in biocompatibility tests. Data analysis further reveals that chitosan particle-infused membranes effectively decrease contact angles and yield favorable SEM and FTIR profiles, as well as optimal swelling and compatibility, indicating their promising use in GBR membrane synthesis for future dental treatments. Despite exhibiting a fibrous membrane surface with ideal porosity, the chitosan membranes show lower mechanical strength, underscoring the need for further research, particularly animal studies,to enhance their structural properties and fully assess their clinical potential.

# REFERENCES

Almatrafi, T. A.,  Almohaimeed, H. M., Chakravarthi, S., Amin, A. H., Jafer, A.,  & Akhavan-Sigari, R. (2024). Reducing metastasis ability of gastric cancer cell line by targeting MMP16 using miR-193a-5p and 5-FU. Advances in Medical Sciences, 69(2), 463-473.

Abidi, N. (2022). FTIR Microspectroscopy: Selected Emerging Applications. Springer Nature.

Akshayaa, & Ganesh S, B. (2024). Preparation of Carrageenan and fucoidan silica nanoparticles based membrane for guided bone regeneration in dental implant sites. Journal of Long-Term Effects of Medical Implants. https://doi.org/10.1615/jlongtermeffmedimplants.2024049789

Chokkattu, J. J., Neeharika, S., Brahmajosyula, I. P., & Thangavelu, L. (2023). Comparative Evaluation Cellular Toxicity Three Heat Polymerized Acrylic Resins: Vitro Study. World, 14(6).

Delaine-Smith, R. M., Green, N. H., Matcher, S. J., MacNeil, S., & Reilly, G. C. (2014). Monitoring Fibrous Scaffold Guidance of Three-Dimensional Collagen Organisation Using Minimally-Invasive Second Harmonic Generation. PLOS ONE, 9(2), e89761.

Dharman, S., Maragathavalli, G., Shanmugam, R., & Shanmugasundaram, K. (2023). Biosynthesis Turmeric Silver Nanoparticles: Its Characterization Evaluation Antioxidant, Anti inflammatory, Antimicrobial Potential Against Oral Pathogens vitro Study. Journal Indian Academy Oral Medicine Radiology, 35(3), 299–305.

Doshi, K., Nivedhitha, M. S., Solete, P., Dp, S., Jacob, B., & Siddique, R. (2023). Effect adhesive strategy universal adhesives noncarious cervical lesions-an updated systematic review meta-analysis. BDJ open. 9.

Gandhi, J. M., Gurunathan, D., Doraikannan, S., & Balasubramaniam, A. (2021). Oral health status for primary dentition - A pilot study. Journal of the Indian Society of Pedodontics and Preventive Dentistry, 39(4), 369–372.

Gopal, T. M., & Rohinikumar, S. (2021). Association of Gingival Biotype and Flap Design Considered at Stage Two Uncovery - A Retrospective Study. Journal of Long-Term Effects of Medical Implants, 31(3). https://doi.org/10.1615/JLongTermEffMedImplants.2021038612

Govindaraj, P., & Shanmugam, R. (2023). Effect chlorhexidine fluoride varnish incidence white spot lesion orthodontic patients. Annals Dental Specialty, 11(1-2023), 35–39.

Harikrishnan, R., Rohinikumar, S., Ganesh, B. S., & Ashok, V. (2021). Relation between Bone Density and Primary Stability in the Posterior Mandibular Region in Patients Undergoing Dental Implant Treatment: A Retrospective Study. Journal of Long-Term Effects of Medical Implants, 31(2). https://doi.org/10.1615/JLongTermEffMedImplants.2021035972

Huang, Y.-C., Huang, K.-Y., Lew, W.-Z., Fan, K.-H., Chang, W.-J., & Huang, H.-M. (2019). Gamma-Irradiation-Prepared Low Molecular Weight Hyaluronic Acid Promotes Skin Wound Healing. Polymers, 11(7). https://doi.org/10.3390/polym11071214

Huan, S., Liu, G., Han, G., Cheng, W., Fu, Z., Wu, Q., & Wang, Q. (2015). Effect of Experimental Parameters on Morphological, Mechanical and Hydrophobic Properties of Electrospun Polystyrene Fibers. Materials, 8(5), 2718–2734.

Hyaluronic Acid Modulates Proliferation, Collagen and Protein Synthesis of Cultured Fetal Fibroblasts. (1993). Matrix, 13(6), 441–446.

Janani, K., Teja, K. V., & Ajitha, P. (2021). Cytotoxicity of oregano essential oil and calcium hydroxide on L929 fibroblast cell: A molecular level study. Journal of Conservative Dentistry: JCD, 24(5), 457–463.

Kabilamurthi, R. S., Abhinav, R. P., Thiyaneswaran, N., Rohinikumar, S., & Gajendran, P. (2021). Effectiveness of Concentrated Growth Factor on Surgical Wound Healing: A Pilot Study. Journal of Long-Term Effects of Medical Implants, 31(3). https://doi.org/10.1615/JLongTermEffMedImplants.2021036412

Kachhara, S., Nallaswamy, D., Ganapathy, D., & Ariga, P. (2021). Comparison of the CBCT, CT, 3D printing, and CAD-CAM milling options for the most accurate root form duplication required for the root analogue implant (RAI) protocol. Journal of Indian Academy of Oral Medicine and Radiology, 33(2), 141–145.

Katyal, D., Jain, R. K., Sankar, G. P., & Prasad, S. (2023). Antibacterial, Cytotoxic, Mechanical Characteristics Novel Chitosan-Modified Orthodontic Primer: : In-Vitro: Study. Journal International Oral Health, 15(3), 284–289.

Klossner, R. R., Queen, H. A., Coughlin, A. J., & Krause, W. E. (2008). Correlation of Chitosan’s Rheological Properties and Its Ability to Electrospin. https://doi.org/10.1021/bm800738u

Lampl, S., Gurunathan, D., Krithikadatta, J., Mehta, D., & Moodley, D. (2023). Reasons for Failure of CAD/CAM Restorations in Clinical Studies: A Systematic Review and Meta-analysis. The Journal of Contemporary Dental Practice, 24(2), 129–136.

Liu, C., Zhu, C., Li, J., Zhou, P., Chen, M., Yang, H., & Li, B. (2015). The effect of the fibre orientation of electrospun scaffolds on the matrix production of rabbit annulus fibrosus-derived stem cells. Bone Research, 3(1), 1–9.

Lu, Y., Geng, W., Li, L., Xie, F., Zhang, M., Xie, H., & Cai, J. (2025). Enhanced antibacterial and antibiofilm activities of quaternized ultra-highly deacetylated chitosan against multidrug-resistant bacteria. International Journal of Biological Macromolecules, 298, 140052.

Meenakshi, P. S., & Rajasekar, A. (2024). Assessment of mechanical properties and antimicrobial effects of Hyaluronic Acid coating on absorbable suture material: An in-vitro study. Journal of Clinical and Diagnostic Research: JCDR. https://doi.org/10.7860/jcdr/2024/66445.19058

Mondal, M. I. H. (2019). Cellulose-Based Superabsorbent Hydrogels. Springer.

Nanosized Drug Delivery Systems: Colloids and Gels for Site Specific Targeting. (n.d.). Google Books. Retrieved March 26, 2025, from https://books.google.com/books/about/Nanosized_Drug_Delivery_Systems_Colloids.html?id=sJX9DwAAQBAJ

Nityasri, A., Prasad, K., Deveswaran, R., & Ranganath, K. (2025). Effect of hyaluronic acid gel with and without metronidazole on healing of extraction sockets in diabetic patients-a randomized controlled study. Oral and Maxillofacial Surgery, 29(1), 72.

Novel Biomaterials for Tissue Engineering 2018. (n.d.). Google Books. Retrieved March 26, 2025, from https://books.google.com/books/about/Novel_Biomaterials_for_Tissue_Engineerin.html?id=mXGGDwAAQBAJ

Pandiyan, I., Arumugham, M. I., Doraikannan, S. S., Rathinavelu, P. K., Prabakar, J., & Rajeshkumar, S. (2023). Antimicrobial and Cytotoxic Activity of Ocimum tenuiflorum and Stevia rebaudiana-Mediated Silver Nanoparticles - An In vitro Study. Contemporary Clinical Dentistry, 14(2), 109–114.

Pavithra, S., Paulraj, J., Rajeshkumar, S., & Maiti, S. (2023). Comparative evaluation antimicrobial activity compressive strength conventional thyme-modified glass ionomer cement. Annals Dental Specialty, 11(1-2023), 70–77.

Priyadharshini, G., Gheena, S., Ramani, P., Rajeshkumar, S., & Ramalingam, K. (2023). Assessment antimicrobial efficacy cytotoxicity Cocos nucifera Triticum aestivum combination gel formulation therapeutic use. World Journal Dentistry, 14(5), 414–418.

Rajeshkumar, S., & Lakshmi, T. (2021). Green synthesis gold nanoparticles using kalanchoe pinnata its free radical scavenging activity. Int J Dentistry Oral Sci, 8(7), 2981–2984.

Ramsundar, K., Jain, R. K., Balakrishnan, N., & Vikramsimha, B. (2023). Comparative evaluation bracket bond failure rates novel non-primer adhesive conventional primer-based orthodontic adhesive-a pilot study. Journal Dental Research, 17(1).

Rieshy, V., Chokkattu, J. J., Rajeshkumar, S., & Neeharika, S. (2023). Mechanism action clove ginger herbal formulation-mediated TiO2 nanoparticles against lactobacillus species: vitro study. Journal Advanced Oral Research, 14(1), 61–66.

Roberts, C. R., Roughley, P. J., & Mort, J. S. (1989). Degradation of human proteoglycan aggregate induced by hydrogen peroxide. Protein fragmentation, amino acid modification and hyaluronic acid cleavage. In Biochemical Journal (Vol. 259, Issue 3, pp. 805–811). https://doi.org/10.1042/bj2590805

Saadh, M. J., Rasulova, I., Khalil, M., Farahim, F., Sârbu, I., Ciongradi, C. I.  (2024). Natural killer cell-mediated immune surveillance in cancer: Role of tumor microenvironment. Pathology-Research and Practice, 254, 155120.

Shenoy, A., Maiti, S., Nallaswamy, D., & Keskar, V. (2023). An in vitro comparison of the marginal fit of provisional crowns using the virtual tooth preparation workflow against the traditional technique. Journal of Indian Prosthodontic Society, 23(4), 391–397.

Singh, S., Prasad, A. S., & Rajeshkumar, S. (2023). Cytotoxicity, antimicrobial, anti-inflammatory and antioxidant activity of camellia sinensis and citrus mediated copper oxide nanoparticle-an in vitro study. Journal of International Society of Preventive & Community Dentistry, 13(6), 450–457.

Sivakumar, N., Geetha, R. V., Priya, V., Gayathri, R., & Ganapathy, D. (2021). Targeted phytotherapy forreactive oxygen species linked oral cancer. Int J Dent Oral Sci, 8.

Spasova, M., Manolova, N., Paneva, D., & Rashkov, I. (2004). Preparation of chitosan-containing nanofibres by electrospinning of chitosan/poly(ethylene oxide) blend solutions. E-Polymers, 4(1). https://doi.org/10.1515/epoly.2004.4.1.624

Subramanian, A. K., Lalit, H., & Sivashanmugam, P. (2023). Preparation, characterization, and evaluation of cytotoxic activity of a novel titanium dioxide nanoparticle-infiltrated orthodontic adhesive: An in vitro study. World Journal of Dentistry, 14(10), 882–887.

Tendon Stem Cells from Basic Biology to Clinical Application. (n.d.). Google Books. Retrieved March 26, 2025, from https://books.google.com/books/about/Tendon_Stem_Cells_from_Basic_Biology_to.html?id=78qPEAAAQBAJ

Thomas, & Jain, R. K. (2023). Influence operator experience scanning time accuracy two different intraoral scanners-a prospective clinical trial. Turkish Journal Orthodontics, 36(1).

Yan, S., Zhang, Q., Wang, J., Liu, Y., Lu, S., Li, M., & Kaplan, D. L. (2013). Silk fibroin/chondroitin sulfate/hyaluronic acid ternary scaffolds for dermal tissue reconstruction. Acta Biomaterialia, 9(6), 6771–6782.

Zhang, W., Liu, Y., Zhang, L., & Shen, X. (2025). Development of hyaluronic acid-based hydrogels for chronic diabetic wound healing: A review. International Journal of Biological Macromolecules, 308(Pt 1), 142273.