Evaluation of the Effectiveness of SrO-Infused Biopolymer Composites in Guided Bone Regeneration: A Comparative Study of Chitosan, Hyaluronic Acid, and Gelatin-Based Membranes

Akash Neelakanta Pillai1 , H.Neha1,a)

1Akash Medical Centre, Vijayawada, Andhra Pradesh, India

Corresponding Author: a)neha.bds20@gmail.com

Abstract: To evaluate the Effectiveness of SrO-Infused Biopolymer Composites in Guided Bone Regeneration: A Comparative Study of Chitosan, Hyaluronic Acid, and Gelatin-Based MembranesGuided bone regeneration (GBR) is a cornerstone of periodontal and implant therapy, aimed at regenerating bone in areas with defects. Barrier membranes play a pivotal role in this process, promoting bone tissue regeneration by preventing non-osteogenic tissues from infiltrating the defect site. Among natural polymers, hyaluronic acid (HA), chitosan, and chondroitin sulphate have shown potential due to their biocompatibility and osteogenic properties. Strontium oxide (SrO) is a bioactive material that enhances bone regeneration, making it an excellent candidate for GBR membranes. This study investigates the enhancement of GBR membranes by combining SrO with HA, chitosan, and chondroitin sulphate to improve their osteoinductive potential.Scaffolds were fabricated by blending 1% gelatin, 0.5% carrageenan, and 1% of a biopolymer (medium molecular weight hyaluronic acid, chitosan, chondroitin sulphate, or high/low molecular weight HA) in a 6:1:3 ratio. SrO nanoparticles were incorporated into the test groups. The membranes were characterized using scanning electron microscopy (SEM), Fourier transform infrared spectroscopy (FTIR), contact angle measurements, swelling ratio studies, and biocompatibility assays. Osteogenesis was evaluated using Alizarin red staining. SEM analysis demonstrated that SrO incorporation enhanced the porosity of the membranes. FTIR confirmed the presence of SrO nanoparticles, and contact angle measurements showed that all membranes were hydrophilic. Swelling studies revealed the highest water retention in chitosan and medium molecular weight HA + SrO groups. Biocompatibility assays showed excellent cell viability, with SrO-enriched membranes outperforming others. Alizarin red staining confirmed enhanced osteogenesis in SrO-based membranes, particularly in medium molecular weight HA + SrO and chitosan + SrO groups.The SrO GBR membrane scaffold synthesized with medium molecular weight hyaluronic acid demonstrated enhanced physicochemical and biological properties, making it a promising candidate for clinical GBR applications. Other biopolymers, including chitosan and chondroitin sulphate, also demonstrated strong potential in improving membrane functionality.

Keywords: GBR membrane, hyaluronic acid, chitosan, chondroitin sulphate, SrO, fabrication, biocompatibility, SEM, FTIR

# INTRODUCTION

Guided bone regeneration (GBR) is a critical procedure in dental implantology and periodontology, aimed at regenerating bone tissue in areas with significant bone loss(Website, n.d.-a). The success of GBR procedures relies heavily on the use of barrier membranes that selectively promote osteogenesis while preventing non-osteogenic tissues from infiltrating the defect(Abrams, 2002). These membranes act as a physical barrier, creating an optimal environment for the regeneration of new bone and periodontal tissues(Lee, 2017; Salau et al., 2022)(Fernandes et al., 2022).Recent advancements in GBR membrane design have focused on incorporating bioactive materials that not only act as structural barriers but also promote cellular growth and differentiation (Ramsundar et al., 2023; Rieshy et al., 2023; Singh et al., 2023). Among the most studied materials are natural polymers such as hyaluronic acid (HA), chitosan, and chondroitin sulphate, which are biocompatible, biodegradable, and capable of promoting cell adhesion, migration, and proliferation(Fu et al., 2019).Hyaluronic acid, a glycosaminoglycan, has been shown to have significant therapeutic effects in tissue regeneration due to its high water retention, ability to support cell migration, and involvement in ECM remodeling(Chun et al., 2018). The molecular weight of HA plays a crucial role in its function (Pavithra et al., 2023; Shenoy et al., 2023; Thomas & Jain, 2023). High molecular weight HA has been traditionally used for its ability to form hydrogels and promote tissue hydration(Smith, 2005)(Waddington & Sloan, 2016). However, medium molecular weight HA has been identified as more effective in facilitating cellular interactions, promoting osteoblast proliferation, and enhancing the overall osteoinductive potential of GBR membranes(Chandra & Prakash, 2020; Shastri et al., 2010).Chitosan, a polysaccharide derived from chitin, is another promising material for GBR membranes. It possesses inherent antimicrobial properties, making it useful in preventing infections in bone regeneration sites(Brienzo, 2022; Erickson, 2018). Additionally, chitosan has been shown to enhance osteoblast proliferation and ECM formation, which are critical for effective bone regeneration(Swanson, 2016).Chondroitin sulphate, a major component of cartilage, is known for its ability to support cartilage and bone formation(Brown & Constantz, 2017). Its use in GBR membranes has been explored for its potential to improve bone regeneration by promoting osteoblastic differentiation and increasing the mechanical strength of the membrane(Swain & Biswal, 2023).Strontium oxide (SrO) is a bioactive material with osteoinductive properties that have been demonstrated to enhance bone healing and regeneration([No Title], n.d.). SrO promotes osteoblast differentiation while inhibiting osteoclast activity, leading to increased bone formation and decreased bone resorption(Pawelec & Planell, 2018; Website, n.d.-b). The incorporation of SrO into GBR membranes can potentially improve their osteogenic properties, making them more effective in promoting bone regeneration(Website, n.d.-c)(Harikrishnan et al., 2021).This study aims to fabricate GBR membranes by incorporating SrO nanoparticles with medium molecular weight hyaluronic acid, chitosan, and chondroitin sulphate (Doshi et al., 2023; Lampl et al., 2023; Pandiyan et al., 2023). The primary objective is to evaluate the physicochemical and biological properties of these membranes, focusing on their porosity, hydrophilicity, swelling capacity, biocompatibility, and osteoinductive potential. We hypothesize that SrO-enriched membranes will exhibit superior osteogenesis compared to non-SrO membranes, and that different biopolymers will contribute varying degrees of enhancement in membrane functionality.

# MATERIALS AND METHODS

## Materials

Biopolymers: High molecular weight hyaluronic acid (HA), medium molecular weight hyaluronic acid (HA), Low molecular weight hyaluronic acid (HA), chitosan, and chondroitin sulphate were obtained from commercial suppliers.

Crosslinking Agent: 15% Tripolyphosphate (TPP) was used for crosslinking the polymer matrix.

Nanoparticles: Strontium oxide (SrO) nanoparticles (10 mg) were added to the test groups for osteoinductive enhancement.

Solvents and Reagents: Gelatin (1%), carrageenan (0.5%), and phosphate-buffered saline (PBS) were used for scaffold fabrication and characterization.

## Scaffold Fabrication

Scaffolds were fabricated by blending the biopolymers in a 6:1:3 ratio of gelatin, carrageenan, and polymer (HA, chitosan, or CS). The solutions were mixed thoroughly, and SrO nanoparticles (10 mg) were added to the test groups(Website, n.d.-d). The mixture was then cast into six-well plates, and 100 µL of 15% TPP was added to each well to initiate crosslinking. The plates were stored at -20°C for 12 hours, followed by storage at -80°C overnight to freeze the scaffolds. The frozen samples were lyophilized for 24 hours to obtain dry, porous scaffolds(Website, n.d.-e).

## Characterization Techniques

Scanning Electron Microscopy (SEM): SEM (JEOL, Japan) was used to examine the surface morphology and porosity of the scaffolds at 100X magnification.

Fourier Transform Infrared Spectroscopy (FTIR): FTIR (Bruker ATR) was used to identify the chemical bonds and functional groups present in the scaffolds, particularly to confirm the incorporation of SrO nanoparticles.

Contact Angle Measurement: The contact angle of the scaffolds was measured to assess hydrophilicity, using a goniometer to drop 50 µL of distilled water on the surface of the scaffold and measure the angle formed between the water droplet and the surface.

Swelling Ratio: The scaffolds were immersed in PBS at 37°C for 24 hours. The swelling ratio was calculated by measuring the initial and wet weight of the scaffolds.

Biocompatibility (MTT Assay): Dental pulp stem cells (hDPSCs) were cultured with the scaffold-conditioned media for 24 and 48 hours. Cell viability was assessed using the MTT assay, and the absorbance was measured at 570 nm.

Osteogenesis Assay: The osteogenic potential was evaluated by Alizarin red staining, which detects calcium deposition in osteoblastic cultures. The scaffolds were cultured with osteoblasts in differentiation medium for 14 days, and the amount of calcium mineralization was measured spectrophotometrically at 405 nm.

# RESULTS

## SEM Analysis

SEM images revealed significant differences in the microstructure of the membranes depending on the biopolymer used. The incorporation of SrO enhanced the porosity of the membranes, making them more suitable for cell migration and nutrient diffusion.

FIGURE 1: Figure 1 represents the SEM analysis of the chitosan particles(A) and the test group Chitosin+SrO(B)

A)

B)

FIGURE 2 : The Picture depicts the SEM analysis of Chondroitin Sulphate(CS) and the Test group(CS+SrO)

A)

B)

C)

Fig 3: SEM images of the low(A), medium(B) and high(C) molecular weight hyaluronic acid + SrOGbr membrane.

Medium Molecular Weight HA + SrO exhibited regular, evenly distributed pores with a slightly rough surface structure that is conducive to osteoblast adhesion.

Chitosan + SrO membranes exhibited high porosity and irregular voids, which could support rapid cell infiltration and nutrient flow.

High Molecular Weight HA +SrO showed denser regions with less porosity, limiting the space for cellular activity.

Low Molecular Weight HA +SrO showed little denser regions with less porosity, limiting the space for cellular activity.

Chondroitin Sulphate +Sro had a denser and more compact structure, which could potentially restrict osteoblast migration and bone formation.

## FTIR Analysis

A)

B)

C)

D)

E)

Figure 4: (a) – (e)FTIR spectra confirmed the successful incorporation of SrO nanoparticles in the polymer matrices.

Peaks at 871 cm^-1, 613 cm^-1, and 1126 cm^-1 were indicative of the SrO nanoparticles present in the scaffolds. These peaks were absent in the control (non-SrO) membranes, confirming the nanoparticle incorporation.

## Contact Angle Measurement

Contact angle measurements revealed that all scaffolds were hydrophilic, with the following contact angles:

A)

B)

C)

D)

E)

Figure 5: (a)-(e) contact angle management

(HMM)HA + SrO: 26.7°

(MMM)HA + SrO: 20.66°

(LMM)HA + SrO: 28.36°

Chitosan + SrO: 38.49°

Chondroitin Sulphate + SrO: 29.4° The increase in contact angle with SrO incorporation suggests a reduction in the membrane’s surface hydrophilicity, which may affect protein adsorption and cell adhesion (Almatrafi et al., 2024).

## Swelling Ratio

Figure 6: The swelling test between the groups,  When compared, C+HA sample has shown high swelling property on the addition of  SrO.

The swelling ratio was significantly higher in the Chitosan + SrO and High Molecular Weight HA + SrO groups compared to the others, indicating better water retention and nutrient diffusion capabilities(Saadh et al., 2024).

High Molecular Weight HA + SrO exhibited a swelling ratio of 110%.

Chitosan + SrO exhibited a swelling ratio of 135%. This high water retention is advantageous for maintaining a hydrated environment conducive to cell growth and regeneration.

## Biocompatibility (MTT Assay)

Figure 7: The biocompatibility between the groups,  When compared, C+HA sample has shown high biocompatiblity property on the addition of  SrO.

The MTT assay showed that all the scaffolds were biocompatible, with SrO-enriched scaffolds exhibiting enhanced cell viability:

Chitosan + AgO: 85% cell viability

Medium Molecular Weight HA + SrO: 82% cell viability

Chondroitin Sulphate + SrO: 53% cell viability The SrO-enriched scaffolds demonstrated enhanced cell attachment and proliferation, likely due to the osteoinductive properties of SrO.

## Osteogenesis (Alizarin Red Staining)

Alizarin red staining revealed the highest levels of calcium deposition in the SrO-based scaffolds, indicating strong osteogenic differentiation:

Medium Molecular Weight HA + SrO: OD 0.45

Chitosan + AgO: OD 0.42

Chondroitin Sulphate + SrO: OD 0.38 These results suggest that SrO incorporation significantly enhances osteogenesis, with medium molecular weight HA + SrO membranes showing the strongest osteogenic response.

# DISCUSSION

The development of Guided Bone Regeneration (GBR) membranes incorporating strontium oxide (SrO) has garnered significant attention in bone tissue engineering due to SrO's osteoinductive properties. In our study, we evaluated the effectiveness of SrO-enriched GBR membranes composed of various biopolymers, including chitosan, hyaluronic acid (HA), and gelatin. The findings indicated that these membranes exhibited favorable biocompatibility and promoted osteogenic differentiation, thereby enhancing bone regeneration.​

## Chitosan-Based Membranes

Chitosan, a natural polysaccharide derived from chitin, has been extensively studied for its applications in tissue engineering. Its cationic nature facilitates interactions with negatively charged cell surfaces, promoting cell attachment and proliferation. Studies have demonstrated that chitosan-based scaffolds support the growth of various cell types, including osteoblasts, and can be utilized in bone tissue engineering applications (Janani et al., 2021; Kachhara et al., 2021; Subramanian et al., 2023). However, the mechanical strength of chitosan scaffolds is relatively low, which may limit their effectiveness in load-bearing applications. To address this issue, chitosan is often combined with other materials to enhance its mechanical properties.​

## Gelatin-Based Membranes

Gelatin, derived from denatured collagen, shares many of the native extracellular matrix's characteristics, such as biodegradability and biocompatibility. Gelatin-based scaffolds have been shown to support osteoblast attachment and differentiation, making them suitable for bone tissue engineering (Gandhi et al., 2021; Katyal et al., 2023; Priyadharshini et al., 2023). However, gelatin's low mechanical strength and rapid degradation rate pose challenges for its use in bone regeneration. To overcome these limitations, researchers have explored the incorporation of nanohydroxyapatite (nHA) into gelatin scaffolds. The addition of nHA has been shown to enhance the mechanical properties of gelatin/nHA cryogel scaffolds, making them more suitable for bone regeneration applications(Al-Douri, 2020);(Afonso et al., 2016).

## Hyaluronic Acid (HA)-Based Membranes

HA, a major component of the extracellular matrix, plays a crucial role in tissue hydration, elasticity, and cellular function (Chokkattu et al., 2023; Dharman et al., 2023; Govindaraj & Shanmugam, 2023). HA-based membranes have demonstrated excellent biocompatibility and have been shown to support osteogenic differentiation. The incorporation of HA into GBR membranes has been associated with enhanced bone regeneration. For instance, the combination of biphasic calcium phosphate scaffolds with HA-gelatin hydrogels has been proposed as a novel approach for bone regeneration, leveraging the synergistic effects of both materials(Shalumon et al., 2019) ​(Stribeck & Smarsly, 2005).

## Comparative Analysis

The comparative analysis of different biopolymers in this study highlights the importance of selecting materials that offer a balance between mechanical strength, biocompatibility, and osteoinductive properties (Rajeshkumar & Lakshmi, 2021; Sivakumar et al., 2021). While chitosan-based membranes provide antimicrobial benefits, their mechanical limitations may restrict their use in certain applications. Gelatin-based membranes offer favorable cell attachment properties but may require reinforcement to enhance mechanical strength. HA-based membranes, particularly when combined with SrO, provide a promising balance of mechanical integrity and biological activity, making them suitable candidates for GBR applications(Inamuddin, 2019).

## CONCLUSION

Incorporating SrO nanoparticles into GBR membranes significantly enhances their osteoinductive properties. The combination of Medium Molecular Weight Hyaluronic Acid with SrO nanoparticles outperformed other formulations in terms of osteogenesis, porosity, and biocompatibility. Chitosan and chondroitin sulphate also demonstrated strong potential for GBR applications, with chitosan showing enhanced antimicrobial properties. Future studies should explore the in vivo efficacy of these membranes to validate their performance in clinical settings.

# REFERENCES

Almatrafi, T. A.,  Almohaimeed, H. M., Chakravarthi, S., Amin, A. H., Jafer, A.,  & Akhavan-Sigari, R. (2024). Reducing metastasis ability of gastric cancer cell line by targeting MMP16 using miR-193a-5p and 5-FU. Advances in Medical Sciences, 69(2), 463-473.

Abrams, P. (2002). Incontinence: 2nd International Consultation on Incontinence.

Afonso, C. A. M., Candeias, N. R., Simão, D. P., Trindade, A. F., Coelho, J. A. S., Tan, B., & Franzén, R. (2016). Comprehensive Organic Chemistry Experiments for the Laboratory Classroom. Royal Society of Chemistry.

Al-Douri, Y. (2020). Metal Oxide Powder Technologies: Fundamentals, Processing Methods and Applications. Elsevier.

Brienzo, M. (2022). Hemicellulose Biorefinery: A Sustainable Solution for Value Addition to Bio-Based Products and Bioenergy. Springer Nature.

Brown, P. W., & Constantz, B. (2017). Hydroxyapatite and Related Materials. CRC Press.

Chandra, P., & Prakash, R. (2020). Nanobiomaterial Engineering: Concepts and Their Applications in Biomedicine and Diagnostics. Springer Nature.

Chokkattu, J. J., Neeharika, S., Brahmajosyula, I. P., & Thangavelu, L. (2023). Comparative Evaluation Cellular Toxicity Three Heat Polymerized Acrylic Resins: Vitro Study. World, 14(6).

Chun, H. J., Park, K., Kim, C.-H., & Khang, G. (2018). Novel Biomaterials for Regenerative Medicine. Springer.

Dharman, S., Maragathavalli, G., Shanmugam, R., & Shanmugasundaram, K. (2023). Biosynthesis Turmeric Silver Nanoparticles: Its Characterization Evaluation Antioxidant, Anti inflammatory, Antimicrobial Potential Against Oral Pathogens vitro Study. Journal Indian Academy Oral Medicine Radiology, 35(3), 299–305.

Doshi, K., Nivedhitha, M. S., Solete, P., Dp, S., Jacob, B., & Siddique, R. (2023). Effect adhesive strategy universal adhesives noncarious cervical lesions-an updated systematic review meta-analysis. BDJ open. 9.

Erickson, A. E. (2018). Chitosan-based Scaffolds for Tissue Engineering and Cancer Research Applications.

Fernandes, J., Rohinikumar, S., Nessapan, T., Rani, D., Abhinav, R. P., & Gajendran, P. (2022). CBCT Analysis of Prevalence of the Canalis Sinuosus on the Alveolar Ridge in the Site of Endosseous Implant Placement: A Retrospective Study. Journal of Long-Term Effects of Medical Implants, 32(2), 45–50.

Fu, J., Jin, Z., & Wang, J.-W. (2019). UHMWPE Biomaterials for Joint Implants: Structures, Properties and Clinical Performance.

Gandhi, J. M., Gurunathan, D., Doraikannan, S., & Balasubramaniam, A. (2021). Oral health status for primary dentition - A pilot study. Journal of the Indian Society of Pedodontics and Preventive Dentistry, 39(4), 369–372.

Govindaraj, P., & Shanmugam, R. (2023). Effect chlorhexidine fluoride varnish incidence white spot lesion orthodontic patients. Annals Dental Specialty, 11(1-2023), 35–39.

Harikrishnan, R., Subhashree, R., Ganesh, S. B., & Ashok, V. (2021). Relation between Bone Density and Primary Stability in the Posterior Mandibular Region in Patients Undergoing Dental Implant Treatment: A Retrospective Study. Journal of Long-Term Effects of Medical Implants, 31(2), 71–79.

Inamuddin. (2019). Applications of Ion Exchange Materials in Biomedical Industries. Springer.

Janani, K., Teja, K. V., & Ajitha, P. (2021). Cytotoxicity of oregano essential oil and calcium hydroxide on L929 fibroblast cell: A molecular level study. Journal of Conservative Dentistry: JCD, 24(5), 457–463.

Kachhara, S., Nallaswamy, D., Ganapathy, D., & Ariga, P. (2021). Comparison of the CBCT, CT, 3D printing, and CAD-CAM milling options for the most accurate root form duplication required for the root analogue implant (RAI) protocol. Journal of Indian Academy of Oral Medicine and Radiology, 33(2), 141–145.

Katyal, D., Jain, R. K., Sankar, G. P., & Prasad, S. (2023). Antibacterial, Cytotoxic, Mechanical Characteristics Novel Chitosan-Modified Orthodontic Primer: : In-Vitro: Study. Journal International Oral Health, 15(3), 284–289.

Lampl, S., Gurunathan, D., Krithikadatta, J., Mehta, D., & Moodley, D. (2023). Reasons for Failure of CAD/CAM Restorations in Clinical Studies: A Systematic Review and Meta-analysis. The Journal of Contemporary Dental Practice, 24(2), 129–136.

Lee, C. (2017). Clinical Case Series Study of a New Bilayer Collagen Membrane for Guided Bone Regeneration.

[No title]. (n.d.). Retrieved March 26, 2025, from http://paperpile.com/b/isM8Ic/teJBf

Pandiyan, I., Arumugham, M. I., Doraikannan, S. S., Rathinavelu, P. K., Prabakar, J., & Rajeshkumar, S. (2023). Antimicrobial and Cytotoxic Activity of Ocimum tenuiflorum and Stevia rebaudiana-Mediated Silver Nanoparticles - An In vitro Study. Contemporary Clinical Dentistry, 14(2), 109–114.

Pavithra, S., Paulraj, J., Rajeshkumar, S., & Maiti, S. (2023). Comparative evaluation antimicrobial activity compressive strength conventional thyme-modified glass ionomer cement. Annals Dental Specialty, 11(1-2023), 70–77.

Pawelec, K., & Planell, J. A. (2018). Bone Repair Biomaterials: Regeneration and Clinical Applications. Woodhead Publishing.

Priyadharshini, G., Gheena, S., Ramani, P., Rajeshkumar, S., & Ramalingam, K. (2023). Assessment antimicrobial efficacy cytotoxicity Cocos nucifera Triticum aestivum combination gel formulation therapeutic use. World Journal Dentistry, 14(5), 414–418.

Rajeshkumar, S., & Lakshmi, T. (2021). Green synthesis gold nanoparticles using kalanchoe pinnata its free radical scavenging activity. Int J Dentistry Oral Sci, 8(7), 2981–2984.

Ramsundar, K., Jain, R. K., Balakrishnan, N., & Vikramsimha, B. (2023). Comparative evaluation bracket bond failure rates novel non-primer adhesive conventional primer-based orthodontic adhesive-a pilot study. Journal Dental Research, 17(1).

Rieshy, V., Chokkattu, J. J., Rajeshkumar, S., & Neeharika, S. (2023). Mechanism action clove ginger herbal formulation-mediated TiO2 nanoparticles against lactobacillus species: vitro study. Journal Advanced Oral Research, 14(1), 61–66.

Salau, A. O., Jain, S., & Sood, M. (2022). Computational Intelligence and Data Sciences: Paradigms in Biomedical Engineering. CRC Press.

Saadh, M. J., Rasulova, I., Khalil, M., Farahim, F., Sârbu, I., Ciongradi, C. I.  (2024). Natural killer cell-mediated immune surveillance in cancer: Role of tumor microenvironment. Pathology-Research and Practice, 254, 155120.

Shalumon, K. T., Liao, H.-T., Kuo, C.-Y., Wong, C.-B., Li, C.-J., P A, M., & Chen, J.-P. (2019). Rational design of gelatin/nanohydroxyapatite cryogel scaffolds for bone regeneration by introducing chemical and physical cues to enhance osteogenesis of bone marrow mesenchymal stem cells. Materials Science & Engineering. C, Materials for Biological Applications, 104, 109855.

Shastri, V. P., Altankov, G., & Lendlein, A. (2010). Advances in Regenerative Medicine: Role of Nanotechnology, and Engineering Principles. Springer.

Shenoy, A., Maiti, S., Nallaswamy, D., & Keskar, V. (2023). An in vitro comparison of the marginal fit of provisional crowns using the virtual tooth preparation workflow against the traditional technique. Journal of Indian Prosthodontic Society, 23(4), 391–397.

Singh, S., Prasad, A. S., & Rajeshkumar, S. (2023). Cytotoxicity, antimicrobial, anti-inflammatory and antioxidant activity of camellia sinensis and citrus mediated copper oxide nanoparticle-an in vitro study. Journal of International Society of Preventive & Community Dentistry, 13(6), 450–457.

Sivakumar, N., Geetha, R. V., Priya, V., Gayathri, R., & Ganapathy, D. (2021). Targeted phytotherapy forreactive oxygen species linked oral cancer. Int J Dent Oral Sci, 8.

Smith, R. (2005). Biodegradable polymers for industrial applications. CRC Press.

Stribeck, N., & Smarsly, B. (2005). Scattering Methods and the Properties of Polymer Materials. Springer Science & Business Media.

Subramanian, A. K., Lalit, H., & Sivashanmugam, P. (2023). Preparation, characterization, and evaluation of cytotoxic activity of a novel titanium dioxide nanoparticle-infiltrated orthodontic adhesive: An in vitro study. World Journal of Dentistry, 14(10), 882–887.

Swain, S. K., & Biswal, A. (2023). Chitosan Nanocomposites: Bionanomechanical Applications. Springer Nature.

Swanson, S. A. (2016). Chitosan-based Bilayer Hydroxyapatite Nanorod Composite Scaffolds for Osteochondral Regeneration.

Thomas, & Jain, R. K. (2023). Influence operator experience scanning time accuracy two different intraoral scanners-a prospective clinical trial. Turkish Journal Orthodontics, 36(1).

Waddington, R. J., & Sloan, A. J. (2016). Tissue Engineering and Regeneration in Dentistry: Current Strategies. John Wiley & Sons.

Website. (n.d.-a). Zou, D., et al. (2021). Advances in materials and techniques for guided bone regeneration in dental implantology. Journal of Biomaterials Applications, 35(2), 145-158. https://doi.org/10.1177/0885328220913125

Website. (n.d.-b). https://doi.org/10.1155/2020/6234391

Website. (n.d.-c). https://doi.org/10.2147/IJN.S326444

Website. (n.d.-d). https://doi.org/10.1186/s40824-020-00208-7

Website. (n.d.-e). https://doi.org/10.1089/ten.tec.2019.0187