Exploration and Evaluation of Copper Nanoparticle Synthesis from Red Seaweed; Comprehensive Cytotoxicity and Mutagenicity in Goldfish Carassius auratus

Akshat M Sakkaria1 , D.Sanjay1,a)

1Akshat Marine Products, Vijayawada, AndhraPradesh, India

Corresponding Author: a)sanjay432242@gmail.com

Abstract: This study explores the synthesis of copper nanoparticles from red seaweed (Gracilaria corticata) and evaluates their cytotoxic and mutagenic effects on goldfish (Carassius auratus). The Copper nanoparticles were characterized using UV-Vis spectroscopy, Fourier Transform Infrared, Scanning Electron Microscopy, and Energy Dispersive Spectroscopy. The UV-Vis spectrum showed a peak absorbance of 1.2 at 580 nm, indicating Copper nanoparticles formation. Fourier Transform Infrared analysis revealed functional groups such as Hydroxyl group, Amine group, Sulfoxide group, Alkyl group, and Alkyl halide group. Scanning Electron Microscopy indicated particle sizes between 20-80 nm. Energy Dispersive Spectroscopy confirmed the presence of Copper alongside other elements. The cytotoxicity tests showed that higher concentrations of Copper nanoparticles caused significant damage to erythrocytes, including cellular deformation and membrane rupture. Additionally, mutagenicity assessments identified nuclear abnormalities, such as binucleated cells, indicating genotoxic effects. These findings highlight the potential cytotoxic and mutagenic risks of biosynthesized seaweed Copper nanoparticles in aquatic organisms, emphasizing the need for further ecological risk assessments.

Keywords: Gracilaria corticata, Nanoparticle, Cytotoxicity, Mutagenicity, Carassius auratus, Aquatic tolerance, Eco-friendly.

# Introduction

Seaweed is broadly classified into green, brown, and red algae, each with distinct characteristics like providing habitat, food, and oxygen to marine life, as well as playing a role in nutrient cycling(Sultana et al., 2023).Seaweed serves as a nutritious food source, a key ingredient in industrial applications like food additives and cosmetics, a natural fertilizer in agriculture, and a potential biofuel(El-Beltagi et al., 2022)(G. & Ganapathy, 2022; Kumar & Ramesh, 2021)).Gracilaria corticata is a species of red seaweed known for its branching, filamentous structure and its ability to thrive in intertidal and subtidal zones, often attaching itself to rocks and other substrates(Sambhwani et al., 2022).Gracilaria corticata contributes significantly to coastal ecosystem health by providing habitat and food for marine organisms, participating in nutrient cycling, and stabilizing sediment(Gholamian et al., 2023). This green synthesis method not only reduces the environmental impact compared to traditional chemical synthesis but also enhances the functional properties of the nanoparticles (Vishwanath & Negi, 2021). Nanoparticles exhibit unique chemical and physical properties. Their small size and large surface area make them highly valuable in diverse fields such as medicine, electronics, and environmental science[6](Khan & Hossain, 2022).Nanoparticles can be synthesized from various materials, including metals, oxides, polymers, and carbon-based substances, each offering specific advantages for different applications(Siwal et al., 2020).Among the different types of nanoparticles, Copper NPs are known for their excellent electrical conductivity, thermal properties, and potent antimicrobial activity(Michaela Corina et al., 2021).Gracilaria corticata mediated copper nanoparticles(CuNPs) combine the beneficial properties of both the seaweed and copper, making them suitable for diverse applications, including antimicrobial coatings, drug delivery systems, and environmental cleanup efforts (Naveenkumar et al., 2024).Also, Gracilaria corticata induced nanoparticles have shown promise in various applications, including biomedical fields for their anti-inflammatory, antioxidant, and anti-microbial properties(Pulakkat & Patravale, 2020).Copper nanoparticles (CuNPs) synthesized from seaweed have attracted interest for their eco-friendly production and potential applications, including evaluating their effects on aquatic organisms like the common goldfish (Carassius auratus) in toxicity studies (Qiao et al., 2022).Goldfish (Carassius auratus) exhibit remarkable environmental tolerance, enduring wide pH variations, high turbidity, significant temperature fluctuations and can remain active under hypoxic conditions for extended periods and even tolerate anoxia(Filice et al., 2022).Goldfish are ideal model organisms due to their resilience to environmental stressors such as wide pH variations, high turbidity, and temperature fluctuations(Menon et al., 2023). The toxicological studies in this research primarily concentrated on erythrocytes, as they are sensitive to environmental pollutants and can indicate the organism's pathophysiological state(Mehra & Chadha, 2021; Zhang et al., 2022). Accordingly, the studies of cytotoxicity and mutagenicity potential on fish erythrocytes are limited(Ajay et al., 2023; Chokkattu et al., 2023; Padarthi et al., 2023). Additionally, micronucleus (MN) and erythrocyte nuclear abnormalities (ENA) assays can serve as indicators of chromosomal damage and mutagenic effects.Copper nanoparticles induce oxidative stress in goldfish tissues, leading to cellular damage and apoptosis, while also affecting blood parameters and liver function, thereby highlighting their toxicological impact on aquatic life (Ahmed & Sheikh, 2020).​

# Materials and method

The seaweed Gracilaria corticata (SIMATS/CMAR/SW/GC-01) samples were collected from the coastal environment of the Gulf of Mannar, South India. The collected samples were placed in a polythene bag and carried to the laboratory (Figure 1A), where it was properly washed with tap water and then with distilled water to remove the debris and salt. After being washed, the sample was shade dried for two to three weeks. The leaves were shade-dried for 2-3 weeks until they were transformed into a fine powder (Figure 1B). Then, 20g of the seaweed sample was combined with 100 ml of distilled water in a conical flask (Figure C). The flask containing the sample was then placed on an orbital shaker for 3 days. After this period, the samples underwent filtration using Whatman filter paper and stored for further analysis (Figure 1D, E).

A

B

C

D

E

Figure1., (A) and (B) (C) Collection and extract preparation of seaweed (D) Extract filtration using Whatmann filter paper (E) Crude extract of Gracilaria corticata

Biosynthesis of Cu NPs, 25 ml of aqueous extract was mixed with 75ml of Deionized water containing 10mM CuSO4. The resulting mixture was incubated in a shaker at 37˚c for 24 hours. Following incubation, a UV-Vis spec was used to detect the change in color from blue green to brownish red of the solution caused by the creation of Copper nanoparticles.Characterization is determined using analytical techniques. The formation of copper nanoparticles was confirmed by Ultraviolet-visible spectral analysis. A wavelength of 200–800 nm was used to determine the absorbance spectra using ultraviolet-visible spectroscopy. The bioactive compounds in the aqueous extract of the seaweed Gracilaria corticata are extracted by FTIR and are used to determine the possible functional group. The Energy-dispersive spectroscopy is used for the elemental analysis or chemical characterization of a sample. Using the Scanning Electron Microscope, the morphological characteristics of the copper nanoparticles were analyzed.Adult ornamental Goldfish were purchased from a commercial fish aquarium in Kolathur, Chennai, then acclimatized in tank at the Marine Biomedical Lab and Environmental Toxicology Unit. They were housed in 10 L aquaria with a max. Density of 1.3 g of fish per liter of water, maintained at 25 ± 2ºC. The water quality was ensured through continuous filtration and aeration. Fish were fed varied diets, including commercial dry pellet feed and dry tubifex worms. Daily health monitoring was conducted through visual examination, except on weekends. The blood sample was collected from the fish for further toxicity studies.Erythrocyte cytotoxicity was evaluated using morphometric analysis and the erythrocyte maturity index from the same slides used for the MN and ENA assays. The erythrocyte Morphometric followed the method of(Mofizur Rahman & Baek, 2019), with some modifications. For each fish, one hundred erythrocytes were randomly measured using Image J software under a light microscope at 100x magnification (Magnus). Morphometric indices of erythrocytes were evaluated using the criteria described by(Castro et al., 2018) . Additionally, the shapes of erythrocytes and their nuclei were analyzed after exposed to biosynthesized copper nanoparticles. The EMI determination was conducted following the method of (Pradhan et al., 2020), with modifications.The micronucleus (MN) and erythrocytic nuclear abnormalities (ENA) assays were performed according to the methods outlined by (Pradhan et al., 2020), with some modifications. Blood samples were collected via cardiac puncture, smeared onto slides, and air-dried. The smears were then fixed with ethanol for 1 minute and stained with Wright-Giemsa for 5 minutes. A total of two thousand erythrocytes per fish were randomly analyzed under a light microscope (Magnus) at 100x magnification using immersion lenses. The ENAs were classified into several categories: micronucleus (MN), lobed nucleus (LN), blebbed nucleus (BN), notched nucleus (NN), binucleated cell (BC), and kidney-shaped nucleus (KN), following the descriptions by(Pradhan et al., 2020) and (Roda et al., 2020), with adaptations.

# Results

The Biosynthesis of copper nanoparticles was successfully achieved using the red seaweed Gracilaria corticata. The cell-free supernatant of the seaweed sample was mixed with a CuSO₄ solution, and the mixture was incubated in a shaker at 37°C for 24 hours. A distinct color change from blue-green to brownish-red was observed (Figure 2A and B), indicating the formation of CuNPs.

A

B

Figure 2 .(A) and (B) Initial and final synthesis of Copper nanoparticles from Gracilaria corticata respectively

UV-Vis spectroscopy analysis confirmed the synthesis of Copper nanoparticles, showing a peak absorbance of 1.2 at a wavelength of 580nm (Figure 3), which is characteristic of copper nanoparticles. FTIR analysis of the synthesized Copper nanoparticles revealed the presence of various functional groups (Figure4). Strong, broad peaks at 3400.45 cm⁻¹ and 3176.58 cm⁻¹ correspond to O-H stretching vibrations, indicative of alcohol and carboxylic acid groups. A medium-intensity peak at 1592.40 cm⁻¹ is attributed to N-H bending vibrations, suggesting the presence of amine groups. Additional strong peaks at 1407.72 cm⁻¹ and 1038.85 cm⁻¹ are associated with S=O stretching vibrations from sulfonyl chloride and sulfoxide groups, respectively. The presence of a peak at 798.70 cm⁻¹ corresponds to C-H bending vibrations in a 1, 2, 3, 4-tetrasubstituted aromatic ring, indicating substituted benzene rings. Lastly, a strong peak at 594.09 cm⁻¹ is due to C-I stretching vibrations, suggesting the presence of halo compounds. SEM analysis revealed that the Copper nanoparticles were formed as aggregates with varying morphologies, ranging in size from 20 to 80 nm (Fig 5A), and included both crystalline and clustered nanoparticles. The Energy Dispersive Spectroscopy analysis confirmed the elemental composition of the Copper nanoparticles, (Fig 5B) showing the presence of carbon (46.6%), oxygen (28.2%), and copper (10.8%) as the primary elements. The analysis also detected aluminum (7.0%), chlorine (6.0%), magnesium (0.7%), and sulfur (0.6%), suggesting the successful synthesis of copper nanoparticles with potential trace impurities or components from the synthesis process.

Figure 3.UV-visible spectrophotometer of Biosynthesized copper nanoparticle from Carassius auratus

Figure 4.FTIR analysis of functional group from synthesized copper nanoparticles of Gracilaria corticata

A

B

Figure 5.(A) and (B) SEM and EDS image of synthesized copper nanoparticle from Carassius auratus

The cytotoxic effects of biosynthesized copper nanoparticles (CuNPs) on erythrocytes of Carassius auratus were rigorously analyzed after a 96-hour exposure period. The observed results, as presented in (Figure 6A), reveal substantial differences in the nuclear morphology of erythrocytes between the control and treated groups, highlighting the impact of CuNP exposure. The erythrocytes in the control group maintained normal cellular and nuclear morphology, with nuclei appearing round, intact, and uniformly stained. This indicates that under standard conditions, the erythrocytes of Carassius auratus remained healthy, with no signs of nuclear abnormalities or cytotoxic stress. The absence of any nuclear deformities serves as a baseline, confirming the experimental setup's integrity and the viability of the control cells. The presence of micronuclei within the erythrocytes is a critical indicator of chromosomal damage or loss. Micronuclei are formed when chromosome fragments or whole chromosomes fail to incorporate into the daughter nuclei during cell division. (Figure 6B, C, D) The occurrence of MN in CuNP-treated cells suggests that these nanoparticles interfere with the mitotic process, possibly by inducing DNA breaks or spindle apparatus malfunction. The frequency of micronuclei formation directly correlates with the level of genotoxic stress, implying that CuNPs may pose significant risks at the cellular level. Erythrocytes with lobed nuclei were prevalent among the CuNP-exposed groups. Lobed nuclei are characterized by irregular, segmented shapes, which can be a result of disrupted nuclear envelope formation or altered chromatin organization. This abnormality suggests that CuNPs may cause structural changes in the nuclear membrane, potentially affecting nuclear integrity and function. Lobed nuclei often indicate a compromised state of the cell, which may lead to impaired cellular processes and reduced cell viability. Nuclear blebbing is typically associated with apoptotic processes, where the cell undergoes programmed death due to irreparable damage. The formation of blebbed nuclei suggests that CuNPs might trigger apoptotic pathways in erythrocytes, leading to cell death. This phenomenon underscores the potential cytotoxicity of CuNPs, which may compromise the survival of exposed cells. The appearance of notched nuclei, with deep indentations or grooves, further indicates nuclear membrane instability in CuNP-exposed erythrocytes. Notching may result from mechanical stress on the nuclear envelope or disruptions in nuclear-cytoskeletal interactions. Such abnormalities can impair nuclear functions, including DNA replication and transcription, leading to cellular dysfunction. Notched nuclei in a significant portion of the treated cells suggest that CuNPs induce structural damage at the nuclear level, which may have broader implications for cell health. The alteration of nuclear shape to a kidney-like form in some erythrocytes reflects a substantial deviation from normal nuclear morphology. This abnormality may be caused by asymmetrical chromatin condensation or uneven nuclear envelope formation. Kidney-shaped nuclei could potentially lead to improper chromosomal segregation during cell division, further contributing to genetic instability. Such nuclear shapes in CuNP-exposed erythrocytes indicate that the nanoparticles may severely disrupt the normal nuclear architecture, which is crucial for maintaining cellular homeostasis.3.4 Mutagenicity activity on Carassius auratus exposed to biosynthesized Copper nanoparticles from Gracilaria corticata

A

B

C

D

Figure 6. Representative photomicrographs of erythrocytic nuclear abnormalities in Carassius auratus after exposure to extract for 96 h: (A) Control group (B)(C)(D) Exposed to copper nanoparticles micronucleus (MN), lobed nucleus (LN), blebbed nucleus (BN), notched nucleus (NN), and kidney-shaped nucleus (KN)

Mutagenicity analysis in erythrocyte cells of Carassius auratus exposed to the biosynthesized CuNPs revealed various nuclear abnormalities. (Figure7A)The control group displayed normal morphology with uniform nuclear shapes. (Figure7B)In contrast, cells exposed to CuNPs exhibited the presence of binucleated cells, a hallmark of cellular response to genotoxic stress, suggesting nuclear division errors induced by the CuNPs. The presence of micronuclei and other nuclear and cytoplasmic abnormalities showed a significant time-dependent increase (p<0.05) compared to the control group, indicating chromosomal damage due to nanoparticle exposure. These results highlight the mutagenic potential of biosynthesized seaweed copper nanoparticles in goldfish cells, leading to nuclear abnormalities and genotoxic stress. The study underscores the potential applications of CuNPs synthesized from Gracilaria corticata while emphasizing the importance of evaluating their cytotoxicity and mutagenicity in aquatic organisms.

A

B

Figure 7.Mutagenicity activity on Carassius auratus (A) Control group (B) Carassius auratus exposed to biosynthesized Copper nanoparticles from Gracilaria corticata

# Discussions

This study investigates the green synthesis of copper nanoparticles (CuNPs) using Gracilaria corticata and evaluates their cytotoxicity and mutagenicity in goldfish (Carassius auratus). The work highlights the potential environmental impact of biosynthesized CuNPs on aquatic organisms. The UV-Visible spectroscopy analysis in this study confirmed the successful biosynthesis of Copper nanoparticles from Gracilaria corticata, with a characteristic surface plasmon resonance (SPR) peak observed at 580 nm. This result aligns with other studies, such as the SPR peak at 570 nm for Acanthophora sp.(Krishnaswamy et al., 2024) and 580 nm for Ulva lactuca(Shanmugam et al., 2023). These findings suggest that the SPR peak varies depending on the type of seaweed extract used, reflecting the differences in nanoparticle formation and stabilization mechanisms(Dharman et al., 2023; S. Sindhu et al., 2023; Sreenivasagan et al., 2023). FTIR spectroscopy further corroborated the synthesis of Copper nanoparticles by identifying functional groups responsible for capping and stabilizing the nanoparticles (Evaluation Composite Restoration Posterior Teeth Proanthocyanidin Pretreatment Liner Using Fédération Dentaire Internationale Criteria: Split-Mouth Randomized Controlled Trial, n.d.; Pranati et al., 2021; Sakthi et al, 2021)). The broad peaks at 3400.45 cm⁻¹ and 3176.58 cm⁻¹ in the FTIR spectra are indicative of O-H stretching vibrations, similar to those reported by(Selmi et al., 2021), who identified polysaccharide peaks and significant binding sites for metal retention in their respective studies on algal-mediated CuO NPs and Asparagopsis taxiformis. These functional groups play a crucial role in the reduction of copper ions and stabilization of the nanoparticles, as seen in other studies using different plant extracts, such as Eichhornia crassipes(Kasabwala et al., 2021; Rajeshkumar & Lakshmi, 2021; Varghese et al., 2023). The SEM analysis in this study revealed that Copper nanoparticles synthesized from Gracilaria corticata form aggregates with varying morphologies, consistent with other reports where SEM and TEM analyses showed spherical morphologies of Copper nanoparticles, ranging from 40-50 nm (Marzban et al., 2022)to 0.5μm(Krishnaswamy et al., 2024). The EDS analysis confirmed the elemental composition of the synthesized CuNPs, including carbon, oxygen, and copper as primary elements, in agreement with findings by(Vidya & Chitra, 2018). Cytotoxicity and mutagenicity assessments demonstrated that the Copper nanoparticles induced dose-dependent cytotoxic effects and nuclear abnormalities in goldfish (Carassius auratus). The significant increase in micronuclei (MN) and other nuclear abnormalities, such as binucleated cells, observed in this study are in line with previous research, which highlighted the potential of nanoparticles to induce chromosomal damage(Ramachandran et al., 2018; Vidya & Chitra, 2018). The observed erythrocyte nuclear abnormalities, including lobed, blebbed, and notched nuclei, mirror the nuclear alterations reported in other fish species exposed to various pollutants, such as AgNPs, effluents, and microplastics(Keerthana & Ramesh, 2021; Murugesan, 2021; Tiwari & Jain, 2021)(Keerthana & Ramesh, 2021; Murugesan, 2021; Subramanian et al., 2021; Tiwari & Jain, 2021). This study, therefore, confirms the mutagenic potential of biosynthesized Copper nanoparticles, emphasizing the importance of assessing both cytotoxicity and mutagenicity when evaluating the environmental and biological impact of nanoparticles(Saadh et al., 2024). Moreover, the observed erythrocyte toxicity, as evidenced by changes in cell morphology and nuclear abnormalities, underscores the importance of using erythrocyte morphometric and nuclear integrity assays as effective tools for monitoring nanoparticle-induced stress in fish, as suggested by (Mofizur Rahman & Baek, 2019). The use of colchicine as a positive control in this study further validated the findings, given its known aneugenic properties and ability to induce micronuclei formation, as previously demonstrated in other fish species(Ramakrishnan et al., 2023; Shenoy & Maiti, 2023; J. S. Sindhu et al., 2023). In conclusion, the findings of this study provide valuable insights into the synthesis, characterization, and biological impact of Copper nanoparticles derived from Gracilaria corticata, while also highlighting the broader implications for environmental and aquatic toxicology research(Almatrafi et al., 2024).

# Conclusion

In conclusion, the synthesis of copper nanoparticles from red seaweed Gracilaria corticata was achieved with notable success, as evidenced by various characterization techniques. The cytotoxicity assessments revealed that elevated concentrations of Copper nanoparticles caused significant damage to goldfish erythrocytes, including noticeable cell deformation and membrane rupture, demonstrating a clear dose-dependent effect. Moreover, the mutagenicity tests uncovered various nuclear abnormalities, such as binucleated cells, signifying genotoxic effects induced by the nanoparticles. These results indicate that while seaweed-derived Copper nanoparticles hold potential for various applications, their environmental and biological impacts warrant further investigation. Addressing these concerns will be crucial for developing safe and sustainable uses of Copper nanoparticles in both industrial and environmental contexts.

# References

Almatrafi, T. A.,  Almohaimeed, H. M., Chakravarthi, S., Amin, A. H., Jafer, A.,  & Akhavan-Sigari, R. (2024). Reducing metastasis ability of gastric cancer cell line by targeting MMP16 using miR-193a-5p and 5-FU. Advances in Medical Sciences, 69(2), 463-473.

Ahmed, I., & Sheikh, Z. A. (2020). Comparative study of hematological parameters of snow trout Schizopyge plagiostomus and Schizopyge niger inhabiting two different habitats. The European Zoological Journal, 87(1), 12–19.

Ajay, R., JafarAbdulla, M. U., Sivakumar, J. S., Baburajan, K., Rakshagan, V., & Eyeswarya, J. (2023). Dental alloy adhesive primers and bond strength at alloy-resin interface: A systematic review and meta-analyses. The Journal of Contemporary Dental Practice, 24(8), 521–544.

Castro, D., Mieiro, C. L., Coelho, J. P., Guilherme, S., Marques, A., Santos, M. A., Duarte, A. C., Pereira, E., & Pacheco, M. (2018). Addressing the impact of mercury estuarine contamination in the European eel (Anguilla anguilla L., 1758) - An early diagnosis in glass eel stage based on erythrocytic nuclear morphology. Marine Pollution Bulletin, 127, 733–742.

Chokkattu, J. J., Mary, D. J., Shanmugam, R., & Neeharika, S. (2023). Evaluation clove ginger-mediated titanium oxide nanoparticles-based dental varnish against Streptococcus mutans Lactobacillus Species: vitro study. World J Dent, 14(3), 233–237.

Dharman, S., Maragathavalli, G., Shanmugam, R., & Shanmugasundaram, K. (2023). Curcumin mediated gold nanoparticles analysis its antioxidant, anti-inflammatory, antimicrobial activity against oral pathogens. Pesquisa Brasileira Em Odontopediatria E Clínica Integrada, 23.

El-Beltagi, H. S., Mohamed, A. A., Mohamed, H. I., Ramadan, K. M. A., Barqawi, A. A., & Mansour, A. T. (2022). Phytochemical and potential properties of seaweeds and their recent applications: A review. Marine Drugs, 20(6), 342.

Evaluation Composite Restoration Posterior Teeth Proanthocyanidin Pretreatment Liner Using Fédération Dentaire Internationale Criteria: Split-mouth Randomized Controlled Trial. (n.d.).

Filice, M., Cerra, M. C., & Imbrogno, S. (2022). The goldfish Carassius auratus: an emerging animal model for comparative cardiac research. Journal of Comparative Physiology. B, Biochemical, Systemic, and Environmental Physiology, 192(1), 27–48.

Gholamian, F., Karimi, N., Gholamian, F., & Bayat, P. (2023). Phycoremediation potential and agar yield of red macroalgae (Gracilaria corticata) against HEDP (hydroxyethylidene diphosphonic acid) and CAPB (cocoamidopropyl betaine) detergents and the heavy metal pollutants. Environmental Science and Pollution Research International, 30(45), 101110–101120.

G., K. E. V., & Ganapathy, D. (2022). Operator errors in failed composite restoration-A review. Int J Dent Oral Sci, 8(7), 2941–2944.

Kasabwala, H., Nallaswamy, D., Subhashree, R., & Ahmed, N. (2021). Evaluation Of Overall Marginal Accuracy Of DMLS Copings Fabricated Using 3 Different DMLS Printing Machines. Int J Dentistry Oral Sci, 8(7), 3335–3340.

Keerthana, T., & Ramesh, S. (2021). Knowledge, attitude and practice survey on awareness of the association between diet and dental erosion. International Journal of Dentistry and Oral Science, 8(2), 1533–1540.

Khan, S., & Hossain, M. K. (2022). Classification and properties of nanoparticles. In Nanoparticle-Based Polymer Composites (pp. 15–54). Elsevier.

Krishnaswamy, J., Christupaul Roseline, P., Kannan, K., Dhanraj, G., & Sivaperumal, P. (2024). Biosynthesis, characterization, and anticoagulant properties of copper nanoparticles from red seaweed of Acanthophora sp. Phytochemical Analysis: PCA. https://doi.org/10.1002/pca.3384

Kumar, I. L., & Ramesh, S. (2021). Knowledge, Attitude and Practices (KAP) survey of shade selection for indirect veneers. Int J Dent Oral Sci, 26, 2856–2864.

Marzban, A., Mirzaei, S. Z., Karkhane, M., Ghotekar, S. K., & Danesh, A. (2022). Biogenesis of copper nanoparticles assisted with seaweed polysaccharide with antibacterial and antibiofilm properties against methicillin-resistant Staphylococcus aureus. Journal of Drug Delivery Science and Technology, 74(103499), 103499.

Mehra, S., & Chadha, P. (2021). Naphthalene-2-sulfonate induced toxicity in blood cells of freshwater fish Channa punctatus using comet assay, micronucleus assay and ATIR-FTIR approach. Chemosphere, 265(129147), 129147.

Menon, S. V., Kumar, A., Middha, S. K., Paital, B., Mathur, S., Johnson, R., Kademan, A., Usha, T., Hemavathi, K. N., Dayal, S., Ramalingam, N., Subaramaniyam, U., Sahoo, D. K., & Asthana, M. (2023). Water physicochemical factors and oxidative stress physiology in fish, a review. Frontiers in Environmental Science, 11. https://doi.org/10.3389/fenvs.2023.1240813

Michaela Corina, C., Mocan, T., & Mocan, L. (2021). Copper nanoparticles: Synthesis and characterization, physiology, toxicity and antimicrobial applications. Applied Sciences (Basel, Switzerland), 12(1), 141.

Mofizur Rahman, M., & Baek, H. J. (2019). Evaluation of erythrocyte morphometric indices in juvenile red spotted grouper, Epinephelus akaara under elevated water temperature. Balsaeng’gwa Saengsig, 23(4), 345–353.

Murugesan, A. (2021). Saravana Dinesh SP evaluation of shear bond strength of ceramic brackets with two different base designs: An in-vitro study. Int J Dentistry Oral Sci. https://www.academia.edu/download/72981941/IJDOS_2377_8075_08_304.pdf

Naveenkumar, S., Kamaraj, C., Ragavendran, C., Vaithiyalingam, M., Sugumar, V., & Marimuthu, K. (2024). Gracilaria corticata red seaweed mediate biosynthesis of silver nanoparticles: larvicidal, neurotoxicity, molecular docking analysis, and ecofriendly approach. Biomass Conversion and Biorefinery, 14(17), 20587–20609.

Padarthi, L. C., Anumula, L., Chinni, S. K., Sannapureddy, S., & Govula, K. (2023). Evaluation Composite Restoration Posterior Teeth Proanthocyanidin Pretreatment Liner Using Fédération Dentaire Internationale Criteria: Split-mouth Randomized Controlled Trial. International Journal Prosthodontics Restorative Dentistry, 13(4), 191–200.

Pradhan, D., Singh, R. K., & Verma, S. K. (2020). Genotoxic potential assessment of the herbicide bispyribac-sodium in a fresh water fish Clarias batrachus (Linn.). Bulletin of Environmental Contamination and Toxicology, 105(5), 715–720.

Pranati, T., Ranjan, M., & Sandeep, A. H. (2021). Marginal adaptability custom made cast post made different techniques-a literature review. Int J Dentistry Oral Sci, 8(8), 3954–3959.

Pulakkat, S., & Patravale, V. B. (2020). Marine resources for biosynthesis and surface modification of anticancer nanoparticles. In Green Synthesis of Nanoparticles: Applications and Prospects (pp. 141–161). Springer Singapore.

Qiao, L., Dou, X., Song, X., & Xu, C. (2022). Green synthesis of nanoparticles by probiotics and their application. In Advances in Applied Microbiology (pp. 83–128). Elsevier.

Rajeshkumar, S., & Lakshmi, T. (2021). Biomedical potential of zinc oxide nanoparticles synthesized using plant extracts. Int J Dent Oral Sci, 8, 4160–4163.

Ramachandran, R., Krishnaraj, C., Kumar, V. K. A., Harper, S. L., Kalaichelvan, T. P., & Yun, S.-I. (2018). In vivo toxicity evaluation of biologically synthesized silver nanoparticles and gold nanoparticles on adult zebrafish: a comparative study. 3 Biotech, 8(10). https://doi.org/10.1007/s13205-018-1457-y

Ramakrishnan, M., Shanmugam, R., Neeharika, S., Chokkattu, J. J., Thangavelu, L., & Khanna, N. (2023). Anti-inflammatory activity and cytotoxic effect of ginger and Rosemary-mediated titanium oxide nanoparticles-based dental varnish. World Journal of Dentistry, 14(9), 761–765.

Roda, J. F. B., Lauer, M. M., Risso, W. E., & Bueno dos Reis Martinez, C. (2020). Microplastics and copper effects on the neotropical teleost Prochilodus lineatus: Is there any interaction? Comparative Biochemistry and Physiology. Part A, Molecular & Integrative Physiology, 242(110659), 110659.

Saadh, M. J., Rasulova, I., Khalil, M., Farahim, F., Sârbu, I., Ciongradi, C. I.  (2024). Natural killer cell-mediated immune surveillance in cancer: Role of tumor microenvironment. Pathology-Research and Practice, 254, 155120.

Sakthi, S.,et al. (2021). Thymus vulgaris mediated selenium nanoparticles, characterization and its antimicrobial activity - an in vitro study. International Journal of Dentistry and Oral Science, 3516–3521.

Sambhwani, K., Kazi, M. A., & Mantri, V. A. (2022). Gracilaria: An emerging source of agar feedstock—with special reference to industrially important species. In Sustainable Global Resources of Seaweeds Volume 2 (pp. 55–76). Springer International Publishing.

Selmi, A., Khiari, R., Snoussi, A., & Bouzouita, N. (2021). Analysis of minerals and heavy metals using ICP-OES and FTIR techniques in two red seaweeds (Gymnogongrus griffithsiae and Asparagopsis taxiformis) from Tunisia. Biological Trace Element Research, 199(6), 2342–2350.

Shanmugam, Pitchiah, S., Suresh, V., & Ramasamy, P. (2023). Biosynthesis of copper nanoparticles from seaweed Ulva lactuca and their in vitro antioxidative potential. Cureus. https://doi.org/10.7759/cureus.48985

Shenoy, N. D., & Maiti, S. (2023). Evaluation marginal fit CAD/CAM crowns using CBCT digital scanners. Annals Dental Specialty, 11(3-2023), 37–44.

Sindhu, J. S., Maiti, S., & Nallaswamy, D. (2023). Comparative analysis on efficiency and accuracy of parallel confocal microscopy and three-dimensional in motion video with triangulation technology-based intraoral scanner under influence of moisture and mouth opening - A crossover clinical trial. Journal of Indian Prosthodontic Society, 23(3), 234–243.

Sindhu, S., Maiti, S., & Nallaswamy, D. (2023). Factors affecting accuracy intraoral scanners-a systematic review. Annals Dental Specialty, 11(1-2023), 40–52.

Siwal, S. S., Zhang, Q., Devi, N., & Thakur, V. K. (2020). Carbon-based polymer nanocomposite for high-performance energy storage applications. Polymers, 12(3), 505.

Sreenivasagan, S., Subramanian, A. K., Mohanraj, K. G., & Kumar, R. S. (2023). Assessment of toxicity of Green Synthesized Silver Nanoparticle-coated Titanium Mini-implants with Uncoated Mini-implants: Comparison in an Animal Model Study. The Journal of Contemporary Dental Practice, 24(12), 944–950.

Subramanian, E., Ravindran, V., & Jeevanandan, G. (2021). Comparison of amount of tooth reduction in primary first molar for stainless steel, zirconia and fibre-glass crowns–in-vitro study. International Journal of Dentistry and Oral Science, 8(7), 3427–3430.

Sultana, F., Wahab, M. A., Nahiduzzaman, M., Mohiuddin, M., Iqbal, M. Z., Shakil, A., Mamun, A.-A., Khan, M. S. R., Wong, L., & Asaduzzaman, M. (2023). Seaweed farming for food and nutritional security, climate change mitigation and adaptation, and women empowerment: A review. Aquaculture and Fisheries, 8(5), 463–480.

Tiwari, A., & Jain, R. K. (2021). The effect of motivational and reminder therapy on the compliance of patients wearing fixed appliances. Int J Dent Oral Sci, 8(7), 3303–3305.

Varghese, R., Maliael, M., & Subramanian, A. (2023). Antibacterial activity of nanoparticle-coated orthodontic archwires: A systematic review. Journal of International Oral Health: JIOH, 15(1), 1.

Vidya, P. V., & Chitra, K. C. (2018). Evaluation of genetic damage in Oreochromis mossambicus exposed to selected nanoparticles by using micronucleus and comet bioassays. Ribarstvo, 76(3), 115–124.

Vishwanath, R., & Negi, B. (2021). Conventional and green methods of synthesis of silver nanoparticles and their antimicrobial properties. Current Research in Green and Sustainable Chemistry, 4(100205), 100205.

Zhang, C., Ye, L., Wang, C., Xiong, X., Li, Y., Li, P., Zhang, X., & Yu, H. (2022). Toxic effect of combined exposure of microplastics and copper on goldfish (Carassius auratus): Insight from oxidative stress, inflammation, apoptosis and autophagy in hepatopancreas and intestine. Bulletin of Environmental Contamination and Toxicology, 109(6), 1029–1036.