Development of energy-saving filterable nonwoven materials based on basalt and wool fibers for cement industry applications

OdilToshbekov a), Boltayeva Iqbol, Berdimurodova Zarina, Salimova Moxigul, Raximova Kamola

Termez State University, Termez, Uzbekistan

a) Сorresponding author: toshbekovo@tersu.uz

Abstract. The demand for filter nonwoven materials for industrial enterprises in the republic is mainly met through imports. This study investigates the development of a technology for producing these nonwoven materials from locally available basalt and wool fibers, as well as the economic efficiency of implementing this technology in practice. The annual economic efficiency was calculated by determining the production costs of the proposed technological option based on the developed methodology. Considering environmental issues, the use of mineral and animal fibers such as basalt and wool fibers is important. Plastic samples reinforced with basalt and wool fibers were subjected to standard tensile, bending, and compression tests. The obtained results will be discussed later, and the analyzed experimental data will be presented and compared.

INTRODUCTION

In recent years, the increased interest in environmental issues has encouraged the use of natural fibers in polymer reinforcement [1]. Many natural fibers such as sisal, hemp, jute, flax, coconut, and banana have been studied and applied. However, plant fibers are very sensitive to thermal and hygroscopic loads and have limited mechanical properties due to the fiber extraction system, difficulties in fiber alignment, fiber size, and interfacial strength.

Due to the recent deep research on designing technical filter non-woven fabrics for industrial enterprises based on local raw materials, over the past 10 years, a number of researchers have been studying the properties and behaviors of various composites made from continuous or short basalt fibers [2]. Undoubtedly, the performance of the non-woven material woven from these basalt and wool fibers and its potential applications remain largely unexplored. Additionally, some discrepancies have been observed among the results obtained by different authors.

Due to improvements in production technology, a new generation of basalt fibers is available on the global market. Spun basalt fibers are obtained at high temperatures from selected molten basalt rocks [3]. The process technology is very similar to that used for glass fibers. The rock is first pre-treated and then melted to obtain continuous fibers. The melt flows through one or more bushings containing hundreds of small holes. It has been established that it is possible to create new generation filters from filaments of non-woven fabrics based on basalt and wool fibers, using molten rock and animal fibers. Then, The filaments are drawn onto the roller. The advantage of this method is that no additives are needed during the production process, resulting in economic benefits and reduced environmental impact. Of course, depending on the type of the original rock and animal wool used, several categories of basalt fibers with different chemical compositions can be obtained. As a result, not all basalt and wool fibers have the same mechanical and physical properties.

Overall, among the positive characteristics of this new generation of basalt and jute fibers are sound insulation properties, excellent heat resistance (better than glass), good resistance to chemical attack, and low water absorption [4]. For the second reason, they are recommended for applications requiring thermal insulation, as well as for hot liquid transport pipes. Another important feature is expressed by high mechanical performance comparable to glass fiber [5], which, combined with a lower cost, can adapt this material to replace glass fibers in various industrial sectors such as aerospace, automotive, cement, asphalt plants, transportation, and shipbuilding.

The most important feature in composites, namely the fiber-matrix interface, has been studied in various basalt-wool fiber-polymer matrix systems [6], where it was shown that the surface area of polymer reinforced with basalt and wool fibers is superior to that reinforced with glass fibers after being immersed in salt water and absorbing moisture. However, remarkable surface shear strength was identified, and it was emphasized that basalt and wool fibers form a better surface compared to glass fibers.

On the other hand, glass fibers are known to be prone to surface damage and to exhibit high sensitivity to alkaline environments. When in contact with other chemical substances, they do not undergo chemical reactions that could be harmful to human health or the environment. Currently, there is no available evidence indicating risks associated with very low fiber diameters. However, according to European regulations [7] (97/69/EC and 1907/2006), fiber diameters greater than 6 mkm should not pose a toxicity risk.

EXPERIMENTAL RESEARCH

For vacuum bag molding plants, a filter cloth reinforced with basalt and wool fibers with flat dimensions of 300 mm × 300 mm was obtained through technical nonwoven fabric. Various types of reinforcements used: dry fabrics made from basalt and wool fibers, 200 g/m2, plain woven (warp 10F/10 mm, weft 10F/10 mm), tex 100, from ZLBM (De) and E-Glass dry fabric, 290 g/m2, plain woven (warp 5F/10 mm, weft 5F/10 mm), tex 300 (Della Betta Group, It, Re 290/50 WEB). The frontal view of both reinforcements is shown (A, B) [8].

Samples of basalt and wool fiber reinforced plastic were subjected to standard tests of tensile, bending, and compression. The obtained results will be discussed later, and the analyzed experimental data will be presented and compared [18-40]. The reported data consist of the average values of five or more tests, as well as standard deviations represented by vertical bars. In all conducted tests, non-woven fabrics made from basalt and wool fibers achieved good results [9].

By comparing the results of mechanical tests conducted on plastic laminates reinforced with basalt and wool fibers, it was possible to determine the feasibility of replacing wool with basalt as a filler in epoxy matrix composites, which are already widely used in applications. Indeed, the basalt composite showed a 35-42% higher Yan's modulus, as well as better compressive strength and bending properties, while the glass material exhibited higher tensile strength [10].

Filterable technical nonwovens  has fulfilled the tasks of expanding the range of technical fabrics using natural local raw materials while preserving all the requirements and characteristics applied to technical fabrics. This, in turn, creates opportunities to enter the global market with new composite technical fabrics [11]. The properties of newly created textiles must meet consumer demands. These requirements are aimed at ensuring that the textiles retain their shape during use, improve hygienic and physical-mechanical properties, and that the nonwoven fabrics produced for the cement plants by the level of consumer expectations [12].

The main properties of sleeve filter fabrics are considered to be air permeability, heat resistance, and strong resistance to high air pressure [13].

RESEARCH RESULTS

The heat resistance of construction materials is indicated by their maximum temperature, and the standard GOST R ISO 11092 2012[16] specifies the requirements for the properties of these materials that enable their use in extreme conditions.

The basalt material is a single-component heating element, made from crushed glass or silicate, and it offers many advantages over similar materials.

The heat resistance of given samples was carried out at the Test Center of the Fire Safety and Emergency Problems Research Institute of the Ministry of Emergency Situations of the Republic of Uzbekistan [17].

Thermal resistance Rct (heat resistance): The temperature difference between the two sides of the material is divided by the unit area along the gradient direction by the exact heat flow. The dry heat flow can consist of one or several conductive, convective, and radiative components.

Thermal resistance Rct, expressed in watts per square meter kelvin, is a textile or composite characteristic indicator that constantly determines the dry heat flow passing through a certain area in response to a stable temperature gradient[14].

The temperature of the measuring device should be Tm=35 °C and the air temperature Ta=20 °C, with a relative humidity of 65%. The air velocity should be Ва=1 m/s. All deviations from these indicators must be within the permissible range.

Thermal conductivity, the resistance of the conductive plate Rct0, is determined by the following formula [15].

Rct0=(Tm-Ta)∙AH-∆Hc.	                                  (1)

Here, Ta- is the air temperature in the Test Chamber, °C; Tm-is the temperature of the measuring device, °C; A-is the area of the measuring device, m²; H-is the heat power supplied to the measuring device installed on the first side of the fabric, Вт; ∆Hc-is the heat power taken from the measuring device installed on the second side of the fabric, Вт.

After placing the test sample on the measuring device, it is necessary to wait until the measured parameters—Tm, Ta, R.H., H—have stabilized. Then, their values are recorded.

Heat resistance is calculated using the following formula:

Rct=(Tm-Ta)∙AH-∆Hc-Rct0, 					(2)

The heat resistance of the cast material Rct is calculated as the average arithmetic value of individual measurements.

Since filter nonwoven fabrics operate in a high-temperature environment, heat resistance is considered their main property.

Figure 1 shows the heat resistance diagram of the samples.

FIGURE 1. Heat resistance diagram of the basalt nonwoven samples

The thermal conductivity of the given samples is higher than samples 1-6. These samples are not recommended for use in nonwoven with its single layer due to their low surface density. The surface density of samples 9-11 is 750-900 g/m2 and the thermal conductivity is 0.029-0.034 m2 K/W and it is recommended to made filter nonwoven products from these samples.

The surface density, air permeability, electrification, tensile strength, and thickness of nonwoven samples were determined by experimental tests at the “Sentexuz” laboratory (Table 1).

TABLE 1. Physical and mechanical properties of nonwoven fabric samples

| Samples Properties |  | Fabric Nonwoven | Nonwoven layer 1 | Nonwoven layer 1,5 | Sample 1 | Sample 2 | 3 Sample 3 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Surface density (10⁻³ g) |  | 198,85 | 266,15 | 290,05 | 770 | 900 | 800 |
| Thickness, mm |  | 0,15 | 0,2 | 0,25 | 1,3 | 1,36 | 1,3 |
| Linear density of nonwoven fabric, tex | warp | 80 | 80 | 80 | 300 | 300 | 300 |
|  | weft | 80 | 80 | 80 | 300 | 300 | 300 |
| Number of threads per 10 cm, pcs | warp | 50 | 50 | 48 | 80 | 80 | 80 |
|  | weft | 50 | 50 | 52 | 160 | 180 | 160 |
| Tensile force, N | Layer 1 | 128 | 600 | 360 | 2370 | 2350 | 2460 |
|  | Layer 1,5 | 260 | 540 | 700 | 4460 | 4300 | 4950 |
| Filling fraction of the nonwoven fabric, % | Layer 1 | 93,271 | 93,240 | 93,240 | - | - | - |
|  | Layer 1,5 | 93,271 | 95,571 | 96,348 | - | - | - |
|  | Total | 99,547 | 99,701 | 99,753 | - | - | - |
| Volumetric filling of the nonwoven fabric, Ev, % |  | 48,546 | 42,447 | 36,373 | - | - | - |
| Air permeability, (cm³/cm²·s) |  | 3,24 | 2,50 | 2,37 | 3,75 | 5,73 | 4,27 |
| Thermal resistance, m²·K/W |  | 0,033 | 0,038 | 0,045 | 0,030 | 0,027 | 0,029 |
| Electrification, (10⁻³ V) |  | 638 | 717 | 158 | 337 | 405 | 382 |

The physical and mechanical properties of the heat-resistant filterable fabrics were determined. The fabric’s surface density was found to be 750–900 g/m², and its thermal resistance 0.029–0.034 m²·K/W. The breaking forces of the fabric in the warp and weft directions were determined to be Fт=2370 H and Fт=4460 H, respectively.

CONCLUSIONS

New prospects have emerged in the use of basalt fiber due to the material's low cost and good mechanical performance, especially at high temperatures. The idea of reinforcing polymer matrices with these fibers has appeared relatively recently and may offer very interesting prospects that have not yet been sufficiently explored. In this work, mechanical tests were conducted on plastic laminates reinforced with comparable E-glass and basalt fibers, with the main aim of evaluating the possibility of replacing glass fibers in many The second was cut with square plates produced using vacuum bag technology. The results obtained in both laminates were compared, showing that the basalt material has higher performance in terms of Young's modulus, compressive and flexural strength, impact strength, and energy. These good properties indicate the potential use of basalt fibers in fields where glass composites are currently widely applied. Short radiation strength tests confirmed the above by showing similar surface adhesion between E-glass and the epoxy matrixThe warp yarn tension (X₁=40 cN), shed height (X₂=130 mm), and middle position value (X₃=60 mm) were identified as alternative factors. The physical and mechanical properties of heat-resistant filter fabrics were determined. The surface density of the fabric was found to be 750–900 g/m², and the thermal conductivity ranged from 0.029 to 0.034 m²·K/W. The breaking forces of the fabric in the warp and weft directions were determined to be Fт=2370 Н and Fт=4460 H, respectively.

REFERENCES

- R. M. Yangiboyev, B. Kh. Boymuratov, and R. Akbarov, “Development and research of flexible fabric electric heaters,” in Problems of Light Industry Development in the Republic of Belarus in the Context of Global Trends, AIP Conference Proceedings 2430, 030006 (2022). https://doi.org/10.1063/5.0077855

- Kompaniya “TEKS,” “Trends in the production of filtration materials,” online resource, available at: https://www.tex-filter.ru/article/tendencii-v-proizvodstve-materialov-dlya-filtracii

- “Fireman Club,” “Flame-resistant fabrics,” online resource (2021), available at: https://fireman.club/statyi-polzovateley/negoryuchaya-tkan

- O. Toshbekov, M. Urozov, S. Yermatov, and M. Khamraeva, “Efficient and economical energy use technology in the processing of domestic coarse wool fiber,” E3S Web of Conferences 461, 01068 (2023). https://doi.org/10.1051/e3sconf/202346101068

- K. Jumaniyozov, M. Urozov, O. Toshbekov, M. Salimova, K. Raximova, and B. Khursandova, “Enhancement of energy-efficient cleaning equipment,” AIP Conference Proceedings 3331, 050007 (2025). https://doi.org/10.1063/5.0307149

- F. Sultonova, O. Toshbekov, M. Urozov, N. Boymurova, Z. Mustanova, and I. Boltaeva, “Enhancing and evaluating the characteristics of specialized workwear for employees in the electric power supply sector,” AIP Conference Proceedings 3331, 050006 (2025). https://doi.org/10.1063/5.0306350

- O. Toshbekov and Z. Mustanova, “Determining the abrasion resistance and high adaptability properties for noise absorption of non-woven fabrics,” Eurasian Journal of Academic Research 3(12–2), 217–221 (2023).

- A. Kurbanov, M. Shomirzaev, S. Tursunov, O. Toshbekov, N. Mukhamadieva, B. Kambarov, and S. Mannobova, “Analysis of the state of cultivation and harvesting of mung bean and agro-biological requirements for threshing and separating its grain,” BIO Web of Conferences 105, 02010 (2024).

- O. Toshbekov, M. Urozov, F. Sultonova, S. Raximqulova, Z. Mustanova, and G. Xulkaliyeva, “Analysis of the thermal conductivity of nonwoven fabrics made from silkworm cocoons and their influence on ambient temperature,” AIP Conference Proceedings 3331, 050005 (2025).

- T. O. Abdullayevich and S. M. A. Qizi, “Types of nonwoven fabrics obtained from coarse fiber and their fields of application,” Eurasian Journal of Academic Research 4(12–2), 12–17 (2024).

- T. O. Abdullayevich and S. M. A. Qizi, “Prospects for the development of technology for producing impermeable nonwoven materials,” Eurasian Journal of Academic Research 4(12–2), 7–11 (2024).

- S. Agarwal, P. Srivastava, S. I. Green, and A. S. Phani, “The influence of microstructure on the tensile properties of a creped tissue paper: Modeling and experiments,” Mechanics of Materials 170, 104505 (2022). https://doi.org/10.1016/j.mechmat.2022.104505

- A. Shaid, L. Wang, and M. Gregory, “Low-cost bench-scale apparatus for measuring the thermal resistance of multilayered textile fabric against radiative and contact heat transfer,” HardwareX 6, e00059 (2019).

- N. Niyozov, B. Khushbokov, G. E. Saidova, and I. Bakhadirov, “Energy efficiency of concrete work technology,” AIP Conference Proceedings, 030025 (2024). https://doi.org/10.1063/5.0218841

- B. Khushbokov, K. Khakimov, J. Kodirov, and F. Khursanov, “Increasing the quality of receiving current through the current receiver by improving the fixator,” AIP Conference Proceedings, 020006 (2024). https://doi.org/10.1063/5.0197788

- A. Rasulov, B. Khushbokov, A. Abdullaev, and A. Tanirbergenov, “Current stabilization based on a magnetic amplifier with an electromagnetic control circuit,” AIP Conference Proceedings 3331, 070020 (2025). https://doi.org/10.1063/5.0306041

- S. F. Amirov, B. Kh. Khushbokov, and N. E. Balgaev, “Multiband current transformers,” Russian Electrical Engineering 80, 119–121 (2009).

- Safarov J., Khujakulov A., Sultanova Sh., Khujakulov U., Sunil Verma. Research on energy efficient kinetics of drying raw material. // E3S Web of Conferences: Rudenko International Conference “Methodological problems in reliability study of large energy systems” (RSES 2020). Vol. 216, 2020. P.1-5.  doi.org/10.1051/e3sconf/202021601093

- Safarov J., Sultanova Sh., Dadayev G.T., Zulponov Sh.U. Influence of the structure of coolant flows on the temperature profile by phases in a water heating dryer. // IOP Conf. Series: Materials Science and Engineering. Dynamics of Technical Systems (DTS 2020). Vol.1029, 2021. №012019. P.1-11. doi:10.1088/1757-899X/1029/1/012019

- Sultanova Sh.A., Artikov A.A., Masharipova Z.A., Abhijit Tarawade, Safarov J.E. Results of experiments conducted in a helio water heating convective drying plant. // International conference AEGIS-2021 «Agricultural Engineering and Green Infrastructure Solutions».  IOP Conf. Series: Earth and Environmental Science 868 (2021) 012045. P.1-6. doi:10.1088/1755-1315/868/1/012045

- Sultanova Sh., Safarov J., Usenov A., Samandarov D., Azimov T. Ultrasonic extraction and determination of flavonoids. XVII International scientific-technical conference “Dynamics of technical systems” (DTS-2021). AIP Conference Proceedings 2507, 050005. 2023. P.1-5. doi.org/10.1063/5.0110524

- Sultanova Sh., Safarov J., Usenov A., Raxmanova T. Definitions of useful energy and temperature at the outlet of solar collectors. // E3S Web of Conferences: Rudenko International Conference “Methodological problems in reliability study of large energy systems” (RSES 2020). Vol. 216, 2020. P.1-5.  doi.org/10.1051/e3sconf/202021601094

- Usenov A.B., Sultanova Sh.A., Safarov J.E., Azimov A.T. Experimental-statistic modelling of temperature dependence of solubility in the extraction of ocimum basilicum plants. // International conference AEGIS-2021 «Agricultural Engineering and Green Infrastructure Solutions». IOP Conf. Series: Earth and Environmental Science 868 (2021) 012047. P.1-5. doi:10.1088/1755-1315/868/1/012047

- Baratov, B.N., Umarov, F.Y., Toshov, Z.H. Tricone drill bit performance evaluation. Gornyi Zhurnal, Moscow, 2021. - № 12. - PP. 60-63. DOI:10.17580/gzh.2021.12.11.

- Toshov, J.B., Toshov, B.R., Baratov, B.N., Haqberdiyev, A.L. Designing new generation drill bits with optimal axial eccentricity | Вопросы проектирования буровых долот нового поколения с оптимальным межосевым эксцентриситетом // Mining Informational and Analytical Bulletin, 2022, (9). - PP. 133–142. DOI: 10.25018/0236_1493_2022_9_0_133

- Toshov J., Makhmudov A., Kurbonov O., Arzikulov G., Makhmudova G. Development and Substantiation of Energy-Saving Methods for Controlling the Modes of Operation of Centrifugal Pumping Units in Complicated Operating Conditions. Proceedings of the 11th International Conference on Applied Innovations in IT, (ICAIIT), November 2023, Koethen, Germany. – РР. 161-165.

- J.B. Toshov, K.T. Sherov, B.N. Absadykov, R.U. Djuraev, M.R. Sikhimbayev, Efficiency of drilling wells with air purge based on the use of a vortex tube. NEWS of the National Academy of Sciences of the Republic of Kazakhstan “Series of geology and technical sciences”. – Almaty, Volume 4, Number 460 (2023), 225–235. https://doi.org/10.32014/2023.2518-170X.331 
Toshov J., Toshov B., Bainazov U., Elemonov M. Application of Cycle-Flow Technology in Coal Mines. Proceedings of the 11th International Conference on Applied Innovations in IT, (ICAIIT), March 2023, Koethen, Germany. – РР. 279-284.

- Usmanov, E., Kholikhmatov, B., Rikhsitillaev, B., Nimatov, K. Device for reducing asymmetry // E3s Web of Conferences 461. 2023. PP, 01052, 1-5. https://doi.org/10.1051/e3sconf/202346101052

- Toshov B., Toshov J., Akhmedova L., Baratov B. The new design scheme of drilling rock cutting tools, working in rotation mode pairs. E3S Web of Conferences 383, 04069 (2023) TT21C-2023 https://doi.org/10.1051/e3sconf/202338304069

- J.B. Toshev, M.B. Norkulov, A.A. Urazimbetova and L.G. Toshniyozov. Optimization of scheme of placing cutting structures on the cone drill bit. E3S Web of Conf., Volume 402, 10039 (2023), International Scientific Siberian Transport Forum - TransSiberia 2023, https://doi.org/10.1051/e3sconf/202340210039

- Toshov J., Baratov B., Sherov K., Mussayev M., Baymirzaev B., Esirkepov A., Ismailov G., Abdugaliyeva G., Burieva J. Ways to Optimize the Kinetic Parameters of Tricone Drill Bits. Material and Mechanical Engineering Technology, №1, 2024, 35-45. https://doi.org/10.52209/2706-977X_2024_1_35

- K.T. Sherov, N.Zh. Karsakova, B.N. Absadykov, J.B. Toshov, M.R. Sikhimbayev, Studying the effect of the boring bar amplitude-frequency characteristics on the accuracy of machining a large-sized part. NEWS of the National Academy of Sciences of the Republic of Kazakhstan “SERIES OF GEOLOGY AND TECHNICAL SCIENCES”. – Almaty, Volume 2, Number 464 (2024), 217–227. https://doi.org/10.32014/2024.2518-170X.405

- Akbar, K., Javokhir, T., Lazizjon, A., Umidjon, K., Muhammad, I., Improvement of soft-start method for high-voltage and high-power asynchronous electric drives of pumping plants. AIP Conf. Proc. 3152, 040006 (2024) / III International Scientific and Technical Conference “Actual issues of Power supply systems” (ICAIPSS2023), 7–8 September 2023, Tashkent, Uzbekistan. https://doi.org/10.1063/5.0218899

- J. Toshov, L. Atakulov, G. Arzikulov, U. Baynazov, Modeling of optimal operating conditions of cyclic-flow technologies with a belt conveyor at coal mine under the "ANSYS" program. AIP Conf. Proc. 3152, 020006 (2024) / III International Scientific and Technical Conference “Actual issues of Power supply systems” (ICAIPSS2023), 7–8 September 2023, Tashkent, Uzbekistan. https://doi.org/10.1063/5.0218904

- Kholikhmatov B.B., Samiev Sh.S., Erejepov M.T., Nematov L.A. Modelling of laboratory work in the science "Fundamentals of power supply" using an educational simulator based on a programmed logic controller // E3S Web of Conferences 384. 2023. РР, 01032, 1-3. https://doi.org/10.1051/e3sconf/202338401032

- Rakhimov F, Rakhimov F, Samiev Sh, Abdukhalilov D. Justification of Technical and Economic Effectiveness of Application of 20 kV Voltage in Overhead Electric Networks //AIP Conf. Proc. 3152, 030023 (2024). https://doi.org/10.1063/5.0218921

- Taslimov A, Mo'minov V, Samiev Sh, Abdukhalilov D. Issues of Optimization of Electrical Network Parameters Medium Voltage //AIP Conf. Proc. 3331, 020007 (2025). https://doi.org/10.1063/5.0305781

- Toshbekov, O., Urazov, M., Yermatov, S., & Khamraeva, M. 2023). Yeffisient and yesonomisal yenergy use teshnology in the prosessing of domestis soarse wool fiber. In Ye3S Web of Sonferenses (Vol. 461, p. 01068). https://doi.org/10.1051/e3sconf/202346101068

- Jumaniyozov, K., Urozov, M., Toshbekov, O., Salimova, M., Raximova, K., & Khursandova, B. (2025, November). Enhancement of energy-efficient cleaning equipment. In American Institute of Physics Conference Series (Vol. 3331, No. 1, p. 050007). https://doi.org/10.1063/5.0307149

- Sultonova, F., Toshbekov, O., Urozov, M., Boymurova, N., Mustanova, Z., & Boltaeva, I. (2025, November). Enhancing and evaluating the characteristics of specialized workwear for employees in the electric power supply sector. In American Institute of Physics Conference Series (Vol. 3331, No. 1, p. 050006).  https://doi.org/10.1063/5.0306350