Study of Structural, Electrical, Mechanical, and Thermal properties of perovskites XScH3 (X= Li, Na, K, Rb and Cs) for hydrogen storage applications using DFT

Rachid OUALAID1, a) , Youssef El bid1,b), Najib El Biaze1, 2, c), Rachid Markazi1, d), Khadija El moudenib3, e) , Mohamed Bouzelmad4, f) and Abdeljabar Aboulkassim5, g)

1 Energies and Sustainable Development Research Team (E2D), Higher School of Technology Guelmim, Ibnou Zohr University, 81000, Morocco.

2Materials and Renewable Energy Laboratory, Ibnou Zohr University, Agadir, 80000, Morocco.

3 Laboratory of engineering sciences for energy (LabSIPE), National School of Applied Sciences Chouaïb Doukkali University, El Jadida, Morocco.

4 Laboratory of Physics, Energy and Information Processing (Lab. PETI) Polydisciplinary Faculty of Ouarzazate, Ibnou Zohr University, 45000, Morocco.

5 Materials, Signals, Systems and Physical Modeling Laboratory, Faculty of Sciences, Ibnou Zohr University, Agadir, Morocco.

Author Emails
a) Corresponding author: rachid.oulaid@edu.uiz.ac.ma
b) youssef.elbid@edu.uiz.ac.ma

c) n.elbiaze@uiz.ac.ma
d) r.markazi@uiz.ac.ma
e) el-moudenib.k@ucd.ac.ma
f) mohamed.bouzelmad@edu.uiz.ac.ma
g) abdeljabar.aboulkassim@edu.uiz.ac.ma

Abstract- In this work, we explore new hydrogen storage materials namely XScH3(where X= Li, Na, K, Rb and Cs), using a first-principles calculations. We investigate their structural, mechanical, electronic and thermal properties within the framework of the Generalized Gradient Approximation (PBE-GGA), where the Perdew-Burke-Ernzerhof is employed to describe the exchange-correlation potential. All five hydrides exhibit both thermodynamic and mechanical stability. Their lattice parameters increase with the atomic size of X from 3.865 Å for LiScH3 to 4.334 Å for CsScH3. Accordingly, the hydrogen storage capacity ranges from 5.50% to 1.67%, whereas hydrogen desorption temperatures range from 229.61 K to 245.71 K. Due to all these physical properties, especially their metallic behavior, XScH3( where X= Li, Na, Rb, and Cs) are promising candidates for hydrogen storage technologies.

Keywords: XScH3; DFT; gravimetric capacity; desorption temperature; electronic properties.

# Introduction

Hydrogen storage represents a crucial area of research for the development of clean, sustainable technologies to meet the fluctuating energy demands of renewable sources such as solar and wind power [1]. Advanced research is actually focusing on new safe and efficient materials for solid-state hydrogen storage [2]. Recent works focused mainly on the study of perovskite hydrides which belong to transition metals. Rafique et al.[3] studied the physical properties of XCoH3 (where X= Mn, Sr, Cd, In and Sn) and accordingly proved their metallic behavior, with hydrogen gravimetric ratios of (2.59 wt.%), (2.03 wt.%), (1.74 wt.%), (1.71 wt.%) and (1.68 Cwt.% ) for MnCoH3, SrCoH3, CdCoH3, InCoH3 and SnCoH3, respectively. R. Song et al. [4]  computed the gravimetric ratios of XPtH3 (where X= Li, Na, K and Rb) perovskites hydrides. They found that their values are (1.45 wt.%), (1.35 wt.%), (1.26 wt.%) and (1.06 wt.%) for LiPtH3, NaPtH3, KPtH3 and RbPtH3, respectively and that the desorption temperatures (Td) of these compounds are (237.77 K), (225.39 K), (162.43 K) and (80.11 K), respectively. Z. Abbas et al.[5] proved the metallic nature for BeMgH3 and CaMgH3 and their highly significant gravimetric hydrogen densities of 8.32 and 4.49 wt.%, respectively. Therefore, these compounds are potential candidates for hydrogen storage.

In the present work, we investigate perovskite hydrides XScH3 (where X= Li, Na, K, Rb and Cs). According to our results, these materials are promising candidates for hydrogen storage applications.

# Computational Methodology

We apply first-principles calculations based on (DFT) and full potential linearized augmented plane wave (FP-LAPW) as implemented in the WIEN2k simulation code [6]. In order to describe the exchange-correlation effects accurately, we use the generalized gradient approximation (GGA) in conjunction with the Perdew-Burke-Ernzerhof (PBE) functional [7]. Structural optimization was performed to determine the equilibrium lattice constants (a0) by applying the Birch-Murnaghan equation of state. The self-consistent field cycle was iterated until the total energy convergence criterion of 10-4 Ry was achieved. The parameters for the cutoff wave (Ecut) were IMAX = 10, RMT*KMAX = 7, -7.00 Ry ,1000 k-points, -6.0 Ry and which were found to be optimal for these calculations.

# Results and discussion

  - Structural properties

Using VESTA software [8], we visualized the three dimensional crystal structures of XScH3. These perovskite hydrides crystallize in the cubic space group Fm-3m (No.221). As shown in FIGURE.1, the (X) atoms are located at coordinates (0, 0, 0), while the scandium (Sc) atoms occupy the center of the cubic unit cell at (0.5, 0.5, 0.5), whereas the hydrogen (H) atoms are situated at the face-centered positions of the unit cell: (0.5, 0.5, 0), (0.5, 0, 0.5) and (0, 0.5, 0.5).

FIGURE 1. Cubic structure of perovskite hydrides XScH3.

In this study, we examine the stability criteria for perovskite materials, with a focus on XScH3 perovskite hydrides. Two straightforward methods are utilized to assess the structural integrity of the crystal lattice, namely the octahedral factor (τ) and the tolerance factor (t). To guarantee stability and high symmetry, the perovskite structure must fall within the ranges of 0.442-0.895 for (τ) and 0.813-1.107 for (t). These parameters can be determined using the following equations:

|  | t=rX+rH2rSc+RH and τ=rScrH | (1) |
| --- | --- | --- |

Here, rSc , rX and rH denote the ionic radii of scandium, the X-site cation and hydrogen, respectively. According to FIGURE.2, both LiScH3 and NaScH3 exhibit lower stability due to their smaller tolerance (t) and octahedral (τ) factors, which generate distortions in the perovskite structure and consequently affect its stability. On the other hand, KScH3 , RbScH3 and CsScH3 . The (τ) values increase until reaching 1 and enhance consequently their octahedral stability. Among the XScH3 perovskite hydrides, CsScH3 is the most structurally stable.

FIGURE 2. Tolerance factor (t) and the octahedral factor (τ) of XScH3 .

Using the WIEN2k software, we obtained the optimized energy-volume curves for XScH3 (where X= Li, Na, K, Rb and Cs) by applying the Birch-Murnaghan equation. To study the structural stability of these hydrides, we compute the total energy for each of them. Our results are presented in FIGURE.3. Their optimized lattice constants (a₀) and the corresponding unit cell volumes are summarized in Table 1. The Birch-Murnaghan equation is given by [9]:

|  | EV= E0V+B0VB'(B'-1)B1-V0V +V0V B'-1 | (2) |
| --- | --- | --- |

In equation (2), E0 , V0 and B'denote the ground-state energy, the equilibrium volume and the pressure derivative of the bulk modulus, respectively.

FIGURE 3. Optimization curves of XScH3 perovskites hydrides.

  - Hydrogen storage properties

The formation energy (ΔHf) can be determined using equation (3) [10]:

|  | ΔHf =E(XScH3-(EX+E(Sc)+3 E(H))N | (3) |
| --- | --- | --- |

In equation (3), EX,ESc, E(H) denote the ground state energy of one atom of  X, Sc, H, respectively, whereas EXScH3  is the total energy of each material and N represents its total number of atoms. FIGURE.4 illustrates its energy formation (ΔHf) . All compounds have negative formation energies, consequently they are thermodynamically stable confirming that their formation processes are exothermic. The formation energy (ΔHf) values, in stability order, are : CsScH3 (-2.49 eV/atom) > RbScH3 (-2.45 eV/atom) > KScH3 (-2.43 eV/atom) > NaScH3 (-2.35 eV/atom) > LiScH3 (-2.33 eV/atom).

FIGURE 4 Formation enthalpy ΔHf (eV/atom). 			FIGURE 5 Gravimetric ratio Cw%.

  - Gravimetric ratio Cw%:

In order to evaluate the hydrogen storage capacity (Cwt%) of materials, we compute their gravimetric ratio given by the following expression [11] :

| Cwt%=HMmHmHost+HMmH×100% | (4) |
| --- | --- |

In equation (4), mH denotes Hydrogen's molar mass and mHost stands for the total molar mass of the compound, whereas HM represent hydrogen atoms to the overall atomic count within each compound. In FIGURE 5, we compare the calculated (Cwt%) values of the gravimetric ratios of each perovskite hydride. Their computed values are: (5.506%) for LiScH3, (4.260%) for NaScH3, (3.472%) for KScH3,(2,266 %) for RbScH3 and (1,671%) for CsScH3.

  - Volumetric hydrogen storage capacity

In order to evaluate the storage capacity of materials, we compute its volumetric storage capacity (ρ) defined by:

| ρ=NH.mHVL.NA | (5) |
| --- | --- |

where NH, mH and V denote the number of hydrogen atoms per formula unit, the hydrogen molecular mass and the volume in liters, respectively, whereas NA represents Avogadro's number. The values of ρ (g. H2/L) of the studied perovskite hydrides , presented in Table 1 and FIGURE 6, are: (86,960 g.H2 /L) for LiScH3, (80,381 g.H2 /L) for NaScH3, (70,886 g.H2 /L) for KScH3,(66,549 g.H2 /L) for RbScH3 and (61,641g.H2 /L) for CsScH3.

Table 1. Volumetric hydrogen storage capacity ρ (g.H2 /L), desorption temperature Td and gravimetric ratio Cw%.

| Compounds | a0 (A°) | V (A°)3 | ρ(g.H2 /L) | Cw% | Td(K°) |
| --- | --- | --- | --- | --- | --- |
| LiScH3 | 3.8652 | 57.7452 | 86.960 | 5.506 | 229.61 |
| NaScH3 | 3.967 | 62.471 | 80.381 | 4.260 | 231.52 |
| KScH3 | 4.137 | 70.839 | 70.886 | 3.472 | 240.05 |
| RbScH3 | 4.225 | 75.456 | 66.549 | 2.266 | 241.95 |
| CsScH3 | 4.334 | 81.464 | 61.641 | 1.671 | 245 .71 |

  - Hydrogen desorption temperature Td

In order to estimate the values of hydrogen desorption temperature (Td) of XScH3, we compute the formation enthalpies of the hydrogen release reaction namely:

|  | X+Sc+32.H2→XScH3 | (6) |
| --- | --- | --- |

Then, we evaluate the desorption temperature Td using the following formula for Gibbs free energy:

|  | ΔG=ΔH-Td ⋅ΔS | (7) |
| --- | --- | --- |

At normal pressures and temperatures (ΔG=0), the desorption temperature  (Td ) is given by:

|  | Td=-ΔHΔS | (8) |
| --- | --- | --- |

Where ΔS denotes the entropy change of hydrogen and (ΔH) stands for the reaction enthalpy for the studied material. The value of ΔS is 130.7 J/mol.K  [12], whereas the computed values of (Td) for each perovskite hydrides, presented in Table.1 and FIGURE.7, are: (229,61 K) for LiScH3, (231,52 K) for NaScH3, (240,05 K) for KScH3, (241,95 K) for RbScH3 and (245,71 K) for CsScH3. These values are due to the presence of an alkali metal (X) in the XScH3 unit cell and is responsible for its thermal stability and its hydrogen release kinetics.

FIGURE 6 Volumetric hydrogen storage capacity ρ (g.H2 /L).		FIGURE 7 Desorption temperature Td

  - Electronic Properties

In this section, we investigate the bands structures at the equilibrium lattice constant (a0) of hydrogen storage materials XScH3 by analyzing their electronic properties. In this regard, we use the GGA-PBE method along the high-symmetry points in the first Brillion zone. Our results are presented in FIGURE.8, where (EF) denotes the Fermi level corresponding to the band gap energy (Eg), which is the necessary amount of energy for electrons to move from the conduction band to the valence one. According to the diagrams in (FIGURE.8), these materials have no band gap energy (Eg ≈ 0 eV) proved therefore their metallic nature.

FIGURE.8 Electronic band structures of XScH3 (where X= Li, Na, K, Rb and Cs).

  - Elastic properties

The elastic constants Cij of XScH3 (where X= Li, Na, K, Rb and Cs) perovskite hydrides were computed using the CASTEP software[13]. Their values are presented in Table 2. In order to evaluate their elastic stability, we apply the Born stability criteria [14] given in equation (9):

|  | C11-C12 >0 ; C11 >0 ; C44 >0 ; C11+2C12 >0 | (9) |
| --- | --- | --- |

Accordingly, the Cauchy's pressure CP is the following:

|  | CP=C12-C44 | (10) |
| --- | --- | --- |

The Shear modulus (G), determined using the Voigt, Reuss, and Hill approximation, is given by equation (11):

|  | G=GV+GR2 where Gv=C11-C12+3C445GR=C11-C125C444C44+3C11-C12 | (11) |
| --- | --- | --- |

The Bulk modulus (B) is calculated by the following formula:

|  | B=C11+2C123 | (12) |
| --- | --- | --- |

In order to determine whether these compounds have brittle or ductile behavior, we use the following criteria for Pugh’s ratio (B/G):

|  | BG<1.75 for brittle behaviorBG>1.75 for ductile behavior | (13) |
| --- | --- | --- |

To guarantee the mechanical stability of these materials, the Bulk modulus must also satisfy the condition C12 < B <C11.

Finally, the other mechanical parameters namely: Young's modulus (E), Poisson's ratio (v), Anisotropy factor (A), Hardness (H) and Machinability index (μM) are respectively given by the following equations:

|  | E=9GB3B+G | (14) |
| --- | --- | --- |
|  | A=2C44C11-C12 With A≠1 for anisotropic behaviorA=1 for isotropic behavior | (15) |
|  | v=3B-2G2(3B+G) with v<0.26 for brittle behavior v>0.26 for ductile behavior | (16) |
|  | H=E(1-2V)6(1+V) | (17) |
|  | μM=BC44 | (18) |

The elastic properties of XScH3 reveal distinct mechanical behaviors. The compressibility modulus indicates comparable resistance to volume deformation across all compounds. Shear modulus (G) varies, with NaScH3 and RbScH3 exhibiting higher resistance to shear forces. Universal brittleness is evidenced by B/G ratios less than 1.75 (FIGURE.9). Poisson's ratio trends (FIGURE.10) show greater ductility in LiScH3 and NaScH3, enabling consequently higher transverse deformation under load. This ratio decreases systematically with increasing alkali metal atomic number (Na to Cs) which induces rising brittleness. Young's modulus confirms that both of LiScH3 and NaScH3 possess superior stiffness. All compounds exhibit elastic anisotropy (A ≠ 1). Hardness (H) is generally moderate, where KScH3 reflects the highest resistance to permanent deformation. Machinability (μM) is correlated with stiffness: LiScH3 and NaScH3 are more machined, whereas RbScH3 and CsScH3 are less machined due to their low mechanical performance.

Table 2. Elastic properties of XScH3.

|  | C11(GPa) | C12(GPa) | C44(GPa) | B(GPa) | G(GPa) | B/G | GV | GR | E(GPa) | ν | CP (GPa) |  | μM | H | A |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| LiScH3 | 99.81 | 19.88 | 19.04 | 46.52 | 27.41 | 1.69 | 27.41 | 24.09 | 68.74 | 0.25 |  | 0.83 | 2.44 | 5.25 | 0.68 |
| NaScH3 | 95.24 | 25.49 | 25.43 | 48.74 | 29.21 | 1.66 | 29.21 | 28.52 | 73.04 | 0.25 |  | 0.05 | 1.91 | 5.60 | 0.12 |
| KScH3 | 75.40 | 21.08 | 28.60 | 39.18 | 28.02 | 1.39 | 28.02 | 28.00 | 67.89 | 0.21 |  | -7.52 | 1.36 | 6.65 | 0.003 |
| RbScH3 | 69.91 | 19.44 | 30.34 | 36.26 | 28.29 | 1.28 | 28.29 | 28.06 | 67.37 | 0.19 |  | -10.89 | 1.19 | 7.39 | 0.040 |
| CsScH3 | 60.39 | 19.42 | 28.69 | 33.07 | 25.41 | 1.30 | 25.41 | 24.72 | 60.68 | 0.19 |  | -9.27 | 1.15 | 6.73 | 0.13 |

FIGURE. 9 Cauchy’s pressure Cp and Pugh’s ratio B/G . 	FIGURE. 10 Poisson’s ratio (v).

  - Thermal Properties

In order to investigate the thermal properties of XScH3 perovskites hydrides, we determine Debye temperature (θD), melting temperature (Tm), transverse (vt), longitudinal (vl) and average (vm) velocities.

Debye temperature (θD) can be evaluated using the following formula:

|  | θD=hk3n4πNAρM1/3×vm | (19) |
| --- | --- | --- |

In equation (19), M, n, ρ, kB, NA and h are respectively: the molecular weight, the number of atoms in the molecule, the density, Boltzmann's constant, the Planck's constant and Avogadro’s number. Additionally, (𝑣𝑚) can be evaluated through the following relation [15]:

|  | vm=132vt3+1vl3-1/3 | (20) |
| --- | --- | --- |

To evaluate (vt) and (vl), we employ the following relations:

|  | vt=Gρ and vl=3 B+4G3ρ | (21) |
| --- | --- | --- |

The melting point (Tm) can be calculated using the following equation [16]:

|  | Tm K=553 K+5.911C12GPa±300 K | (22) |
| --- | --- | --- |

The calculated acoustic properties of the XScH3 materials are presented in Table 3, where: (vt) stands for the transverse wave velocity. It depends on shear rigidity and is the highest for NaScH3 (5405 m/s) and the lowest for CsScH3 (5041 m/s). (vl) denotes longitudinal wave velocity reflecting compressive resistance. Its peaks are: (7242 m/s) for LiScH3 and (4271 m/s) for CsScH3 (FIGURE.11). The average sound velocity (vm) ranges from 2873 m/s (CsScH3) to 4424 m/s (LiScH3), signifying overall elastic stiffness. Debye temperature (θD), which depends on the phonon spectra and material stiffness, varies from 337 K (CsScH3) to 583 K (LiScH3) (FIGURE.12). The melting temperature (Tₘ) measures the thermal stability. It is the highest for NaScH3 (704 K) and the lowest for CsScH3 (668 K). KScH3 material exhibits intermediate values of these thermal parameters. Both LiScH3and NaScH3 demonstrate superior mechanical rigidity and higher Debye temperatures, while RbScH3 and CsScH3 materials have lower values of them. According to its melting temperature (Tₘ), NaScH3 material possesses the highest thermal stability. All these systematic variations emphasize the significant influence of the X-site cation size on the thermal and mechanical features of our studied XScH3 perovskites hydrides.

Table 3. Thermal properties of XScH3

| Compounds | ρ (g/cm3) | vt (m/s) | vl(m/s) | vm(m/s) | θD(K) | Tm(K) |
| --- | --- | --- | --- | --- | --- | --- |
| LiScH3 | 1.584 | 5236.029 | 7242.318 | 4424.146 | 583.420 | 670.528 ± 300 |
| NaScH3 | 1.890 | 5404.997 | 6811.715 | 4329.733 | 555.851 | 703.683 ± 300 |
| KScH3 | 2.037 | 5294.053 | 6130.528 | 4097.799 | 503.854 | 677.615 ± 300 |
| RbScH3 | 2.971 | 5319.680 | 4990.768 | 3413.016 | 411.212 | 667.933 ± 300 |
| CsScH3 | 3.671 | 5040.833 | 4270.766 | 2872.890 | 337.152 | 667.791 ± 300 |

FIGURE 11. Representation of (vl), (vm) and (vt) velocities.	 FIGURE 12. Representation of (Tm) and (θD) temperatures.

# Conclusion

In this work, we investigated the properties of the perovskite hydrides XScH3 (where X= Li, Na, K, Rb and Cs) using the DFT approach based on Win2k software. Our calculations prove that these materials can be used in hydrogen storage technologies. In this context, we found the following results: the gravimetric capacities (Cwt%) are 5.50%, 4.26%, 3.47%, 2.26% and 1.67% for LiScH3, NaScH3, KScH3, RbScH3 and CsScH3, respectively. Additionally, according to the results of our geometry optimization applied on them, we showed that all these materials are structurally stable, with lattice constants (a0) of 3.865 Å, 3.967Å, 4.137Å, 4.225Å and 4.334Å for  LiScH3, NaScH3, KScH3, RbScH3 and CsScH3, respectively. Finally, our study of the electronic, mechanical and thermal properties shows that all these perovskite hydrides have metallic behavior, mechanically and thermally stable.

# Acknowledgments

We are deeply grateful to Professors Rachid Markazi and Najib El Biaze for their valuable assistance and kindly support during the preparation of this paper.

# References

- E. Kabalci, « Design and analysis of a hybrid renewable energy plant with solar and wind power », Energy Conversion and Management, vol. 72, p. 51‑59, août 2013,doi: 10.1016/j.enconman.2012.08.027 .

- A. Züttel, « Materials for hydrogen storage », Materials Today, vol. 6, no 9, p. 24‑33, sept. 2003, doi: 10.1016/S1369-7021(03)00922-2.

- A. Rafique, M. Usman, J. U. Rehman, A. Nazeer, H. Ullah, et A. Hussain, « Investigation of structural, electronic, mechanical, optical and hydrogen storage properties of cobalt-based hydride-perovskites XCoH3 (X = In, Mn, Sr, Sn, Cd) for hydrogen storage application », Journal of Physics and Chemistry of Solids, vol. 181, p. 111559, oct. 2023, doi: 10.1016/j.jpcs.2023.111559.

- R. Song, Y. Chen, S. Chen, N. Xu, et W. Zhang, « First-principles to explore the hydrogen storage properties of XPtH3 (X=Li, Na, K, Rb) perovskite type hydrides », International Journal of Hydrogen Energy, vol. 57, p. 949‑957, févr. 2024, doi: 10.1016/j.ijhydene.2024.01.116.

- Z. Abbas, Z. Zafar, H. H. Raza, A. Parveen, et S. F. Shaikh, « Density-functional quantum analysis of optoelectronic, elastic, thermodynamic and hydrogen storage properties of AMgH3 (A= be, ca) perovskite-type hydrides: Prospects for clean energy hydrogen-storage fuel and optoelectronic applications », International Journal of Hydrogen Energy, vol. 60, p. 212‑228, mars 2024, doi: 10.1016/j.ijhydene.2024.02.081.

- P. Blaha, K. Schwarz, G. Madsen, D. Kvasnicka, et J. Luitz, « WIEN2k: An Augmented Plane Wave plus Local Orbitals Program for Calculating Crystal Properties », Technische Universität Wien, Wien, vol. 28, janv. 2001.

- J. P. Perdew, K. Burke, et M. Ernzerhof, « Generalized Gradient Approximation Made Simple », Phys. Rev. Lett., vol. 77, no 18, p. 3865‑3868, oct. 1996, doi: 10.1103/PhysRevLett.77.3865.

- K. Momma et F. Izumi, « VESTA 3 for three-dimensional visualization of crystal, volumetric and morphology data », J Appl Cryst, vol. 44, no 6, p. 1272‑1276, déc. 2011, doi: 10.1107/S0021889811038970.

- R. Oualaid et al., « Study of mechanical, optical, electrical and structural properties of magnesium-based double perovskites Mg2XH6 (X= V, Cr) for hydrogen storage applications using DFT », Solid State Communications, vol. 404, p. 116102, oct. 2025, doi: 10.1016/j.ssc.2025.116102.

- N. Xu et al., « First-principles investigations for the hydrogen storage properties of XVH3 (X=Na, K, Rb, Cs) perovskite type hydrides », Journal of Materials Research and Technology, vol. 26, p. 4825‑4834, sept. 2023, doi: 10.1016/j.jmrt.2023.08.218.

- G. Surucu, A. Gencer, A. Candan, H. H. Gullu, et M. Isik, « CaXH3 (X = Mn, Fe, Co) perovskite-type hydrides for hydrogen storage applications », International Journal of Energy Research, vol. 44, no 3, p. 2345‑2354, 2020, doi: 10.1002/er.5062.

- N. Xu, Y. Chen, S. Chen, S. Li, et W. Zhang, « First-principles investigation for the hydrogen storage properties of XTiH3 (X=K, Rb, Cs) perovskite type hydrides », International Journal of Hydrogen Energy, vol. 50, p. 114‑122, janv. 2024, doi: 10.1016/j.ijhydene.2023.06.254.

- S. J. Clark et al., « First principles methods using CASTEP », Zeitschrift für Kristallographie - Crystalline Materials, vol. 220, no 5‑6, p. 567‑570, mai 2005, doi: 10.1524/zkri.220.5.567.65075.

- B. Ahmed, M. B. Tahir, A. Ali, et M. Sagir, « DFT insights on structural, electronic, optical and mechanical properties of double perovskites X2FeH6 (X = Ca and Sr) for hydrogen-storage applications », International Journal of Hydrogen Energy, vol. 50, p. 316‑323, janv. 2024, doi: 10.1016/j.ijhydene.2023.10.237.

- H. Li et al., « First-principles study of mechanical and thermodynamic properties of Ti-Ga intermetallic compounds », Journal of Alloys and Compounds, vol. 700, p. 208‑214, avr. 2017, doi: 10.1016/j.jallcom.2017.01.052.

- S. A. Dar, V. Srivastava, U. K. Sakalle, A. Rashid, et G. Pagare, « First-principles investigation on electronic structure, magnetic, mechanical and thermodynamic properties of SrPuO3 perovskite oxide », Mater. Res. Express, vol. 5, no 2, p. 026106, févr. 2018, doi: 10.1088/2053-1591/aaabcd.