Effect of the Density of Raw Gin on the Changes in the Amount of Short Fibers

Nodir Navruzov1, а), Kamoliddin Yakubov1, b), Erkin Berdanov1, c)
Khanimkul Pardayev1, d) and Sherkul Khakimov1, e)

Tashkent Institute of Textile and Light Industry, 5 Shohjahon street, Tashkent, 100100, Uzbekistan

a) Corresponding author: nnavruzov86@gmail.com
b) yakubov19kamol91@gmail.com
c) berdanoverkin1985@gmail.com
d) hanimkul@bk.ru
c) lionandlion9@mail.ru

Abstract. This article examines the effect of raw gin roll density on the short fiber content of cotton fiber. The relevance of the work lies in the fact that spinning plants often receive cotton fiber with a high content of short fibers (less than 0.5 inches or 12.7 mm), which negatively affects the production of high-quality yarn and leads to an increase in spinning waste. An increased proportion of short fibers reduces yarn strength, deteriorates its texture, and causes significant economic losses, making this issue critical for the textile industry. The study involved experimental work on 4DP-130 gin equipment using first-grade raw cotton. The influence of raw roll density and seed comb position on the variation in the amount of short fibers was analyzed. Additionally, the dependency of short fiber content on the rotation speed of gin machine working parts and the force and uniformity of fiber handling was investigated. The results demonstrated that optimizing these parameters not only reduces the proportion of short fibers but also improves fiber consistency within the batch. Based on the experiments, recommendations were provided for optimizing ginning parameters. Specifically, adjustments to raw roll density, the angle of the seed comb, and the dynamic tuning of the working parts' speed were suggested. These measures reduce the short fiber content in cotton fiber by 15–20%, ensuring quality preservation, increased processing productivity, and minimized waste. This study emphasizes the critical role of precise tuning of technological parameters to enhance sustainability and efficiency in textile production.

Keywords: standard, cotton fiber, short fiber, raw roll density, fiber defects, seed comb, HVI system.

INTRODUCTION

Life insistently puts forward demands to improve the quality of fabrics and reduce their cost. If the textile industry is required to give the best fabric in the world, then the cotton gin industry must also be required to give the best fiber in the world, in which the cotton coming into processing at the spinning mill is always more or less clogged with large and small impurities of organic and inorganic origin. These impurities contain particles of leaves of boxes and stems, sand, dust, etc. In addition to cotton, there are so-called defects or defects of natural origin, dead or immature fiber, diseased fiber, gining defects caused by the nature of raw cotton: nodules, lumps or immature seed, mature seed and its particles, skin with fiber and fluff, and finally, defects formed during gining: curls, flagella, combined defects and short fibers. In recent years, the main objections from spinning enterprises are the unevenness of the fiber, that is, the high content of short hairs in the fiber, which negatively affects the production of high-quality yarn. Short fibers are fibers less than 0.5 inches (12.7 mm) long. It is known that fibers of this length break up into waste when preparing the fiber for the spinning process, as a result of which the amount of waste becomes larger than usua [1, 2, 3, 4, 5, 6].

The increase in the number of defective impurities and short fibers is explained by the fact that there is no compliance with the required regulations when preparing raw cotton for the gining process, as well as the high density of the raw gin roller. One of the reasons for the high density of the raw gin roller is the difficulty of getting the gin seeds out of the working chamber of the gin.

G.I. Miroshnichenko [7] points out that when gining, the output of seeds from the working chamber lags behind the process of releasing them from the fiber. About 90% of the fibers will already be removed within a minute of gining, and the seeds released from the working chamber are only 26-27%, and 60% of the fully gined seeds are in the raw roller. The fact that the fully gined seed remains in the working chamber for a long time and is encountered several times by the teeth of the saw. As a result, the short fibers on the surface of the seeds are scraped off by the saw and mixed into the fiber composition.

In his works, N.G. Gulidov [8] came to the conclusion that the trajectory of the flight of the seed on the surface of the grate depends on the pulse created by the saws.

The results of R.Sulaimonov's research claim that the separation of gined seeds into the interstitial spaces in the zone of the seed comb does not occur from the impulse of forces created by the saws, but from the magnitude of their distance from the inner periphery of the apron and from the degree of their adhesion to the fibrous roller, which determines the speed of loss of connection of the fly with the raw roller [9].

S. Fazldinov in his work came to the conclusion that it is difficult to isolate seeds from the gin working chamber, which leads to an excessive delay in the stay of seeds in the working chamber, their overgrowth, i.e. clogging of the fiber with lint with a decrease in fiber length, and to an increase in fiber porosity and seed damage due to excessive growth of the density of the raw roller [10].

Hadzhinova M.A. found that with an increase in the density of the raw roller, the damage to the fiber increases significantly (with a weak roller, the damage to the fiber is 9%, with a dense one more than 25%) [11].

It is known from earlier studies by B.A. Levkovich that the productivity of gin and porosity depend on the speed of rotation of the mass of the raw roller, the degree of its fibrousness and density. However, gining up to a certain limit is determined by the amount of raw cotton supply to the working chamber of the gin, i.e. the greater the supply of raw cotton to the working chamber, the greater the productivity of the gin. At the same time, with an increase in the supply of raw cotton to the working chamber, i.e. with an increase in the productivity of the gin, the mass of the raw roller and its density increases [12].

The effect of cotton temperature on the technological processes of primary cotton processing has not been sufficiently studied. During cotton ginning, changes in its temperature influence properties such as fiber length, strength, elasticity, and moisture content. These are considered important factors in the process of separating fiber from seeds.

Despite the fact that a number of studies have studied the density of raw gin roller, its exact numerical values and limits have not been determined. Many studies have cited the causes of fiber defects, but the change in the number of short fibers in the fiber content has not been sufficiently studied.

The Short Fiber Index (SFI) refers to fibers less than 0.5 inches (12.7 mm) long. It is known that short fibers are separated into waste in the preparatory process for spinning, as a result of which the amount of waste exceeds the norm. The fact that this figure ranges from 2% to 20% is emphasized in a number of works [13].

It is known that the temperature of the raw cotton fed to the saw gin, along with the improvement of the ginning process, affects the fiber length indicators [14].

RESULTS AND DISCUSSION

To study the effect of raw cotton temperature on fiber length indicators, the ginning process was carried out using the DL-10 laboratory equipment after heating the cotton to 10°C, 30°C, and 60°C in the SXL-3 laboratory device. The experiments were conducted in 3 repetitions. The length indicators of the obtained fiber samples were determined in the HVI-1000 system (Figs. 1 and 2).

FIGURE 1. Time variation of fibre length during ginning of raw cotton at different temperatures
1- cotton at a temperature of 10 0C; 2- cotton at a temperature of 30 0C; 3- cotton at a temperature of 60 0C

In Figure 1, a reduction in fibre length was observed in all variants. However, within 15 seconds of starting the ginning process, the fibre length at raw cotton temperature of10 0C was 1.13 in. and when the raw cotton was heated to 30 0C, the fibre length increased to 1.147 in. and at 60 0C, the fibre length increased to 1.151 in.

FIGURE 2. Time variation of short fibre fibre index during ginning of raw cotton at different temperatures
1-cotton at a temperature of 10 0C; 2-cotton at a temperature of 30 0C; 3-cotton at a temperature of 60 0C

As can be seen from Figure 2, during the ginning process at raw cotton temperature of 10 0C, the number of short fibres in the fibre separated during the first 15 seconds was 7.1%, and at raw cotton temperatures of 30 and 60 0C, the number of short fibres in the fibre decreased by 6.8 and 6.5%, respectively. According to the results of experiments it was established that when cotton is fed into the ginning process its temperature should be within 30-35 0C, and such quality indicators of the produced fibres as fibre damage, staple length of fibre, index of short fibres in the fibre composition are at the level of the established norms.

Considering the positive effect of cotton temperature at 30-350C on fiber length indicators during the ginning process, experimental production tests were conducted to determine the influence of raw material roller density on fiber length characteristics.

Scientific research was carried out on the 4DP-130 gin equipment installed at the Buka cotton gin plant in order to study the effect of the density of the raw roller and the state of the gin seed comb on the increase in short fibers in the fiber composition. Experimental studies were carried out on raw cotton of the C65-24 variety, first grade, with a moisture content of 7.2%, a clogging content of 1.8%, which was cleaned according to a regulated technological process before gining. The research experiment began with a gin capacity of 6 kg/ saw.hour, and the position of the seed comb was 200.The start of work was recorded using a stopwatch, after 30 minutes from the place of transition from the gin to the fiber cleaner , 100 g of fiber was taken as a sample in three repetitions. After the samples were taken, the gin was stopped. To determine the density of the raw gin roller, it was necessary to open the front apron of the gin, where a 100 mm wide sample is cut from three places along the entire length of the raw roller using a special device that was prepared in advance.

After samples were taken for analysis, the raw roller of the gin was unloaded, that is, the working chamber of the gin was cleaned and the operability of the working parts of the gin was checked. The genie was restarted with the position of the seed comb at 440 relatives to the horizontal axis. After 30 minutes, samples were taken for analysis, as indicated above. The experiment was also carried out with the position of the seed comb at 660.

Experiments were also carried out with a capacity of 6.6 and 11 kg/saw.an hour with the above method of three positions of the seed comb in 200, 440 and 660. The obtained fiber samples were tested for the short fiber index (SFI) and fiber staple length (len) in the HVI system, which determines 14 indicators of cotton fiber.

Before measuring the properties of cotton fiber, the HVI system must be in standard climatic conditions: air temperature (21±)0C and relative humidity (65 ±)%-0.1 0C on the scale of the Astman psychrometer or using devices for measuring air temperature and humidity equivalent to its accuracy. Samples taken in accordance with the state standard “O'zDst-614” for measurement should have a humidity ratio of 6.75% to 8.25% [15].

The HVI 1000 system must be calibrated in accordance with the operating instructions, standard samples and samples. Calibration is recommended to be carried out twice a day, before starting work and every 4-5 hours after work. Calibration of the HVI 1000 system in terms of micronaire, high average length, length uniformity coefficient, short fiber index, fiber maturity (relative tensile strength) is carried out using standard cotton fiber samples at the beginning and the last two points of the measurement criterion.

FIGURE 3. Change in the density of gin raw valig by the state of the seed comb
1. 6 kg/ saw.hour; 2. 8 kg/ saw.hour; 3. 10 kg/ saw.hour

For the reliability of the experimental results, each experiment and laboratory analysis were carried out in three repetitions. The results obtained are shown in the form of a histogram in Fig.3 and 4.

As can be seen from Figure 1, when the gin capacity was 6 kg/saw.an hour with the position of the seed comb at 200, the density of the raw roller was 385.5 kg/m3 and with the same productivity in the position of the seed comb 440 and 660, the density of the raw roller decreased from 350.5 kg/m3 to 293.4 kg/m3, respectively.

FIGURE 4. Fiber by length uniformity index (Unf)
1. 6 kg/ saw.hour; 2. 8 kg/ saw.hour; 3. 10 kg/ saw.hour

There was also observed a normalisation of the density of the raw material roll with increasing angle of opening of the seed comb of the gin relative to the horizontal at productivity of 6 and 10 kg/saw-hour. At the same time, the increase in gin productivity led to a decrease in fibre yield. The analysis of fibre samples obtained at 3 different saw gin capacities and different seed comb positions is shown in Figures 2 and 3.

The analysis of fibre samples in HVI-1000 system showed that at a gin capacity of 8 kg/saw.hour and gin seed comb position at 200 the fibre uniformity index was 82.1%, and at seed comb positions at 440 and 660 we can observe an increase in this index from 82.8% to 83.2% (Fig. 5). The fiber uniformity index is expressed as a percentage, determined by the ratio of the average fiber length to the high average length. The uniformity index should be on average above 80%.

FIGURE 5. Short fiber index up to 12.7 mm
1-6 kg/ saw.hour; 2-8 kg/ saw.hour; 3-10 kg/ saw.hour

In the experimental variants, the best fibre length indexes were achieved at a gin productivity of 6 kg/saw hour and with the increase in the opening angle of the seed comb, the length uniformity index improved.

In turn, the short fiber index was 7.1% when the gin productivity was equal to 6.6 kg/saw.an hour, and the position of the seed comb is 200. However, with the same performance in the position of the gin seed comb in 440 and 660, the short fiber index decreased from 7.1% to 6.6% (figure 5).

CONCLUSION

The conducted experimental studies demonstrated that the density of the raw cotton roll and the position of the seed comb have a significant impact on the short fiber content in cotton fiber. An increase in the seed comb angle led to a reduction in raw roll density and, consequently, a decrease in the short fiber index. The optimal raw roll density can reduce the proportion of short fibers by 15–20%, which improves fiber length uniformity and reduces production waste. Increasing the gin’s productivity without considering the density of the raw roll may lead to deterioration in fiber quality. The optimal parameters for reducing fiber defects are: productivity of 6 kg/saw.hour, seed comb angle of 44–66°, and cotton temperature of 30–35°C. Preheating the cotton before ginning also contributes to lowering the short fiber percentage and increasing the staple length. It was found that at a cotton temperature of 60°C, the short fiber index was minimized — at 6.5%. The obtained data confirm the necessity of precise adjustment of the gin’s technological parameters. This will improve fiber structure, enhance its quality, and reduce waste. It is also important to consider fiber moisture prior to testing to ensure the reliability of results. Reproducibility of experiments and laboratory analyses increases the reliability of the conclusions. The proposed recommendations are applicable in industrial cotton ginning plants. Further research will allow for accurate determination of the optimal relationships between gin parameters and fiber quality characteristics. Thus, this study makes a significant contribution to improving the sustainability and efficiency of textile production.

REFERENCES

- Jing-shan TIAN “Fiber damage of machine-harvested cotton before ginning and after lint cleaning” Journal of Integrative Agriculture Volume 17, Issue 5, May 2018, P. 1120-1127.

- Azimjon Parpiyev, Ilkhom Sabirov, Alisher Usmankulov, Nodir Navruzov “Study of the Influence of Main of the Regenerator Ginning Machine on the Qualitative Indicators of the Fibers and Seeds” E3S Web of Conferences ICECAE 2021-p.304.

- Coordinated technology of cotton production (PDI 30-75-2017).

- Parpiyev. Improvement of Saw Ginning. Int. J. Edvanced Research in Science, Engineering and Technology 5 (9).

- A. Parpiev, N. Navruzov, K. Yakubov. Analysis of residual fiber of ginned cotton seeds. Modern Science: Current Issues, Achievements and Innovations, 72-75.

- Parpiyev., N.Navruzov. The analysis of residual fibration of seeds after saw ginning. European Science Review, 253-258.

- Parpiyev A. et al. Study of the Influence of Main Parameters of the Regenerator Ginning Machine on the Qualitative Indicators of the Fibers and Seeds //E3S Web of Conferences. – EDP Sciences, 2021. – Т. 304. – С. 03001.

- Azimjan P., Nodir N. The analysis of residual fibration of seeds after saw ginning //European science review. – 2018. – №. 7-8. – С. 253-258.

- Qaxramonovich S. I., Parpiyevich P. A., Djuraevich D. A. Modeling of dynamics of movement of fibres ulyuk a clap on a forward side of a tooth saw the cylinder of gin of the second step //European science review. – 2016. – №. 5-6. – С. 195-197.

- Tillyaev M.T. “Research on the influence of the raw material roller rotation accelerator on the main indicators of the ginning process.” Diss. Cand. Sci. (Eng.), Tashkent, 1974, p. 145

- Rashida Ergasheva, Jamoliddin Ergashev, Juramirza Kayumov,Bakhromjon Dadamirzaev “Study of the Effect of Air Flow on the Release of Bare Seeds from the Working Chamber of the Saw Gin” International Journal of Advanced Science and Technology 04 IJAST

- Mukai Y., Suh M. Design and characterization of a cotton fabric antenna for on-body thermotherapy //Journal of Industrial Textiles. – 2022. – С. 15280837221107160.

- Zhou, C., Dong, J., Zhang, S., Zhang, Q., Wang, M., Zheng, L., ... & Jiang, W. (2022). Classification of waste cotton from different countries using the near-infrared technique. Textile Research Journal, 00405175221116059.

- Dash, Ashwini Kumar, and Sanat Kumar Sahoo. "Role of Enzymes in Textile Processing." Bioprospecting of Enzymes in Industry, Healthcare and Sustainable Environment. Springer, Singapore, 2021. 395-410.

- Navruzov N.A., Eshmurodov D.D., Yakubov K.N., Abdumazhidov A. (2022). The influence of cotton structure on gin productivity. Universum: technical sciences, (7-2 (100)), 35-38.